## Slide 1: Cortex Structure
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Janelle Hocking Edwards, The University of Western Australia.
Notes: This module describes the structure of the cortex of fibres. There are photomicrographs and descriptions of individual cortical cells and the different types of cortical cells that form the cortex. For more detailed descriptions see the modules “Detailed Cortex Structure” and Cortex Formation”
Useful reference: Chapman, R.E. and Ward, K.A. (1979) In: Physiological and Environmental Limitations to Wool Growth. Eds.: Black, J.L. and Reis, P.J. UNE Publishing Unit, Armidale, NSW, Australia.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Janelle Hocking Edwards, The University of Western Australia.

## Slide 2: Cortex
long, thin cells with finger-like ends
  the ends interlock
cell membrane complex holds the cells of the fibre together
finger-like
end
nuclei
2 cells
Janelle Hocking Edwards
Notes: <number>
<footer>
Written by: Dr. Janelle Hocking Edwards, The University of Western Australia.
Cortex consists of tightly packed, elongated cells (80-100µm long; 3-6µm wide). These cells are cemented together by cell membrane complex.
This photomicrograph shows individual cortical cells that have been released from the fibres from strongwool Merinos by formic acid. Note the projections on the ends of the cells, the degraded nuclei and how some cells are still attached end to end.

## Slide 3: Cortical cell types
cortical cell types
  orthocortex (O)
  paracortex (P)
  mesocortex
  metacortex
Follicle
Fibre
(20µm)
O
P
Janelle Hocking Edwards
Notes: Written by: Dr. Janelle Hocking Edwards, The University of Western Australia.
There are a number of cortical cell types that have different properties:
Orthocortex has less sulfur than paracortex and the intermediate filaments are arranged in a whorl-like pattern
Paracortex has a high sulfur content and the intermediate filaments are arranged in a hexagonal pattern
Mesocortex is intermediate between ortho- and paracortex and occurs in lambs wool.
Metacortex contains cells that are more basophilic than orthocortical cells and is present in Southdown and Corriedale wool.
This photomicrograph shows staining patterns of ortho and paracortex in a strongwool Merino. The skin has been stained with methylene blue which stains the paracortex blue and leaves the orthocortex unstained. Also note that the cuticle stains blue.

## Slide 4: Variation in cortical structure
Fine wool <25µm
Bilateral segmentation
Cuticle
Cortex
Medulla
Orthocortex
Paracortex
Broad wool; >30µm
Radial/concentric segmentation
Metacortex
more basophilic than ortho.
Mesocortex
intermediate between ortho. and para
Janelle Hocking Edwards
Notes: <number>
<footer>
Written by: Dr. Janelle Hocking Edwards, The University of Western Australia.
This slide summarises the different components of the fibre and highlights possible differences in gross morphology of the fibre, in particular:
  The presence or lack of a medulla
  The distribution of orthocortex and paracortex
  Different characteristics of the cortex type.

## Slide 5: Ortho- and para-cortex patterns in wool fibres
Primary follicle
Bilateral
Suint
gland
Orthocortex (clear)
Diffuse
Bipolar
Paracortex (dark)
Janelle Hocking Edwards
Notes: Written by: Dr. Janelle Hocking Edwards, The University of Western Australia.
This photomicrograph shows staining patterns of ortho and paracortex in a strongwool Merino.
Note the predominantly bilateral staining of the finer fibres but more unusual patterns such as diffuse and bipolar in the broader fibres.
There is only one primary follicle in this view and many secondary follicles.