## Slide 1: Chemical Bonding in the Fibre
Produced for the CRC for Premium Quality Wool undergraduate program by;
Kevin Ley, CSIRO Textile & Fibre Technology.
Notes: <number>
<footer>
Each intermediate filament consists of large numbers of so-called low-sulfur protein molecules, which are single protein chains, arranged in a specific manner. The individual low-sulfur protein molecules interact with each other to form pairs of protein chains or dimers. In turn, the dimers interact with each other to form tetramers. Within the intermediate filament large numbers of tetramers are arranged end to end thereby constituting a long subfilament; the tetramer, with its four constituent protein chains, is regarded as the repeating unit in the longitudinal direction. A small number of subfilaments, probably eight, are bundled together side by side in a cylindrical arrangement, with a certain stagger between them in the longitudinal direction, to form the intermediate filament.
This module contains a number of questions and answers to test the understanding of the structure of the mammalian hard a-keratins which is covered by information contained in the modules “Keratin Structure”, “The molecules of the wool intermediate filaments”, “Dimers of Intermediate Filaments”, “Tetramers of Intermediate Filaments” and “Subfilaments of Intermediate Filaments”.
Produced for the CRC for Premium Quality Wool undergraduate program by Kevin Ley, CSIRO Textile & Fibre Technology.

## Slide 2: Exercise
When a wool fibre is extended it first offers stiff resistance, then it gives somewhat, then it stiffens again and finally breaks.
1. What could be happening to the IF’s in
  a) the initial phase, and
  b) the middle phase?
2. What could be the role of the inter-tetramer S-S bonding within the subfilament during extension?
3. What could be the role of S-S which might connect HS protein chains in the matrix to LS protein chains in the IF’s?
Kevin Ley
Notes: <number>
<footer>
Written by: Kevin Ley, CSIRO Textile & Fibre Technology.
1. In the initial phase (the stiff Hookean region of the stress-strain curve), the -helical regions of the low-sulfur protein chains act as stiff springs, where the -helical conformation of the protein chains is maintained by hydrogen bonding between successive turns of the -helical springs. In the middle phase (the Yield region of the stress-strain curve, where the fibre gives somewhat), the applied force has become so great that the hydrogen bonds maintaining the -helical conformation are stressed so much that these bonds break, and so the individual turns of the -helical springs are pulled apart. However it is possible that some of the -helical regions in the low-sulfur protein chains are protected from the applied force by disulfide bonding between the low-sulfur protein chains and the high-sulfur protein chains, and that these protected -helical regions do not open up until the applied force becomes even greater, in the Post-Yield region of the stress-strain curve, when the fibre stiffens up again.
2. Obviously if disulfide bonding occurs between linearly adjacent tetramers in a subfilament (whether this bonding occurs between overlapping -helical 2B regions from each tetramer, or whether the bonding links non-helical tail regions from each tetramer), then such disulfide bonding helps to maintain the integrity of the subfilament as it is extended during the extension of the fibre.
3. If low-sulfur protein chains in the intermediate filaments are disulfide linked to high-sulfur protein chains which are themselves stabilised by further disulfide bonding (both intra-chain and inter-chain?) within the high-sulfur protein matrix, then the whole disulfide bond network helps to protect the intermediate filaments from breaking down when force is applied to pull the two ends of the fibre apart.

## Slide 3: Exercise
Water swells the fibre.
  Water does not penetrate and swell IF’s.
    Why?
  Most of the swelling due to water penetration occurs in the matrix.
    How is this fact relevant to the question of whether the disulfide bonding in the matrix is intermolecular or intramolecular?
Kevin Ley
Notes: <number>
<footer>
Written by: Kevin Ley, CSIRO Textile & Fibre Technology.
The close packing of the protein chains within the various organisational levels of structure within the intermediate filament helps to exclude water. Moreover, the exclusion of water will be particularly effective for the coiled-coil region of the dimer, where the adhesive contact region between the two coiled -helices is comprised only of apolar sidechains contributed by the two facing -helices.
A three dimensional network of inter-chain disulfide bonds within the matrix is likely to help restrict bulk swelling of the matrix. Bulk swelling will not be restricted so effectively if the disulfide bonding is intra-chain. Note also that, quite independently of the observation of swelling in the matrix (based on X-ray diffraction), amino acid sequence data for a number of high-sulfur proteins suggest that the positioning of the half-cystine residues, within the sequences of the amino acid residues in the protein chains, is such as would favour intra-chain disulfide bonding.