## Slide 1: Follicle Shutdown and Staple Strength
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Tony Schlink, CSIRO Animal Production.
Notes: <number>
<footer>
Primitive sheep have a photoperiod driven follicle cycle that leads to an annual shedding of the fleece. However, Merino shedding appears to be driven by nutrition rather than photoperiod, but the role of photo-period should not be ignored. It is important to be aware of follicle shutdown as it results in a reduction in staple strength and the possible loss of fibres from the fleece. Better breeding and nutrition will help prevention of shedding
This module describes the relationship between follicle shutdown and staple strength.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Tony Schlink, CSIRO Animal Production.

## Slide 2: Fibre Ends
BROKEN FIBRE SHED FIBRE
Tony Schlink
Notes: <number>
<footer>
Written by: Dr. Tony Schlink, CSIRO Animal Production.
These scanning electron micrographs show the difference between fibres that have been broken and fibres that have been shed from the follicle. The magnification of the photos are different and both fibres actually have the same fibre diameter at the point of break. When examining staples and fleeces for shed fibres, the staples are washed in a solvent and dried, then stained with picric acid (yellow) and eosin (pink). The fibres are then examined with a microscope and the proportion of fibres with inner root sheath (IRS) (which stains pink) still attached to the fibre are estimated. These fibres have been shed from follicles which have shutdown and look like the fibre in the right hand photo.

## Slide 3: Effect of fibre shedding on staple strength
Tip
Base
Tony Schlink
Notes: <number>
<footer>
Written by: Dr. Tony Schlink, CSIRO Animal Production.
This diagram illustrates how shed fibres decrease staple strength. The shed fibres contribute to the weight of the staple which influences the linear density (ktex) but does not contribute to the force required to break the staple (Newtons) as shed fibres are already discontinuous. So staple strength (N/ktex) is decreased as the numerator is lower and the denominator is higher.

## Slide 4: Relationship between fibre shedding and staple strength
Shedding (%)
Staple Strength (N/ktex)
Tony Schlink
Source: Schlink, T.
Notes: <number>
<footer>
Written by: Dr. Tony Schlink, CSIRO Animal Production.
Adapted from Schlink, A.C. and Dollin, A.E. (1995) Wool Technology and Sheep Breeding 43, 268-284.
This graph shows the relationship between staple strength and the proportion of shed fibres in the staple. There is a an exponential decline as shedding decreases, staple strength increases. If there are more that 10% shed fibres in the staple, the staples would be considered tender, however, if there are less than 10% shed fibres in the staple, staple strength can vary from rotten to very sound. This suggests that shedding does affect staple strength but it is not the only cause. Changes in fibre diameter along the staple is usually the major component of staple strength change.
In Merino sheep, the incidence of shedding under normal grazing conditions is generally low (<1%) and linked more to seasonal changes in feed, physiological condition and stress. However, Schlink and Dollin (1995) found the incidence to range from 0 to 30% in adult Merino wethers in the Mediterranean environment of WA, under conditions resulting in body weight loss during late summer. Those wethers with high levels of shed fibres produced the lowest staple strengths. But note that at levels <5% shed fibres, staple strength still ranged from as low as 20 to as high as 60 N/ktex. So obviously other causal factors are involved.
(adapted from Crook B, 1999, Wool Production, CRC for Premium Quality Wool Lecture Series).