## Slide 1: Optical Fibre Diameter Analyser: Medullation Measurement
Produced for the CRC for Premium Quality Wool undergraduate program by;
Mark Brims, BSC Electronics Pty Ltd., and
Dr. Peter Auer, The University of New South Wales.
Notes: This module examines the measurement of fibre medullation or opacity by the Optical Fibre Diameter Analyser (OFDA).
For information on the components of the OFDA measurement system see the module “Optical Fibre Diameter Analyser: Measurement of Fibre Diameter”.
Produced for the CRC for Premium Quality Wool undergraduate program by Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.

## Slide 2: Opacity measurement
OFDA option to estimate medullated & flat fibres
no extra sampling or measurement
Mark Brims & Peter Auer
Source: http://www.ofda.com
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
Source: http://www.ofda.com/products.htm
The OFDA is the first automatic instrument to measure fibre opacity and fibre curvature. Fibre opacity directly measures the ability of each fibre to transmit light, and is determined by the fibre’s shape, internal structure, colour and surface quality. In white animal fibres, the main cause of opacity is medullation (hollow fibres). Medullated fibres stand out in a dyed cloth since they reflect light differently. For more information on medullation see module “Dark Fibre: Medullated Fibre”
If the opacity option in the OFDA software is enabled then the measurement of medullation occurs simultaneously with fibre diameter and fibre diameter distribution measurement. There is no extra sampling or measurement process involved.
The estimation of medullation is included with the OFDA’s histogram data of mean fibre diameter (MFD), standard deviation of FD, coefficient of variation of FD, prickle factor, spinning fineness and curvature (if curve option is enabled).

## Slide 3: Field Images
Bright Field
Dark Field
Medullated fibres
appear dark
Mark Brims & Peter Auer
Source: http://www.ofda.com/latest.html
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
Source: http://www.ofda.com/latest.html
As OFDA scans the slide containing the fibre snippets it obtains a dark field image and the normal bright field image almost simultaneously. The program analyses the bright field image as normal and then overlays the position of the detected fibres onto the dark field image. From the dark field image, the light transmitted by the fibre is measured and the opacity of this fibre is calculated and stored. If the opacity exceeds a pre-set threshold then this fibre is marked as medullated.
Flat fibres transmit light because they are hollow and have collapsed. They are easily identified as distinct from non-collapsed medullated fibres because they have a wide band of light that often is as wide as the fibre. OFDA can identify the 3 groups of fibres; flat, medullated and non-medullated. Flat fibres are classed as a sub-group of medullated fibres and included in the number of medullated fibres.

## Slide 4: Standard
IWTO-57-96
  Determination of medullated fibre content of wool and mohair samples by opacity measurements using OFDA
Mark Brims & Peter Auer
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
The above IWTO standard for the measurement of medullated fibres using OFDA is now a full test method.

## Slide 5: Fibre Diameter histogram with medullation option
Mark Brims & Peter Auer
Source: Brims. M.A. (1994)
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
Source: Brims, M. A. (1994) Measuring Fibre Opacity and Medullation using OFDA: Theory and Experimental Results on Mohair, IWTO, New Delhi, March 1994, Report No: 21.
The distribution of medullated fibres can be seen as the darker lines overlaying the diameter distribution.

## Slide 6: Opacity histogram
Mark Brims & Peter Auer
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
This slide is an example of an Opacity distribution histogram produced by the OFDA instrument.

## Slide 7: Further information
http://www.ofda.com/latest.html
Mark Brims & Peter Auer
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.