## Slide 1: The Measurement of Hauteur (H) and CVH
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: <number>
<footer>
This module defines Mean Fibre Length in the top and how this relates to Hauteur and Barbe. Measurement of average length of fibre in a top is covered.
The significance of this measurement and other derived measurements such as coefficient of variation of Hauteur (CVH) in the spinning operation is also covered.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Top Properties
Diameter
% fibres >30um
Hauteur
CV Hauteur
Evenness
Linear Density
Regain
Invoice Mass
Colour
VM Count
Nep Count
Oil Content
pH
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The list on this slide is an array of the top properties that topmakers are trying to match to their customers needs.
The average fibre length of the top (also known as Hauteur and commonly shortened to H), and the spread of that measurement, (called the Coefficient of Variation of Hauteur, CVH) are important parameters in the topmaking operation.

## Slide 3: Standards
Comb Sorter
  IWTO-1-59(E): Method of determining ‘Barbe’ and ‘Hauteur’ for wool fibres using a Comb Sorter.
Fibre Diagram Machine
  IWTO-16-67(E): Method of test for wool fibre length using WIRA Fibre Diagram Machine.
Capacitance (Almeter)
  IWTO-17-85(E): Determination of fibre length distribution parameters by means of the Almeter.
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
There are several standards which are used for the measurement of the mean fibre length in tops.
The Comb Sorter is labour intensive and subject to some operator bias, since it is a manual operation to some extent.
The WIRA Fibre Diagram Machine is a long established instrument used in textile testing laboratories around the world for the determination of mean fibre length and distribution.
The use of capacitance has been developed by Centexbel, a Belgian research company, and marketed by the Peyer company as the Almeter machine.

## Slide 4: Definition
Mean Fibre Length
MFL =  [n(i)L(i)] /  n
estimate n
  using weights of different fibre length groups
  using capacitance sensor
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Mean fibre length (MFL) is defined by the formula on this slide (i.e. the number of fibres of each length multiplied by each length divided by the total number of fibres. This formula requires knowledge of the number of fibres of each length.
This number of fibres can be estimated using the weights of fibre length groupings, e.g. the comb sorter was the original apparatus for measuring fibre length, starting from the tip of an aligned tuft, fibres were separated into length groups and weighed.
A more modern technique utilises the principle of capacitance to estimate the number of fibres.

## Slide 5: Hauteur and Barbe
H =  [A(i)L(i)] /  A(i)
  A(i) cross-sectional area of each length group
  linear density bias
  cross sectional area bias
B =  [ W(i)L(i) ] /  W(i)
  W(i) weight of each length group
  weight bias
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
MFL can be expressed either as Hauteur (H) or Barbe (B). These terms are calculated according to the above formulae.
These formulae would be used if a manual determination of H and B were performed.
H is derived by dividing the total weight of fibre by the sum of the weight of each length group divided by the length of each group.
H= W(i) / [W(i) / L(i)]
Since fibre cross-sectional area (A) is equivalent to linear density, which is weight (W) divided by length (L), H can be expressed as shown in above formulae.
B is derived by first summing the product of the weight of each length group by the length of each group. This product (of weight and length) is then divided by the total weight of fibre.
If fibres were the same linear density, H and B would be equivalent.
But wool fibres are NOT all the same linear density. The linear density of coarse fibres (which tend to be longer) is greater than that of finer fibres (which tend to be shorter), therefore H is said to be length or cross-sectionally biased.
However, B is always greater than H for wool fibres.
The Almeter measures H using capacitance measurement, and calculates B.
Conversion: B = H (1+(CVH)2)

## Slide 6: WIRA Fibre Diagram Machine
Peter Auer
Source: ‘The WIRA Directory”, 1999
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The WIRA Fibre Diagram Machine is universally suited to processors of natural and synthetic fibres. The WIRA Fibre Diagram Machine test is approved by IWTO as detailed in the IWTO standard, IWTO-16-67.
The top sample to be measured is clamped in a sealing unit. A squared end is then produced by removing the protruding fibres with a special grip. The squared end of the fibres are then bonded to a strip of plastic tape and gentle pulled away. Once a fibre draw has been prepared from a sample of top, the testing operation is automatic. The machine transports the fibre draw through the measuring head and transmits data to a computer. The computer generates calculations of mean fibre length and coefficient of variation of fibre length and can be printed out together with a graph of the fibre diagram.

## Slide 7: Almeter: Grip
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The Almeter provides a direct measurement of Hauteur. The apparatus consists of two parts, the Grip and the Sensor.
The sample is prepared in the Grip (this can be manual or automatic). After fibres are withdrawn in tufts from the cut end of a top, they are aligned such that every fibre has one end at the base of the beard. This means that the Sensor knows when the end of all fibres has been reached during the measurement phase.
The sliver to be measured is 15-30 kilotex. 30-40 passes are made in the Grip at start-up which "squares out" the sliver end such that a representative tuft is withdrawn during preparation of the sample. The final sample must be representative of the length classes in the original sliver or roving. The number of passes for a proper beard can vary; an adequate sample will be approx. 15 passes.

## Slide 8: Almeter: Sensor Apparatus
Beard of
fibres
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The prepared sample is then transferred to the Sensor measuring apparatus which has undergone a zero run. The Sensor apparatus measures changes in capacitance caused by a prepared wool sample passing over the sensor. The measured signal from the Sensor is proportional to a cumulative Hauteur diagram. Changes in the signal for each fibre grouping can be related to the number of fibres in that grouping. A direct readout of Hauteur is obtained from the Sensor.
The following results are calculated: CVH, B, CVB, %longer /shorter, length exceeded by % fibres.
(NB capacitance measurements are influenced by moisture changes, therefore the regain of the test specimen must be controlled).

## Slide 9: Hauteur Diagram
2.5%
5.0%
7.5%
10.0%
Histogram
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
This is an example of the diagram obtained from the Almeter. There are two graphs plotted on the page.
The dotted line is the Hauteur diagram which is a cumulative percentage diagram. The units for this diagram are shown on the left Y-axis.
The squared line is the Hauteur histogram. This denotes the frequency of each length group. The units for this are shown in the right Y-axis. However this axis is not usually shown, but is dented by “Full Scale Histogram 12.5%”.
The X-axis represents the length groups broken into 5mm groupings. This is peculiar to the measurement of long staple fibres. Short staple fibres such as cotton use different length groupings.
Commonly the MFL expressed as Hauteur is calculated, along with CVH, and some other parameters designating the % of fibres less than certain lengths, and the length exceeded by certain % of fibres.
Exercises
What % of fibres are less than 100mm? (100 - 20 = 80%)
What % of fibres are between 60 and 80mm? (59 - 40 = 19%)
What length do 20% of fibres exceed? (100mm)
What does L 1% mean? (1% of fibres > 144.5mm)

## Slide 10: Practical Aspects of H and B
Hauteur (H)
CVH
%<40mm
%<25mm
%<15mm
L 5%
L 1%
CV Barbe
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Hauteur is used in yarn spinning since this can indicate the number of fibres in each length group. Research has shown that increasing H can improve spinning performance and evenness.
Coefficient of variation of Hauteur (CVH) is a measure of the scatter of the fibre length distribution. By definition the length grouping which are CV% either side of H encompass 66% of the fibres. An optimum of 42-52% CVH is an industry practice that is being challenged at present.
%<40mm is a standard IWTO value used in the trading of tops. A value of 10-50% is acceptable depending on the application.
%<25mm is used to judge combing performance. An industry standard is 8%. Very good combing performance would return a figure of 2%. If a figure of >16% was found, recombing would be necessary.
%<15mm is the figure used to judge spinning performance. It is fibres in length groupings which will lead to problems with breakage in spinning, as well as problems with yarn evenness. Some of these problems are referred to as slubs or thick and thin places.
L 50% is the median fibre length value.
L 5% used to adjust drawing system (short staple) and L 1% is used to adjust drawing system (long staple). The drawing system is that used immediately before twisting. If fibres are too long here they will be caught in both sets of rollers and be broken.
Some Barbe figures are used in spinning. A CVB of 30-33% indicates that the highest draft possible can be used. %<25mm indicates how much weight of fibre will be lost in re-combing.