## Slide 1: Associations Involving Fibre Curvature
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module presents phenotypic correlations involving mean fibre curvature and curvature variation.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Fibre Curvature: phenotypic associations
Fine
Merino
1
Fine
Merino
2
Peppin
Merino
3
Multiple
Breeds
4
Average curvature
& crimp frequency
0.54
0.85
-
0.95
CV% curvature
& crimp definition
0.14
-
0.05
-
SD curvature
& SD diameter
0.04
-
-0.06
-
1. Nivison et al. (unpub); 2. Nimbs et al. (1998);
3. Crook (unpub.); 4. Edmonds (1997)
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Sources:
Nimbs, M.A., Hygate, L. and Behrendt, R. (1998). Proc. Aust. Soc. Anim. Prod. 22: 396.
Edmonds, A. (1997). Wool Tech. Sheep. Breed. 45: 227.
Fibre curvature represents a relatively new and cheap fibre measurement, with measures of mean curvature and curvature variation being available. But what exactly do these measurements reflect?
Mean fibre curvature shows a relatively strong relationship with crimp frequency, although the relationship appears to be lower in finer wool types.
Given that there is a relationship between fibre length and fibre crimp frequency, such that faster growing fibres generally have a lower crimp frequency, high length variation could reduce crimp definition due to high variation between fibres in crimp frequency. Curvature variation has therefore been put forward as a measure of crimp definition. However the relationship does not appear to be strong. Furthermore, if the link to crimp definition is by way of length variation, then a relationship between curvature variation and diameter variation should be expected, as length and diameter are positively correlated within the fleece. Evidence to date indicates that curvature and diameter variation are not correlated.