## Slide 1: Competing Fibres “Shingosen”
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module presents examples of recent developments in synthetic fibre technology as applied to consumer apparel products.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Profiles
Source: Okamoto, M. & Kajiwara, K. (1995)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Okamoto, M. & Kajiwara, K. (1995), Engineering Future Products: Prospects for Applications for the New Materials and Processing, Proc. 76th World Conference of the Textile Institute, The Textile Institute, p. 350
The development of various fibre profiles has been driven by the need to develop fabrics with different handle characteristics. Initially nylon and polyester fibres had a round X-section. Altering this changed the bending properties of the fibres.

## Slide 3: Ultra-fine filament
Source: Okamoto, M. & Kajiwara, K. (1995)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Okamoto, M. & Kajiwara, K. (1995), Engineering Future Products: Prospects for Applications for the New Materials and Processing, Proc. 76th World Conference of the Textile Institute, The Textile Institute, p. 352
The production of the fibres in these examples has utilised various methods to achieve ultra-fine filaments. Each method produces fibres with different X-sectional shape, different textures, and different linear densities.
The following slides contain m scales which give a idea of the extent of the diameter reductions achieved with this technology. Generally, the fibre profile and production method is evident from the slides.

## Slide 4: Suede-type artificial leather
Source: Okamoto, M. & Kajiwara, K. (1995)
Notes: Source: Okamoto, M. & Kajiwara, K. (1995), Engineering Future Products: Prospects for Applications for the New Materials and Processing, Proc. 76th World Conference of the Textile Institute, The Textile Institute, p. 351

## Slide 5: Peach Skin Type Shingosen
Source: Okamoto, M. & Kajiwara, K. (1995)
Notes: Source: Okamoto, M. & Kajiwara, K. (1995), Engineering Future Products: Prospects for Applications for the New Materials and Processing, Proc. 76th World Conference of the Textile Institute, The Textile Institute, p. 354

## Slide 6: New Silky Type Shingosen
Source: Okamoto, M. & Kajiwara, K. (1995)
Notes: Source: Okamoto, M. & Kajiwara, K. (1995), Engineering Future Products: Prospects for Applications for the New Materials and Processing, Proc. 76th World Conference of the Textile Institute, The Textile Institute, p. 355

## Slide 7: New Spun Type Shingosen
Source: Okamoto, M. & Kajiwara, K. (1995)
Notes: Source: Okamoto, M. & Kajiwara, K. (1995), Engineering Future Products: Prospects for Applications for the New Materials and Processing, Proc. 76th World Conference of the Textile Institute, The Textile Institute, p. 356

## Slide 8
Dry Touch Type Shingosen
Source: Okamoto, M. & Kajiwara, K. (1995)
Notes: Source: Okamoto, M. & Kajiwara, K. (1995), Engineering Future Products: Prospects for Applications for the New Materials and Processing, Proc. 76th World Conference of the Textile Institute, The Textile Institute, p. 357

## Slide 9: Major Reference
Okamoto, M. & Kajiwara, K. (1995), Engineering Future Products: Prospects for Applications for the New Materials and Processing, Proc. 76th World Conference of the Textile Institute, The Textile Institute