## Slide 1: Prediction of Spinning Performance & Yarn Quality
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Lamb, CSIRO Textile & Fibre Technology.
Notes: This module examines how spinning performance and yarn quality can be predicted from fibre properties.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Lamb, CSIRO Textile & Fibre Technology.

## Slide 2: SIROLAN - YARNSPEC
wool top properties
  diameter
  CV diameter
  Hauteur
  Curvature
  bundle tenacity
yarn parameters
  count (tex)
  twist level
processing parameters
Best Commercial Practice
The Prediction of Spinning Performance and Yarn Quality
yarn tenacity
yarn elongation
yarn evenness
  thick & thin places, neps
ends-down in spinning
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile & Fibre Technology.
Sirolan-Yarnspec is a model that uses the inputs on the left of this slide to predict the important yarn production and performance parameters listed on the right of this slide.

## Slide 3: Best Commercial Practice
random limit due to probability
  mean number of fibres in yarn X-section
no one beats spinning limit
  determined by thin place breaks
  ~35 fibres in X-section
quality of yarn = quality of drafting
similar machinery used in mills
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile & Fibre Technology.
The Sirolan-Yarnspec modelling program utilises the concept of “best commercial practice”, which a good mill should achieve if no mistakes are made. This level of performance can be estimated because it is primarily determined by the statistical limit from a finite number of fibres in the yarn cross-section.
There are no devices in practice which control the number of fibres emerging from the front rollers of the drafting zone of the spinning frame. The probability of too few fibres being present is limited by the random statistics of the average number of fibres in the yarn cross-section. The commercial limit depends on the cost of labour to mend the breaks but is rarely below an average of ~35 fibres in the yarn cross-section.
In essence the quality of the yarn is a result of the quality of drafting that occurs in the drafting zone. All modern spinning frames are similar in this respect and no mills have special machinery that can allow significant improvements relative to their competitors.

## Slide 4: Prediction of Yarn Evenness
15
17
19
21
23
15
17
19
21
23
Measured Evenness CV %
Predicted Evenness CV %
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile & Fibre Technology.
This slide shows how well Yarnspec can predict yarn evenness.

## Slide 5: Prediction of Yarn Tenacity
4
5
6
7
8
9
4
5
6
7
8
9
Measured Tenacity cN/tex
Predicted Tenacity cN/tex
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile & Fibre Technology.
This slide shows how well Yarnspec can predict yarn tenacity.

## Slide 6: Effect of Twist on Tenacity
0.6
0.7
0.8
0.9
1.0
1.1
60
70
80
90
100
110
120
130
Metric Twist Factor
Correction Factor
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile & Fibre Technology.
A well-known phenomenon in twisting is that yarn tenacity will increase with increasing twist up to a point. After this point the application of more twist will cause a decrease in yarn tenacity.
The Yarnspec model takes this phenomenon into consideration in its calculations.

## Slide 7: Fibre Bundle Strength
bundle strength staple strength
  better indicator of fibre strength
wool strength varies
  damaged by chemical treatments
    dyeing (esp. at high temp.)
    bleaching (not common)
affects spinning performance
10% increase reduces ends-down by 50%
SIROLAN - TENSOR
  measures bundle strength

Peter Lamb
Notes: Written by: Dr. Peter Lamb, CSIRO Textile & Fibre Technology.
Studies have shown that the inclusion of results for bundle strength improve prediction of yarn strength and spinning performance - as measured by ends-down. Bundle strength is measured on the top and differs from staple strength which primarily measures whether there is a thin place in the staple.
Normally, wool fibre strength does not vary much, unless the fibre has been treated chemically. This may occur to the fibre before spinning if tops are dyed, which is quite common, or bleached which is less common.
A 10% increase in bundle strength has been shown to improve ends-down by 50%.
Bundle strength is measured on an instrument called the Sirolan-TENSOR, which is illustrated on the next slide.

## Slide 8: SIROLAN - TENSOR
Peter Lamb
Notes: Written by: Dr. Peter Lamb, CSIRO Textile & Fibre Technology.
This machine consists of a set of jaws which hold the specially prepared bundle sample. The jaws are moved apart at a constant rate of extension. After breaking, the sample is weighed and the results are recorded and measured on a PC.
The relevant results gathered are bundle strength, and elongation which are used in the Yarnspec calculations.