## Slide 1: Later Stage Processing
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module is a brief overview of the later stage processes of fabric and garment manufacture, dyeing and finishing.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Weaving & Knitting
Weaving
  interlaced sets of yarns
Knitting
  weft knitting
    looped yarn
  warp knitting
    interlocked warp yarns
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Weaving is the interlacing of two sets of yarns on a machine called a loom. The yarns parallel to the fabric direction are called the WARP yarns. The yarns perpendicular to the fabric direction are called the WEFT yarns.
Depending on the manipulation of these yarns sets, the fabric formed can be quite endless. Warp yarns are able to be manipulated individually, although the machinery gets more complex. Usually the warp yarns are raised and lowered in sets to form a gap (“shed”) so that a weft yarn can be passed across the fabic width. The next warp movement traps the weft yarn, formimg the fabric. The fabric shown in this slide is the simplest interlacing called a plain weave.
The constant raising and lowering of warp yarns leads to high abrasion forces. These are overcome by either coating the warp yarns with a “size” to protect them. In usual practice the yarns are also plied yarns. For more information see the “Yarn Production” module. Modern looms use high speed weft insertion which places demands on the strength of the weft yarns.
Weft knitting is the interlooping of yarn on a knitting machine. The simplest weft knitted fabrics can use only one looped yarn. More complex fabrics use more yarns and more complex loops. The knitted fabric in this slide is the simplest weft knitted fabric. Weft knitting is the most common way of producing knitted apparel goods.
Another way of producing knitted fabrics is by warp knitting (not shown). In this technique parallel warp yarns are crossed over each other and interlaced to form a fabric. This technique is used in the production of some domestic textiles such as curtains. False lace effects are possible with this technique.

## Slide 3: Garment Make-up
convert fabric to garments
processes
    pattern-making
    laying out
    cutting
    sewing
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Garment Make-up is the process of taking finished fabric and converting it into garments, based on design patterns. The process includes such stages as laying out, cutting, and sewing.
This slide illustrates the laying out and cutting of fabric to a pattern. Multiple layers of the fabric are usually processed together. The latest textile cutting apparatus uses lasers to cut the fabric. Patterns can be generated using CAD/CAM software to maximise fabric usage and design patterns quickly.
The sewing process is mainly manual, and employs machinists to convert the 2D fabric into 3D garments.

## Slide 4: Dyeing
Peter Auer
aims
  even (difficult)
    batching
  permanent
  low fibre damage
conditions
  prolonged heat
  acid dyes (wool)
fibre damage
  strength loss
  fabric performance
blends
  polyester
    different dyes
    severe conditions
  nylon
    similar dyes
    similar conditions
    wool packs
low temp dyeing
  minimise strength loss
  Sirolan LTD
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The dyeing process aims to add colour to processed input by adding organic molecules which become intimately integrated into the fibre structure.
The science and development of dyes and dyeing technology is a complete couple of subjects themselves, and is beyond the present scope of this subject.
However, in most cases dyeing aims to be permanent, without unduly damaging the fibre. This has implications for blending, in that if one fibre requires conditions to be dyed which would lead to damage of the other fibre, then the dyeing of the fibres would have to occur separately.
A good example would be the blending of wool and polyester. Polyester is difficult to dye at conditions suitable for wool. The conditions required are far more severe, involving high temperature and pressure, and special dyeing agents and different dye molecules.
On the other hand nylon dyeing can be achieved at similar conditions to wool, using similar dyes and therefore the dyeing can be achieved in a blend, although care must still be taken with the relatively weak wool fibre where strength loss can be critical.
The similar dyeing behaviour of wool and nylon has been the reason that the composition of wool packs has changed from high density polyethylene (HDPE) tape, which is impossible to dye with current technology, to nylon multi-filament yarns.
The study of the conditions required to dye wool has lead to the development of Low Temperature Dyeing (Sirolan LTD) by CSIRO DWT. This process achieves successful dyeing of wool at relatively mild conditions, therefore avoiding much of the strength loss inherent in wool dyeing. Dyeing equipment needs to be controlled accurately for Sirolan LTD to be successful.

## Slide 5: Finishing
aims
  dimensional stability
  aesthetics
    handle
    drape
    cover
    surface
conditions
  heat
  water
  (chemicals)
processes
  crabbing
  decatising
  pressing
  milling
  raising
  shearing
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The finishing process aims to prepare the input for garment manufacture and ultimately consumer usage.
Finishing will improve the dimensional stability of the input, and also affect the aesthetics of the input, such things as drape, handle, coverage, surface properties.
In terms of the wool fibre, finishing is achieved with mainly water and heat, although some chemicals are used to augment the process, especially in Europe.
The basic changes that occur involve a relaxation of the forces inherent in a processed fabric by breaking the chemical bonds within the fibres, and changing the yarn configuration to a degree, and then setting the fabric by allowing new bonds to form.
The variety of machines used in wool finishing is fairly extensive. The processes are things like:
milling
crabbing
decatising
pressing
raising
shearing
Finishing remains somewhat of an “art”, although the chemical and physical processes are now quite well understood, and the ability to achieve good finishing should be in the reach of all finishers.