## Slide 1: Gilling
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module looks at Gilling as a process, explaining the features and functions of a gillbox.
The module also examines the separate but similar processes of Preparation Gilling, which prepares card slivers for combing, and Finisher Gilling, which is carried out on the combed sliver to form a worsted top.
It is recommended that the modules “Drafting” and “Evenness” are viewed before this module.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Typical Gillboxes
Intersector Gillbox
BACK ROLLERS
FRONT ROLLERS
C - working fallers, D - return fallers, J - funnel guide, K - press rollers
Chain gill
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Gilling is achieved using a machine called a gillbox. This slide shows two types of gillboxes commonly used in worsted processing, although generally modern mills would feature the more efficient chain gills.
These are both examples of long staple gillboxes. Since long fibres are being drafted, a fair degree of room is required between the rollers, since the longest fibres may be up to 140mm long. Also there must be room for an appropriate fibre control device which, in both cases, involves pins embedded in bars which lie across the machine. These bars are generally called “faller bars”.
The real difference between the devices lies in the movement of the faller bars. In an intersecting gillbox they travel on an endless worm drive in the space between the front and back rollers. The chain gill employs faller bars which travel on an endless chain. The chain gill is a lot faster and hence a more productive machine. The principles are the same.

## Slide 3: Gilling
Functions
  evenness modulation
    doubling
  drafting
    sliver attenuation
    roller drafting
  fibre control
  fibre blending / mixing
  fibre alignment
  fibre straightening
    hooks removed
Features
  input slivers
  positive feed
    minimise tension
  drafting zone
    ratch setting
  faller bars
    fibre control (pins)
  output sliver delivery
  cans
    sliver transport
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The functions of a gillbox are listed on this slide. A number of input slivers are doubled before being drafted between the front and back rollers. The doubling operation achieves the majority of the fibre blending and mixing, while fibre alignment and straightening is achieved when the fibres are moving forward and are “combed” by the pins in the faller bars.
Other features include the Ratch Setting which is the distance between the end of the faller bars and the nip of the front rollers. This can be adjusted to account for different mean fibre lengths. Longer fibres require a longer ratch setting.
The input slivers are fed into the gillbox by positive feeding to minimise tension, rather than being pulled into the gillbox. Any tension at this stage could lead to uncontrolled drafting of the slivers and subsequent evenness problems.
The output sliver (there is only one) must be delivered to the next process which can be another gillbox or the comb. This is achieved usually through a condensing funnel and calender rollers which take the output of the front rollers (again minimum tension is used) and place it in cans (tubes closed at one end). Later developments have seen the use of rail-road systems to minimise materials handling.

## Slide 4: Preparation Gilling
doffer
1st Gill
can
can
2nd Gill
can
3rd Gill
can
comb
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
A card sliver has a majority of trailing hooks caused by the action of the doffer removing fibres from the last card swift. However, leading hooks and hooks on both ends of the fibre are also possible. For more information see the “Worsted Card Features” and “Fibre / Pin Interaction in Carding” modules.
These hooks need to be straightened out as much as possible before combing to improve the combing efficiency. Poor fibre alignment can cause longer fibres than necessary to be combed out in this process.
Since trailing hooks cause less fibre breakage in worsted combing, (see the “Combing Principles” module), ideally the hooks that remain after gilling should be trailing hooks.
This will be achieved if there are an ODD number of gilling operations between carding and combing. The diagram on this slide illustrates this point.
As the sliver leaves the card and is put into a can, a phenomenon called “sliver reversal” occurs, i.e. the end of the sliver in the can becomes the leading end going into the next operation. This means that the trailing hooks become leading hooks and vice versa.
The combing action of fibres being dragged through the pins in a gillbox means that gilling straightens only trailing hooks, and therefore the 1st Gill will only straighten a few fibres.
After sliver reversal again between operations, the 2nd Gill will straighten more fibres, while the 3rd Gill and subsequent sliver reversal will mean that most fibres are straightened, but the remaining hooks are mainly trailing hooks.
Ideally fibres should be completely straight before combing. This doesn’t occur so the compromise position of remaining hooks trailing is illustrated above. Research has shown that adding more gilling operations improves fibre straightening, however there is an unacceptable processing cost involved compared to any saving in later fibre breakage. More neps are also generated.

## Slide 5: Finisher Gilling
regularisation
  linear density
    kilotex
  combed sliver properties
    cohesion
mixing / blending
regain adjusted
oils added
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Combed sliver has poor cohesive properties caused by the “open-end nature” of combing. The combed slivers are really overlapped tufts of fibres. The sliver cohesion needs to be improved by re-gilling.
“Stuffer boxes” have appeared on combs in recent years to improve sliver cohesion during finisher gilling. The process can be run faster.
Finisher gilling involves doubling and drafting and will therefore lead to regularisation of the slivers in terms of linear density and cohesive properties. The doubling and drafting occurring will also have positive implications for mixing and blending of fibres. The evenness will also improve, but remember that each operation also adds unevenness. More gilling also means that there is a greater chance of neps being generated.
Therefore finisher gilling is really re-gilling. There are generally 2-3 operations, i.e. 2-3 machines involved. Finisher gillboxes are characterised by progressively higher pin densities for maximised straightening and fibre control.
Typically, drafts of 5 are used, with 20-24 doublings in the first 2 gillboxes, then 2 doublings in the last finisher gillbox
This is also an opportunity for the top-maker to adjust the regain by water sprays (standard regains are specified by customers), and also spinning oils may be added at this stage.
The product from finisher gilling is finally called a TOP.

## Slide 6: Autoleveller Gillbox
1
2
1
3
4
back
front
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
A device called an Autoleveller is common in finisher gilling.
This device is illustrated above.
Firstly (1) a tongue-in-groove sensor detects linear density changes which are transmitted via mechanical action to changes in the back roller speed. The back rollers may also be the sensor in some set-ups.
The mechanical action of the sensor causes sliding feeler bars on a rotating drum (2) to form a profile specific to the linear density changes.
The profile is transmitted mechanically to a cone drive via movement of the drive belt on the cones (3).
Finally (4), the back roller speed changes because of the change to the speed of the cone drive.
NB The timing of the mechanism is such that the change in fibre speed doesn't occur until fibres are at half the mean fibre length from the front rollers. Therefore the change in speed occurs at the right time to “auto-level” the fibre assembly.

## Slide 7: Top Packaging
Balling and Coiling Units
    customer specification
  BOBBINS
  BUMPS
  HANKS
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Balling and coiling units are fitted to the last finisher gillbox. These form the packages which the top-maker sells, or go to the drawing operation.
Two types of package are common:
Bobbins (illustrated in this slide) are cylindrical package wound onto a solid core. These bobbins are shipped as produced without further modification.
Bumps are almost spherical packages with no core. As such they can be compressed and tied to reduce and stabilise volume before shipping. These are popular for export operations.
Hanks are loose multiple loops of top tied at the circumference which can be used for intermediate batch top dyeing. However, bobbins and bumps are also suitable for continuous top dyeing.