## Slide 1: Combing: Advanced Aspects
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Notes: This module will give more detailed explanations of specific parts of the combing operation than that found in the ‘Combing Principle’ module.
The specific sections covered are pin densities, front comb operation and VM retention, comb production rate and sliver crimping.
Some illustrations of these principles will be covered in the ‘Combing: Latest Developments & Future Trends’ module.
Users are urged to review the modules on ‘Gilling’ and ‘Combing Principles’ before using this module.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.

## Slide 2: NSC PB32
Circ Comb
Funnel
Input Nip
Front Comb
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
This slide shows a view of a modern comb, in this case an NSC PB32. It is possible to make out the fibre feed from the input nip, the front comb, the circular comb, the delivery apron, and finally, the condenser trumpet delivery of the combed fibre into a can below (not shown).
The PB32 is the model-before-last comb from NSC. It was released at ITMA95 (International Textile Machinery Association exhibition) in Milan. The PB32 runs at 240 cycles/min (c/min) with low vibration, which was obtained by reducing the stroke of the Apron Carriage from 86mm to 60 mm. The feed loading can be between 400 - 600 ktex. The comb loading is dependent on fibre diameter.
The circular comb in this case, which can just be made out in the picture, is pinned with Staedtler & Uhl VARIO bars.

## Slide 3: Production Rate
Production Rate = Loading (g/m) x Speed (m/min)
Speed = Rotation Speed (c/min) x Feed (m)
Fibre Diameter Loading Prod Rate
m ktex kg/hr
18 380 38
25 500 50 34 600 60
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
A good estimate of the production rate of a comb can be worked out by considering the input side. The output side is complicated because of the oscillation of the apron, which is necessary for overlapping the tufts, and the level of noil, which may be unknown in the production environment.
As with all textile machines, the production rate is the product of the speed at which the material passes through the machine and the mass of material per metre. This is shown in the first line of the slide.
The speed of the material is, in turn, given by the product of the speed of the machine, in cycles/min (c/min), and the feed length of the input fibre per cycle. This gives the production rate in g/min. The production rate, which is more accurately the feed rate, is then obtained by multiplying this result by 60/1000 to give units of kg / hr.
The table shows recommended loadings for the given fibre diameters. The equivalent production rates are also shown, taking the feed per cycle as 7 mm, and assuming that the speed of the comb is 240 cycles/min.
It is quite common, however, to run combs slower in order to improve the quality of the sliver, particularly for finer wool.
The important message from this slide is that fine wool is more costly to comb than coarser wool, since the production rate of the comb (kg/hr) is less. More mill time is required for the same mass of wool.

## Slide 4: Typical Comb Pin Densities
Ken Atkinson
Fibre
Diameter
m
Feed
Gill
#/cm
Fine Segment
Circular
Comb
#/cm
Front
Comb
#/cm
18-25
25-30
30-34
5,6 or 7
5,6 or 7
5,6 or 7
Vario
20-32
Vario
18-30
Vario
18-28
28
25
25
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Pin densities of the various elements used in combing are of central importance.
The pin density on the feed comb is relatively coarse and is insensitive to fibre diameter. This is because the role of the feed comb is to carry the fibre forward as part of tuft detachment and importantly, to control the fibres not gripped by the detaching rollers, thereby preventing catastrophic fibre movement and loss of fibre control.
The purpose of the front comb is to prevent transfer of contaminants from the input to the output on the tails of the fibres as they are detached onto the delivery apron. Only about 20 mm of the leading ends of the fibres are combed by the circular comb leaving up to 130 mm to be combed by the front comb. Contaminants that are prevented from transferring with the tails, and left in the beard, are removed in the next circular combing cycle.
The pin density on the circular comb is critical to the operation of the comb. The reason is that the circular comb is the primary means for removing short fibre, nep, and VM.
The pinning on modern circular combs consists of an initial coarse segment followed by a fine segment. The table shows only the figures for the fine segment with both VARIO and pin strips. VARIO bars are graduated in fineness from coarse to fine around the circular comb. For pin strips, the final pinning can be a very high 32 pins/cm for 18 - 25 µm fibres.

## Slide 5: Photo of S & U Vario Bar
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
This slide shows a VARIO bar. The curved back of the VARIO bar is attached to the face of the front comb holder.
VARIO bars are manufactured by Staedtler and Uhl (S&U) and are a de-facto industry standard. Nakagawa, a Japanese company, also make an equivalent product.
As with pin bars, the pin density becomes progressively finer towards the end of the circular combing cycle, which in this photo is on the right hand side.
The photo clearly shows two segments. The circular comb rotates in an anticlockwise sense as presented in this photo, with the fibre feeding from right to left. The left hand segment is covered with coarser pinning and is referred to as the coarse segment. The right hand segment is covered with finer pinning and, logically enough, is referred to as the fine segment.
The advantage of VARIO bars is that they can be kept much cleaner than pin strips because the bristles of the circular brush are better able to clean between the pins and remove debris such as short fibre, dust, and VM.
The modern tendency is to use VARIO bars, or their equivalent, because of their higher reliability and the lower maintenance costs compared to pin strips.

## Slide 6: Front Comb Parameters
Ken Atkinson
Pin
Density
#/cm
Pin
Length
mm
Pin
Width
m
Pin
Gap
m
Void
%
S&U
Naka-
gawa
28
30
28
28
8.2
8.2
8.2
9.6
258
253
277
242
91
73
80
115
26.1
22.4
22.4
32.2
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
The figures in the table show measured characteristics of both S&U and Nakagawa front comb pin strips.
For the S&U front combs, the two finest pin densities are shown. The length of the pins is a standard 8.2 mm. The width of the pins was measured as 258 µm and the gap was measured on average as 91 µm, which was slightly finer than specification. On this basis there would be 28.6 pin/cm. The results for the 30 pin/cm strip are also shown.
For Nakagawa, the finest pin strip studied had 28 pin/cm but they came with two different length pins. The significance of the longer pins will be discussed later. Note the excellent agreement between measured properties and the specifications. Note also that the longer pins are also slightly thinner, leaving a wider gap between the pins, which is of concern given the mode of operation of the front comb.
It is interesting to calculate the number of fibres per dent (pin gap) of the front comb. Assuming a 400 ktex input loading of 21 µm wool fibre, with the comb operating at 210 cycles/min, and an input feed of 7 mm, the mass of fibre detached per cycle is 2.8 g. If the Hauteur is taken to be 75 mm, the number of fibres in 2.8 g is 82,400. The number of dents for the S&U 30 pin/cm pin strip of width 440 mm is about 1320.
Thus there are about 62 fibres per dent, which compares with about 3300 per dent during preparer gilling. Nowhere else in wool processing is the ratio of fibres to pins lower. This reflects the critical nature of the front combing operation.

## Slide 7: Front Comb Penetration
Too Shallow:
Allows VM & Nep underneath
Correct:
Max removal of VM & Nep
Too Deep:
Fibres jam; higher noil
Shovel Plate
Front Comb
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Good nep and VM removal are dependent on the correct timing and depth of penetration of the front comb (FC) into the circularly combed beard.
The timing is critical because insertion of the front comb needs to be precise and quick. The wrong positioning of the FC, or slow insertion may allow VM and nep to pass through the comb. This follows because the length of the uncombed tails of the fibres is much longer than that of the circularly combed leading ends.
The physical problem is that there is a tendency for fibres to pass under the FC during the early stages of penetration. In fact, penetration of the beard by the FC is often incomplete until the tip of the beard is gripped by the detaching rollers and tension is imparted. This may mean, depending on the length of the feed, that a section of uncombed beard gets past the front comb, potentially reducing the efficiency of the comb. A related problem is that penetration becomes more difficult the greater the input loading.
The other problem relating to the front comb is the setting of the depth of penetration. The situation is outlined in the above figure. If the front comb is set too shallow there is an opportunity for fibre to pass underneath and thereby carry VM and nep through. On the other hand, there is a problem associated with too deep a setting: fibres can jam in the bottom of the pins increasing the noil (through fibre breakage). The correct setting is to arrange for the bottom of the pins to reach about 2 mm below the shovel plate during detaching.

## Slide 8: Sliver Cohesion
Continuous Sliver from Gill
Comb
Overlapped Tufts out
Crimper to increase tuft-to-tuft cohesion
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
A problem with combing is that the tenacity of the output sliver is marginal given the speed of modern gills, 400 m/min on the output and 66 m/min on the input, and the large cans that are often used (up to a diameter of 1000 mm). Remember that finisher gilling is the next process and the combed sliver must be able to withstand the applied forces in this process.
Combed sliver has less strength than gilled slivers because of the arrangement of the fibres into self-contained tufts during detaching. The tufts are simply overlapped after combing to form a sliver with only minimal intermingling of fibres between the tufts. This is the reason for the low tenacity of combed slivers. Measures are needed to increase the tenacity for subsequent processing.
The method commonly used to improve sliver tenacity is to fit a crimper, or stuffer box onto the output of the comb. The effect of this unit is to insert fine crimp into the combed sliver that increases the cohesion between the tufts and consequently the tenacity of the sliver.

## Slide 9: Sliver Cohesion
Sliver Tenacity
mN/ktex
Prepared 290
Combed (after crimper) 175
Tenacity of combed sliver marginal for feeding from large cans into the next gill
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
This slide shows the results of measurements of the tenacity of prepared (input into comb) and combed slivers. The forces were measured on slivers of a linear density of approximately 20 ktex, using an Instron with a gauge length of 250 mm.
The results show that even after the crimper the tenacity of the combed sliver is significantly lower than that of the gilled sliver.
Low tenacity of the combed sliver will ultimately limit the productivity of finisher gilling, so further developments are needed here.

## Slide 10: NSC PB32 Crimper
Funnel
Crimper
J Tube
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Crimpers are simply two angled plates into which the sliver is forced by a pair of nip rollers. When the space between the plates is full of sliver, the incoming sliver at the nip rollers is folded left and right by the high back-pressure into a crimped state. The fine crimping so induced in the sliver increases the intermingling between the fibres and consequently the sliver tenacity.
The photo shows the funnel feeding the sliver into the crimper of an NSC PB32. The output of the crimper is directed into a J-tube and then out over a pulley into a can.

## Slide 11: SAN P90 Crimper
Crimper
Sliver from
comb
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
The SAN crimper is very similar to the one shown earlier. This view shows the crimper in the process of being swung away from the comb to provide access for maintenance etc.
The principle of operation is exactly the same as for the NSC machine.