## Slide 1: Worsted Card Features
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module examines the features of a worsted card in more detail. This detail includes features such as card variables, card clothing, mechanisms for VM removal, the measurement of card production and card performance and the principle of doffing.
It is recommended that the “Carding Principles” and “Card Types” modules be viewed before this module.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: General Card Layout
Primary
  Forepart
    Lickerin roller (takerin)
    Breast cylinder
  Swift / Worker / Stripper
    carding unit
  Doffer
    doffer comb
    condensing funnel
Secondary
  Feed Section
  VM Removal
    Morel Unit, Burr Beaters
  Sliver Take-up
    cans, direct feed
Hopper
Spiked carrier
Stripper apron
Weighing pan
balanced by the weight
Feed lattice to carder
Peter Auer
Source of illustration of Branwell Automatic Feed
Murphy, W. S., The Textile Industries
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source of illustration of Branwell Automatic Feed
Murphy, W. S., The Textile Industries, Volume 2, Gresham Publishing Company, London, p68.
Generally speaking the features of a worsted card can be classified as primary or secondary.
The primary features work to produce a sliver of separated and aligned fibres, the secondary features deliver the input material, try to get as much contamination out of the fibre as possible, and make sure that the sliver is taken care of afterwards.
The feed section generally consists of a hopper arrangement to hold scoured wool. This wool is coming from the blending operation after scouring and drying. This is illustrated in this slide.
The wool is then fed into the card at a nominally constant weight. This can be achieved by weighing the fibre in a weighpan which automatically dumps the wool on to the feed lattice. The feed lattice carries the wool into the forepart of the card.
Recent developments in high speed carding have seen this gravimetric method replaced by more sophisticated methods from other fibre industries. For more information see the module on “High Speed Carding”.
A detailed description of the working of the carding unit can be found in the “Carding Principles” and also the “Fibre/Pin Interactions in Carding” module.
Vegetable matter (VM) removal is detailed in a slide later in this module, and also in another more advanced module, “VM Removal in Carding”.

## Slide 3: Bradford-type Worsted Card
Legend:
BB burr beater STRP stripper
TI taker-in WK worker
TD top divider FNCY fancy
BT bottom tightener SWFT swift
BD bottom divider DFR doffer
MRL morel roller
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
This slide depicts the layout of a Bradford-type Worsted Card. This type of card was developed in England to process relatively short Merino wool. This card type has largely been superseded by the continental worsted cards, of which the Thibeau CA7 is a good example. A Continental-type card is featured in the next slide.
However, some features of this card are common between cards. The Bradford-type card features a double swift (cylinder) arrangement (SWFT1 & SWFT2), upon which are 6 carding units (swift, worker, stripper). For more information on how these work see the modules “Carding Principles” and “Fibre / Pin Interaction in Carding”.
The raising action on the swifts is performed by fancy (FNCY1 &FNCY2) rollers.
The forepart of the card after the feed section is quite long and is utilised to break the fibre clumps up and remove VM. VM removal is achieved in this section through burr beaters. This is covered in more detail in a later slide in this module. There are 8 burr beaters in the forepart of this card.
This layout also has 1 burr beater after the first swift and also a small Morel section for VM removal.
The doffer sections (DFR1 & DFR2) perform the same function which is removing fibre from the swifts, however the second doffer is fitted with a doffing comb to form the sliver.

## Slide 4: Continental-type Worsted Card
BURR
BEATER
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
In contrast, a “Continental-type” card has a shorter forepart characterised by a Lickerin section and a Breast section. These sections act to break up the fibre clumps. The breast section contains 3 carding units, the lickerin section has one, plus one burr beater.
These two sections prepare the fibre for the Morel section which is the main VM removal section, supplemented by 2 burr beaters.
The fibre are then carded on a swift with 4 carding units and a raising set-up analogous to a fancy roller.
Finally fibre is removed from the card by the doffer.

## Slide 5: Card Variables
card clothing
    type of pins
surface clearance
    how close are the working surfaces?
  card settings
surface speeds
    how fast are those surfaces moving past each other?
production rate
    how much fibre is feeding through the card?
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
There are many variables on a worsted card. These are some of the most important.
Card clothing is featured in detail on the next slide. This variable refers to the type of pins employed on a card. These pins can also be varied to aid VM removal using a special type of wire called Morel wire, which is featured in a later slide in this module detailing VM removal.
Other variables that can be varied include the clearance between rollers. These clearances are also referred to as the card settings. The distance between rollers can influence the severity and efficiency of the carding action. Some mills will have developed card settings for various wool types, although a more usual practice is to process wool which is suited to the card configuration. This has implications for mill efficiency.
Similarly the relative surface speeds of the rollers can influence the carding efficiency, however these speeds are also usually static in practice. However it is possible to change the speed of the entire card, referred to as the card speed.
The calculation of card production rate will be covered in a later slide in this module.
The manipulation of both card speed and card production rate is the basis for the important development of high speed carding. This development is covered in detail in the module “High Speed Carding”.

## Slide 6: Card Clothing
Flexible Fillet wire
Short metallic wire
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
This slide examines the card pins/teeth/wires of the card surface. This slide shows two types of wires; flexible fillet wire and short metallic wire. Most worsted cards today employ the short metallic wire on the swift or cylinder, while flexible fillet wire might be used on the worker and stripper. Short metallic wire is more durable and requires less maintenance. Flexible fillet wire is still used extensively in short staple carding (eg. cotton carding).
The flexible fillet wire is usually embedded in strips of material which can be helically glued onto a roller. The short metallic wire is usually a single strip like a thin saw blade which is inserted into helical slots on the roller.
The gauge or number of teeth per area generally changes throughout the card. Heavier gauge clothing (less teeth but larger) is used at the start of the card while finer gauge clothing (more teeth but finer) are required as the fibre separation increases later in the card.

## Slide 7: Card Performance
Fibre Breakage
  optimal is zero breakage
  ~40% of fibres are broken
Fibre Alignment
  optimal is ALL straight and parallel
  gilling / combing required
Neps
  small fibre conglomerates
  carding removes and generates
Trash
  small level of residue
  mostly removed in combing
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Card performance can be judged on the parameters listed in this slide.
Ideally fibre breakage would be zero in carding but due to the entangled nature of fibres and their finite strength, fibre breakage is inevitable. It is estimated that about 40% of fibres are broken during carding. This aspect of carding is covered in more detail in the module “Fibre Breakage in Carding”.
Ideally all fibres would emerge from the card completely straight and parallel. However, the fibre configuration is far from ideal, and leading and trailing hooks are common. It is estimated that 50% of fibres have trailing hooks, 15% have leading hooks, 15% have hooks at both ends and only 20% of fibres emerge from carding completely straight. Hence the need for gilling and combing in the worsted system.
In addition to hooks, the fibres may become entangled and form “neps”. These small fibre conglomerates are difficult to disperse. It has been found that carding removes some neps, but also generates its own neps. The generation of neps is an important card performance parameter.
The objective of fibre cleaning should lead to fibre that is free of trash, however there is always a small level of residue. Whilst there are techniques available to minimise trash in carded fibre, the final level is a function of the initial trash level. Hence the need for combing in the worsted system. VM Removal is covered in more detail in the module “VM Removal in Carding”.

## Slide 8: Card Production
amount of fibre passing through the card
  Fresh Fibre Density (FFD)
    expressed as kg / hr / m
  influenced by
    the fibre capacity of cylinder
      Total Fibre Density (TFD)
    the width of the card
    the speed of the card
    swift speed
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The card production rate is a measurement of the amount of fibre passing through the card. This can be expressed as a term called the Fresh Fibre Density (FFD) which has the units kg/hr/metre width of card.
This figure is influenced by the variables listed in this slide, and a more detailed calculation can be found in the module, “High Speed Carding”.
This is an important card feature since the production rate of worsted cards has consistently lagged behind that of short staple cards, so developments in this area have been a major breakthrough in worsted carding.

## Slide 9: VM Removal
Burr Beaters
  high speed, across width of card
    twigs, hard-heads
    “golf ball” effect
Morel Wire
    special profile card wire
  Lickerin
  Morel Unit
Taker -in
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
There are a number of mechanisms for VM removal on a worsted card.
The first mechanism is the burr beaters which occur throughout the card. They are designed to remove large VM particles such as burr and twigs. The effect as the large VM is removed has been likened to a golf club striking a golf-ball (K. Atkinson, pers. comm.). Essentially burr beaters are straight blades mounted radially on a rotating shaft across the card width. As a blade section hits the VM at speed, the particle is flung out of the fibre mass. A very small amount of fibre is lost in this process.
Another mechanism employs specialised card wire called Morel wire. The diagram in this slide shows the profile of this wire, like a flattened sawtooth. The wire is wound helically on rollers, and as fibres are deposited on the roller they tend to sit in between the wires. The profile design ensures that VM particles sit proud on top of the wires, and can be removed by close set burr beaters or similar devices, as shown on this slide.
These are the main design features for VM removal used on modern worsted cards.

## Slide 10: VM Removal
Grid bars
Knife edge
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Some secondary VM removal mechanisms are displayed in this slide.
The presence of grid bars or knife edges mounted underneath rollers in the forepart of the card can cause more VM and dirt to be removed from the scoured wool.
Essentially, the contaminants are being removed by mechanical force generated as the moving VM strikes the stationary obstruction. The force is not as high as that experienced in the burr beater system, for example.

## Slide 11: Doffing
Swift
(Cylinder)
Doffer
1
2
3
V > V
c d
carding action
  main source of trailing hooks
oscillating doffer comb
card sliver formed
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The last feature of the card worth noting is the doffing system. The doffer roller takes fibre off the last swift cylinder so that the fibre web can be condensed into a card sliver.
During this carding action the fibres tend to be brushed forward by the fast moving swift while they are under the influence of the pins on the doffer roller. This is illustrated as a fibre travelling from position 1 to position 2.
As a consequence the fibre configuration of trailing hooks tends to predominate as mentioned in the slide on Card Performance in this module.
The doffer comb shown at position 3, oscillates into and out of the wires on the doffer roller forming a web the width of the card. This web is taken up by calender rollers which gently pull the web through a condensing funnel, thus forming the card sliver.
The card sliver is then either coiled into a can or directly fed into the gillboxes.