## Slide 1: Performance of Wool Blend Fibre Fabrics
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module examines how the blend composition of fabrics affects their performance in the areas of aesthetics, wear properties, durability and garment performance.
The major reference used for this module was published in 1963, but the ideas and principles outlined are just as relevant today.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Consumer Preference
Aesthetics
  first attraction
  primal desire to decorate body
Performance
Price
Blend Design
  emphasise the best features of component fibres
  minimise less desirable qualities
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Three features of garments may attract the consumer; aesthetics, performance and price.
Aesthetics includes appearance (color, lustre, texture, cover, drape), and handle (liveliness, fullness, firmness, loft, dryness, smoothness, softness). Performance includes a functional (end-use) component (wrinkle resistance, warmth, durability, fastness), and a processing component (tailorability). Price has components of fibre cost (blend composition) and processing efficiency (spinnnability and weavability, dyeing and finishing).
The first feature of a garment that attracts the consumer is its aesthetics. Performance and price are secondary features that may finally combine and lead to a purchase.
This attraction seems to stem from a primal need to decorate the body, rather than modesty, or protection from the environment. Many examples exist of primitive people living practically naked in extreme conditions, but decorating their bodies with whatever is available, such as shells or feathers. The advent of fabric manufacture fulfilled this need.
Fibres can be blended to make yarns to go into fabrics. The principle of blending must always be to emphasise the best features of the component fibres while minimising the less desirable features.

## Slide 3: Crease Recovery
Peter Auer
Source: reproduced from von Bergen, W. (1963)
Crease Recovery
(after 15s s.t.p.)
50
60
70
80
90
100
0
20
40
60
80
100
% wool
Crease Recovery (%)
Dacron
Orlon
Crease Recovery
(after 300s s.t.p.)
50
60
70
80
90
100
0
20
40
60
80
100
% wool
Crease Recovery (%)
Dacron
Orlon
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: reproduced from von Bergen, W. (1963) (ed.), Wool Handbook, Volume 1, pp. 536-546.
Following are some selected results from studies on intimate fabric blends of wool with polyester (Dacron) and acrylic (Orlon) fibre.
This work was undertaken in the 1960’s to derive appropriate blend compositions to maximise the aesthetic properties of the fabrics derived from wool, and also maximise the properties that synthetic fibres could bring to the blends.
All care was taken to isolate the effect of blending. The yarns were spun to a specific diameter, rather than to the same linear density. Each fabric type was woven, to the same linear density, and each fabric was given the same finishing treatment.
Dacron type 54 and Orlon type 42 regular low shrinkage fibres were used in this work. Wool of 58’s quality count and 64’s quality count respectively, was used for the 18 oz. serge, and 6 oz. tropical fabrics tested.
Crease Recovery is tested by creasing the fabric, and then allowing it to recover for 300 seconds or 15 seconds respectively, in standard conditions (21oC and 65% r.h.).
The results are quite different depending on the fibre type. Polyester (Dacron) appears to slightly improve Crease Recovery in blends. However, the inclusion of acrylic (Orlon) in the blend would appear to have a deleterious effect on crease recovery.

## Slide 4: Felting Shrinkage
Felting Shrinkage
(10 commercial launderings)
0
1
2
3
4
5
6
0
20
40
60
80
100
% wool
Shrinkage (%)
Dacron
Orlon
Peter Auer
Source: reproduced from von Bergen, W. (1963)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: reproduced from von Bergen, W. (1963) (ed.), Wool Handbook, Volume 1, pp. 536-546.
These tests were conducted on wool which was not shrink resistant. Modern shrink resist treatments have overcome the problems with the felting shrinkage of wool fabric during use.
However, these tests reveal that the inclusion of Dacron and Orlon in blends above about 60% improves the performance of felting shrinkage remarkably. It would appear that acrylic fabrics are subject to more felting shrinkage than polyester fabrics.

## Slide 5: Tensile & Tear Strength
Tensile Strength
(Dacron only)
10
20
30
40
50
60
70
80
90
0
20
40
60
80
100
% wool
Tensile Strength (kg)
Serge
Tropical
Tear Strength
(Dacron, 8 oz. tropical)
0
0.5
1
1.5
2
2.5
3
3.5
4
4.5
0
20
40
60
80
100
% wool
Tongue-tear Strength (kg)
Peter Auer
Source: reproduced from von Bergen, W. (1963)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: reproduced from von Bergen, W. (1963) (ed.), Wool Handbook, Volume 1, pp. 536-546.
Wool fibre strength is well known to be considerably lower than the strength of other fibres. This would account for the strength loss demonstrated in these results. Acrylic fabric is considerably weaker than polyester fabric.
It should be noted that in these tests the fabrics are taken to failure. The forces involved are far greater than those experienced by the fabrics in general wear.

## Slide 6: Abrasion Resistance
Abrasion Resistance
(Dacron)
0
5
10
15
20
25
30
0
20
40
60
80
100
% wool
100's of cycles (Stoll flex)
Serge
Tropical
Peter Auer
Source: reproduced from von Bergen, W. (1963)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: reproduced from von Bergen, W. (1963) (ed.), Wool Handbook, Volume 1, pp. 536-546.
The improvement in Abrasion Resistance as measured using the Stoll flex apparatus can also be largely explained by the differences in fibre strength.

## Slide 7: Reference
Bercaw, J. (1963), Wool Blends with Man-made Fibres Chapter 7 in von Bergen, W. (1963) (ed.) Wool Handbook, Volume 1, Interscience Publishers, New York
Notes: Written by: Dr. Peter Auer, The University of New South Wales.