## Slide 1: Fibre Effects in Spinning
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Lamb, CSIRO textile & Fibre Technology
Notes: This module examines the relative importance of fibre properties on ring spinning performance and yarn properties.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Lamb, CSIRO Textile and Fibre Technology.

## Slide 2: Fibre Diameter
determines 70% of raw wool price
number of fibres in yarn X-section
  spinning limit (~35 fibres)
    yarn autolevelling possible
  ends-down during spinning
  yarn evenness
FINE YARNS REQUIRE FINE FIBRES
  tex (yarn count)  (diameter)2
“golden bale”
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile and Fibre Technology.
Fibre diameter currently accounts for about 70% of the variation in raw wool price. It is overwhelmingly the most important parameter for spinning performance.
For a given yarn count (linear density), fibre diameter determines the number of fibres in the yarn cross-section. During an economical spinning operation a practical limit is reached for the average number of fibres in the yarn cross-section. This minimum number of fibres is referred to as the “spinning limit”, and in modern mills is about 35 fibres. It is important to remember that this is an average value, there is no mechanism in drafting during ring spinning that controls the number of fibres coming out of the front rollers of the draft zone. The laws of probability apply, such that there is a finite probability that just a few fibres will be present and this probability is dramatically dependent on the average number of fibres in the yarn cross-section.
Research has shown that a form of yarn autolevelling could control the number of fibres in the yarn cross-section better, but the practical application of this knowledge has proved uneconomic at this stage.
In practice, if the number of fibres being twisted is too low to support the forces applied to the yarn during twisting and yarn take-up, the yarn will break, causing an “end-down”. This stoppage at that particular spindle must be fixed by piecing the yarn together, lowering production efficiency, and the singles yarn now has a join which affects the yarn quality.
The number of fibres in the yarn cross-section varies inversely as the diameter squared. Having a minimum average number of fibres in the yarn cross-section means that the only way fine yarns can be achieved is by using fine fibres. Martindale’s theorem also shows that for a given yarn linear density or count (tex) more fibres in the yarn cross-section will produce a more even yarn (i.e. less variation in linear density). Ideally the spinner would like to use fine fibres to make even yarns. These concepts may make it clearer why so much money is paid occasionally for a “golden bale” of ultrafine fibres.

## Slide 3: Fibre Diameter Distribution
D
=
20
m
CV
=
25 %
D
=
21
m
CV
=
20 %
D
D









variation mostly within one staple
CVD% varies from 14% to 28%
  consignment average = 10.5 + D/2
5 - to - 1 rule
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile and Fibre Technology.
Research has shown that the variation in fibre diameter occurs mostly between fibres within any one staple. The CVD% can vary between 14% and 28% for sale lots. From 1st July 2000 the value of CVD will be available for all wools sold at auction, it will then be possible to put consignments together of lower than average CVD. Meanwhile the observed average of CVD for consignments of Australian wool is approximately 10.5 + D/2.
For spinning performance, yarn strength and evenness, yarn bending stiffness and coarse fibres, the “5-to-1” rule applies to a good approximation, i.e. a change of 5 in CVD% is equivalent to a 1m change in mean fibre diameter.
In the example on this slide, the yarn produced from these two wools would be indistinguishable in properties and spinning performance.

## Slide 4: Mean Fibre Length - Hauteur
yarn tenacity & ends-down
1µm

10 mm
yarn evenness
1µm

25 mm
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile and Fibre Technology.
The next most important fibre property after diameter is mean fibre length in the top, or Hauteur.
Research has shown that for yarn tenacity and ends-down an extra 10 mm will give an equivalent improvement in performance to using 1m finer wool.
The effect of extra length on yarn evenness is smaller, with 25mm of extra Hauteur needed to compensate for a 1m increase in fibre diameter.

## Slide 5: Effect of H on Evenness
1
1.05
1.1
1.15
1.2
50
60
70
80
90
100
Hauteur mm
Index of Irregularity (I)
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile and Fibre Technology.
The effect of Hauteur on yarn evenness as measured by the Index of Irregularity (I) is shown in this slide. The relationship on the previous slide is derived from this work.

## Slide 6: Fibre Length Distribution
no optimum CVH%
  “Cup of Spinning Performance”
  nonsense
24
20
20
40
60
CV%
CV
H
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile and Fibre Technology.
A long standing specification in the wool spinning industry has been the CVH of the wool top, the fibre length distribution. This is based on work which postulates a “Cup of Spinning Performance”, as shown in this slide. This graph says that a minimum yarn unevenness (CV%) will be achieved when a CVH of 40% is used.
No experimental evidence has been found that supports this claim. The cup is empty!
It should be noted that a degree of fibre length variation is important for drafting performance. This is demonstrated by the fact that synthetic fibre manufacturers put a certain degree of fibre length variation into their staple fibre production but 20% has been found to be easily sufficient.

## Slide 7: Fibre Crimp
Crimp definition
  all fibres curving together
  irrelevant after scouring
Crimp frequency
  crimps/cm
  survives processing
Less crimp gives more even yarns
  yarn bulk is lower
Peter Lamb
Notes: <number>
<footer>
Written by: Dr. Peter Lamb, CSIRO Textile and Fibre Technology.
Crimp definition refers to how all fibres in a staple may curve together. It may be associated with less entanglement during scouring and therefore longer Hauteur. Apart from this, the property is irrelevant after scouring where the staple structure is destroyed.
Fibre crimp frequency is seen in the staple, and measured in crimps/cm. Fibre crimp is lessened in processing but can be recovered by wet relaxation of the untensioned fibre unless it is permanently set in a new straightened configuration, by, for example, yarn dyeing.
Lower fibre crimp appears to give rise to less combing waste (noil) and longer Hauteur but there is a very strong association between staple length, which also gives longer Hauteur, and crimp. It is interesting to note that breeding for increased fleece weight while keeping diameter constant leads to longer staple length and lower crimp.
Research has shown that the level of fibre crimp has an effect on spinning performance as measured by ends-down and yarn evenness. Lower levels of crimp produce more even yarns. This may be due to subtle differences in drafting performance during spinning.
Because of crimp recovery the level of fibre crimp has an effect on yarn bulk. Higher crimp fibres will produce more bulky yarns (when untensioned). Similarly, higher crimp will lead to heavier, bulkier fabrics particularly in looser knitwear constructions.