## Slide 1: Drafting Principles
Produced for the CRC for Premium Quality Wool undergraduate program by;
Assoc. Prof. Xungai Wang, Deakin University, and
Dr. Peter Auer, The University of New South Wales.
Notes: This module introduces the concept of the drafting of fibre assemblies. The principles in this module can be applied to the roller drafting of slivers and rovings comprising discrete staple fibres.
It is recommended that this module is used in conjunction with the modules “Fibre Assemblies” and “Evenness”.
Produced for the CRC for Premium Quality Wool undergraduate program by Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.

## Slide 2: Aims of Drafting
  attenuation of a fibre assembly
  fibre straightening
Drafting & Drawing defined
Types of Drafting
  hand drafting
  toothed drafting
  Roller Drafting
Xungai Wang & Peter Auer
Notes: <number>
<footer>
Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
The principle aim of drafting is the attenuation of a fibre assembly, which makes a fibre assembly thinner and longer.
During drafting, fibres slide past one another. This can straighten some fibres that have hooked ends.
The terms drawing and drafting are often used synonymously. Strictly speaking, drawing entails doubling and drafting. Doubling (combining slivers together) is used to blend slivers together to improve the evenness. But drafting always increases irregularity, mainly because of the reduced number of fibres in the cross section of the drafted material.
Drafting can be achieved in a number of ways. The simplest form of drafting is to attenuate the fibres manually, i.e. hand drafting such as that carried out by the hand-spinner before twist is applied to the yarn.
Another form of drafting can use teeth to attenuate the fibre assembly. Carding is a form of toothed drafting, where the pins or teeth on the rollers are acting on the fibre assembly, drawing it out from clump of fibres to become a long, thin sliver.
By far the most common form of drafting in textile processing is roller drafting. This will be explained in more detail on the following slides.

## Slide 3: Basic Elements of Roller Drafting
back rollers
speed = X
front rollers
speed = DX
FTE
FLE
input slivers
output sliver
Xungai Wang & Peter Auer
two sets of rollers
drafting zone (ratch setting)
Perfect Roller Drafting
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
The basic elements of roller drafting are illustrated in this slide. For simplicity we will talk about slivers as the fibre assembly.
There are two sets of rollers, back and front. The input sliver feeds through the back rollers (BR) and are drafted by the front rollers (FR). FR must be going faster than BR for drafting to occur. The draft displayed above would be estimated to be DX / X = D. The line across the rollers where they meet is called the nip, formed by the contact between the rollers.
The distance between the roller nips is referred to as the ratch setting. This distance is determined by the length of fibres being drafted. Adjustments of ratch settings are possible on most drafting arrangements. The space between the rollers is commonly referred to as the drafting zone. Some machines have several drafting zones.
The concept of perfect roller drafting is very important. This states that a fibre should move at the speed of the back rollers until its fibre leading end (FLE) reaches the front rollers. Once it reaches the front rollers it should be instantly accelerated to the speed of the front rollers. The fibre will be under the influence of the front rollers until the fibre trailing end (FTE) leaves the front rollers.
If this phenomenon occurred then drafting would be no trouble, however not all fibres in the drafting zone behave according to the requirements of perfect roller drafting. Fibre control is often necessary to improve this situation, as will be discussed later.

## Slide 4: Draft Measurement
material draft
  input linear density / output linear density
    material draft or “real draft”
mechanical draft
  FR surface speed / BR surface speed
  ratio of the roller rotational speeds
    “machine draft”
    draft estimate
material draft < mechanical draft
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
The amount of draft can be measured in a number of ways.
The most accurate method is to find the ratio between the linear densities of the input and output materials. This is referred to as the material draft or real draft.
The draft can be estimated by comparing the roller surface speeds, or the roller rotational speeds. In the second instance, the roller diameter need to be the same for a direct comparison. This is also referred to as the machine draft.
The material and mechanical drafts often differ slightly, because of irregular drafting caused by fibre and machine factors.
The causes of irregular drafting are covered on the next slide.

## Slide 5: Irregular Drafting
Machine Factors
  variation in nip position
  roller speed variation
  roller eccentricity
  slippage between fibre and rollers
Result
  lack of evenness
  strength variation
Fibre Factors
  length variation (short fibres)
  fibre entanglement (poor alignment)
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
The causes of irregular drafting can be grouped into those caused by machine factors and those caused by fibre factors.
Mechanical or electrical defects in the machinery can lead to variation in the actual nip position, or rollers can change speed intermittently or regularly, or rollers may be eccentric or out of shape.
A cause of irregular drafting may be slippage between the fibres and the rollers. This would cause the real draft to be less than the machine draft.
Fibre factors such as poor fibre alignment and the presence of short fibres may also cause irregular drafting. Fibres are effectively placed out of turn during drafting by these effects.
The result of irregular drafting is that the evenness (as measured by the linear density variation) will not be as good as anticipated. This variation in the number of fibres in the cross-section of the fibre assembly may lead to strength variation, especially in yarns (since less fibres support lower tensile forces).
Some of these effects will be expanded further on the following slides.

## Slide 6: Roller Eccentricity

back rollers
front rollers
periodic irregularity (unevenness)
  repeats every roller rotation
wavelength () is distance between repeats
identified by evenness testing
  Spectrographs
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
Roller eccentricity can be caused by rollers wearing out, or by the surface of the roller varying in distance from the shaft. It is a major mechanical cause of irregular drafting. Whatever the cause of the eccentricity, it leads to periodic irregularity in the fibre assembly which is repeated every roller rotation.
The wavelength of the irregularity is defined as the distance between repeats, and would equate to the circumference of the offending roller if it was the front roller. The irregularity wavelength would be the circumference times the draft if it was the back roller.
This is simple enough if only one machine is involved, say a gillbox. However if multiple machines are involved in a process, say multiple gillings, then the final wavelength will be the roller circumference multiplied by the various drafts involved on each gillbox.
These wavelengths can be identified by the use of analysis tools like the Spectrograph function on the Uster Evenness Tester. For more information see the “Evenness” module.

## Slide 7: Floating Fibre Effect
Xungai Wang & Peter Auer
Fibre length variation
  long fibres
    effectively controlled
  shorter fibres
    NOT under positive control
    FLOATING fibres
    interaction with other fibres
      slow-moving (slow them down)
      fast-moving (speed them up)
Result
  more fast contacts
  thick spot, followed by a thin spot
DRAFTING WAVES
  approx. 2.5x m.f.l.
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
Real slivers contain fibres of differing lengths. The ratch setting is set to be just longer than the longest fibres to avoid fibre breakage. Therefore long fibres are effectively under control by the back rollers until the FLE reaches the front rollers.
However shorter fibres are not controlled once they leave the back rollers, and can be subject to fibre migration caused by longer fibres moving past them as they are being drafted forward. Similarly the fibres may be retarded by slow-moving fibres and fibre entanglement.
These short fibres are referred to as “floating fibres” or “swimming fibres”, and are a major cause of irregular drafting and the formation of drafting waves.
The frequency of these drafting waves has been measured to be about 2.5 times the mean fibre length (m.f.l.) in the fibre assembly.
The drafting waves distort the distribution of the the number of fibres in the cross-section of a fibre assembly beyond that expected by probability alone.

## Slide 8: Sliver Elasticity Effect
Slivers are elastic over small strains
  fibre crimp
  fibre entanglement
  poor fibre orientation
“stick-slip” effect
DRAFTING WAVES
  approx. 2.5x m.f.l.
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
Another effect adding to assembly irregularity is the sliver elasticity effect. Slivers are elastic over small strains due to the presence of fibre crimp, fibre entanglement and poor fibre orientation. This means that a sliver will stretch without effect when a small force is applied.
However, when the elasticity of the sliver is exceeded, the whole fibre assembly will move forward, a so-called “stick-slip” effect.
This phenomenon is another cause of irregular drafting which can lead to drafting waves of similar frequency to that found with floating fibres.

## Slide 9: Ideal Pressure Distribution
back rollers (BR)
  maintain pressure as long as possible
  gradually decrease pressure near FR
front rollers (FR)
  more concentrated pressure
back roll nip
front roll nip
ideal
actual
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
Another variation from perfect roller drafting can be caused by the pressure on the fibres in the drafting zone being less than ideal.
The diagram in this slide illustrates the ideal pressure distribution (solid black line), where pressure is maintained on the fibres as long as possible before and after the back rollers. Ideally, the pressure near the front rollers should be more concentrated so that fibres can be accelerated instantaneously when they approach the front roller nip, as required by perfect roller drafting.
In actual practice, rollers have a very narrow nip zone back and front as shown by the dotted red line. So the pressure is high only at one point. After the back roller nip the pressure drops off very quickly in the drafting zone without some artificial mechanism.
There needs to be some way of changing this pressure distribution towards the ideal. Some of the various mechanisms are discussed on the next slide.

## Slide 10: Fibre Control in Roller Drafting
pressure bar
Xungai Wang & Peter Auer
Aims
  minimise drafting waves
  maximise control of short fibres
Mechanisms
  pressure bars
    cotton drawframe
  pins
    worsted gillboxes
  aprons
    worsted ring spinning
  false twist
    woollen ring spinning
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
Fibres in the drafting zone between rollers do not travel at the same speed as the back rollers all the time. This can lead to problems with evenness embodied in drafting waves in the fibre assembly. The main fibres out of control are short fibres.
These effects could be alleviated if the pressure distribution on the fibres was increased and fibre control was maximised.
There are various mechanisms to achieve this control. Drafting rollers in the short staple system are spaced very closely, therefore the fibre control mechanisms have to be small. An example of a pressure bar is shown on this slide. This increases fibre control when cotton fibres are being drafted.
The worsted system processes long staple fibres which uses a longer ratch setting. Therefore larger fibre control mechanisms can be employed in some processes such as pins in gillboxes (refer to “Gilling” module). Alternatively, false twist devices are used in woollen spinning (refer to “Yarn Production” module).
Another fibre control mechanism used in ring spinning is the apron system also shown in this slide. This is used in the drafting zone of spinning frames.

## Slide 11: Law of Doubling
CV (in) = CV
n
multiple sliver input
  overall CV of input decreased
single sliver output
  increases the evenness
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
As mentioned earlier, drawing entails doubling and drafting.
The Law of Doubling says that the variation in linear density of the input slivers (CVin) will be the average of the linear density of all the slivers divided by the square root of the number of slivers doubled together.
This is because some of the thick spots in a sliver may be matched against thin spots in other slivers, so the overall variation in linear density will fall if more than one sliver is being drafted. Another way of looking at this is that after doubling, the number of fibres increases in the cross section, which improves the evenness of the doubled material.
Therefore, the evenness of the output sliver will be increased by using doublings. The more doublings the better. This concept is seen many times in early stage processing, in gilling, in combing, in finisher gilling, in drawing for examples.

## Slide 12: Law of Addition
CV (in)
CV (added)
CV (out)
CV (out) = CV (in) + CV (added)
2
2
2
each machine adds a certain amount to the irregularity of the finished product
processing adds unevenness
  reduced fibre no, imperfect drafting
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
Therefore, simply by using doublings the evenness can be minimised, but the process has limits due to another phenomenon.
It must be remembered that each drafting operation ADDS variation in linear density, because it reduces the fibre number in the assembly cross section, and adds other drafting defects.
This phenomenon is embodied in the Law of Addition shown on this slide. The variation in linear density of the final sliver will be increased because the machine is adding variation. The amount of variation is a function of each machine, and is different for each machine.