## Slide 1: VM Removal in Carding
Produced for the CRC for Premium Quality Wool undergraduate program by;
Gary Robinson, CSIRO Textile & Fibre Technology.
Notes: This module examines how the moisture content of carded wool can affect the make-up of VM in the card sliver.
An optimum regain is found for scoured wool, as determined by the number of particles permissible in the top as specified by the top specifications.
Produced for the CRC for Premium Quality Wool undergraduate program by Gary Robinson, CSIRO Textile & Fibre Technology.

## Slide 2: Removal of VM in carding
Morel Wire
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
One of the most important requirements of worsted processing is the efficient removal of any vegetable matter (VM) that may be present.
VM is removed deliberately during carding at various points along the card. Heavy VM (twigs and hard-heads) is initially removed by a burr-beater at the Lickerin section. The Morel section is designed to remove the majority of VM in carding. This section is coated with Morel type wire whereby the fibre sits in the wire profile while the VM is presented to the burr beater to be struck out of the fibre mass.
VM can reach the final fabric if it isn’t removed in early stage processing (carding and combing). If it reaches this stage it is removed by a process called mending which involves inspection and picking the VM particles out by hand.
The cost of removing VM remnants from fabric varies between $0.05 and up to $2.00 per particle depending on the degree of intertwining of the VM particle and the fabric structure. In contrast, the cost of VM removal during carding is less than 0.005 CENTS per particle.
Therefore improved VM removal is a serious issue in worsted processing, due to the considerably high cost imposts it incurs in later stages of processing.

## Slide 3: Effect of regain on VM particle count
200
160
120
80
40
8
4
12
16
20
24
28
32
Total Particle Count in Top (No./100g)
Control, Burr
Control, S/S
S/S
Burr
0
0
Mean Regain (%)
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
This slide shows the results of a study whereby the regain of scoured wool being fed to the card was adjusted to various levels and the number of VM particles in the top was counted at each regain level.
It would appear that for burry wools, the level of VM in the top appears to have a minimum at about 8-10% regain, and increases for both high and low regains.
The results also indicate that for Seed and Shive (S/S) there is a minimum amount of VM at about 14% regain.

## Slide 4: Effect of regain on particle size (card sliver)
A Burr - 2.5% regain B Burr - 29% regain
C S/S - 2.5% regain D S/S - 28% regain
A
B
C
D
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
The explanation of the VM count variation with regain can be explained by taking into account the following factors:
(i) increased brittleness of VM at low regain
(ii) assessment of VM in the top is in terms of numbers and not weight of VM.
The diagram shows that burr at low regains breaks up into small particles due to its brittleness, while at higher regains the burr becomes less rigid and unravels into longer pieces.
In terms of the weight of VM, the variation in VM content is not marked.
Therefore the optimum regain would be determined by the specification for the number of particles permissible in a top.
This has implications for the on-line monitoring of scoured wool regain. Ensuring a more uniform moisture content after exiting the dryer would allow better control of the number of VM particles in the top.