## Slide 1: Modified Wool Fibre Technology (OPTIMTM Fibres)
A Collaborative Project between
CSIRO Textile & Fibre Technology & The WoolMark Company.
Produced for the CRC for Premium Quality Wool undergraduate program by;
Gary O’Loughlin, CSIRO Textile & Fibre Technology.
Notes: This module examines an exciting new development in wool technology. This is the ability to modify wool at the fibre level using OPTIMTM technology.
A Collaborative Project between CSIRO Textile & Fibre Technology & The WoolMark Company.
Produced for the CRC for Premium Quality Wool undergraduate program by Gary O’Loughlin, CSIRO Textile and Fibre Technology.

## Slide 2: Developments in Fibre Technology
Competing Fibres
  linear density
    microfibres
  profiles
    CoolmaxTM
  surface effects
    delustring
  latent effects
  new chemistry
    PP
  re-launch old chemistry
    TencelTM
Wool
  finishing
    shrink-resist fibres
    insect-proof fibres
    flame-proof fibres
    enzyme treatment
  blending
    new specs
      fibre properties
  linear density
  profiles
  surface effects
  latent effects
Gary O’Loughlin
Notes: Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
The implementation of new fibre technology a key strategy among competing fibre producers. The developments have been in the form of linear density modification (e.g. microfibres), fibre X-sectional profiles (e.g. CoolmaxTM), surface effects to change the surface lustre of fibres (e.g. addition of TiO2 to polymers, enzyme treatment of cotton), the development of fibres with latent effects (e.g. heat-shrink acrylic fibre), the development of fibres with a new chemical basis (e.g. the successful manufacture of polypropylene (PP) for fibre usage), or the re-launch of fibres with the same chemistry, but improved performance (e.g. TencelTM, which is rayon re-launched).
The wool industry has been able to develop new fibre technologies over the years based on the areas of finishing and blending. The development of shrink, insect and flame-resist fibres is well known. Perhaps less well known is the application of enzymatic finishing to improve the comfort factor of wool fabrics.
The development of new customer specifications for wool products containing wool with differing fibre properties has been a possibility since wool metrology has developed to a point where these properties can be specified in the market-place. The recent involvement of groups selling wool fibre on this basis is illustrated by the SRSTM and Egelabra groups.
However, until recently the wool industry hasn’t been able to modify wool at the fibre level. It now can, using a technology developed in collaboration between CSIRO Textile & Fibre Technology (CSIRO TFT) and The WoolMark Company (WMC).
As we will see in the following slides, this new technology can alter the linear density, the X-sectional profile and the surface lustre of wool fibres.
A further benefit of the technology is that it can be used to also produce a fibre that has the potential to provide light, warm garments by inducing latent effects in the modified fibre.

## Slide 3: Consumer Preference
Consumer Trend
  lighter fabrics
  softer fabrics
Linear density of fibres needs to be reduced
Now wool is able to meet the challenge better
OPTIMTM technology
  OPTIMTM fine
  OPTIMTM max
Gary O’Loughlin
Notes: Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
There is a clear trend to lighter and softer fabrics by consumers. Meeting this trend requires the use of finer fibres, from a technical and aesthetic viewpoint. Finer fibres make light-weight yarns possible in today’s spinning environment, while the bending properties of fine fibres provide the required softness.
Until now, the only way the wool industry has been able to respond adequately to this trend is to provide finer fibres through breeding and selection on-farm, and by blending sale lots into consignments post-farm. While both of these strategies are effective, breeding for finer fibres has a long lead time and is unsuitable for many woolgrowers. Related to this, the building of suitable consignments is restricted by the supply of suitable wool.
To meet this consumer preference WMC / CSIRO TFT, have developed a technology to modify wool at the fibre level. Not only is the linear density of fibres reduced, but the X-sectional profile and the surface lustre of the fibres is different as well. A closely related technology produces a fibre that can retract under the right conditions.
Both fibres are produced with OPTIMTM technology.
The fibres produced are called:
OPTIMTM fine, and,
OPTIMTM max.
Firstly, a reduced diameter wool fibre (OPTIMTMfine) is possible. Typically a 19m wool fibre is reduced in diameter to a fibre 3-4m finer.
Secondly, a retractable wool fibre (OPTIMTMmax) is produced with a latent contraction that will relax, under certain conditions, by 20-25% in length. The analogy to this is a heat shrinkable acrylic fibre.

## Slide 4: OPTIMTMfine Technology
WOOL SLIVER
TWIST
DRAW/EXTEND
PERMANENTLY SET
BACKWASH
OPTIMTMfine FIBRE
[e.g. 19 micron]
[15 micron]
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
The process for producing OPTIMTMfine wool fibre involves the steps shown on this slide.
A wool sliver is twisted to lock fibres against each other so they don’t draft when they the sliver is extended. This process is very similar to the process of “stretch-breaking” which is used to convert continuous filament yarn to staple yarn. For further information see “Blending Fibres” module.
After drawing and extending the sliver and hence the fibres, the fibres are permanently set by the action of heat and moisture. Chemically speaking, the disulphide bonds holding the polymer chains together in the fibre are re-arranged in a new permanent configuration.
The process is a continuous sequence of operations encompassed in one set of machines.
The reduction in fibre diameter is about 4m across a wide range of wool.

## Slide 5: OPTIMTMmax Technology
WOOL SLIVER
TWIST
DRAW/EXTEND
PARTIALLY SET
OPTIMTMmax FIBRE
[25% latent contraction]
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
The process for producing OPTIMTMmax wool fibre involves a similar sequence of processes, however during the process, the fibre is only partially set.
The resultant fibre is stable in water at room temperature, but a treatment in hot water brings about a 25% length contraction. The fibre is also returned to its original near circular cross-section and diameter.

## Slide 6: Chemical / Mechanical Process
EXTEND / DRAW
Gary O’Loughlin
Notes: Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
The treatment of the fibres is carried out on fibre in the form of a continuous sliver, which is represented in this slide.
After twisting the sliver is extended and either partially or permanently set.

## Slide 7: Bulk Generation in Yarn
OPTIMTMmax FIBRE
NORMAL WOOL
RELEASE YARN IN HOT WATER OR DYEBATH
BLEND
SPIN
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
As shown in this slide intimate blending of the OPTIMTMmax fibre with untreated wool is achieved in a re-gilling process.
Spinning is followed by a release of the latent contraction in hot water which results in a bulky wool yarn similar to a high bulk acrylic.

## Slide 8: Bulky Yarn Appearance
Normal Wool Yarn
OPTIMTMmax Yarn
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
The slide shows how the retraction of the partially set wool causes a buckling of the untreated fibres and a consequent bulking of the yarn.
This slide illustrates how the retractable wool fibre is predominantly in the core of the yarn.
The buckled fibres in the outer surface are predominantly the untreated wool or the other component of the blend.

## Slide 9: Cross-section of OPTIMTMfine Wool
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
This slide shows a scanning electron micrograph of a cross-section of OPTIMTMfine modified wool fibres.
It is obvious that the cross-sectional-shape of the wool fibre has changed from near circular to a polygonal form.
The shape change is a consequence of the transverse force imposed during the extension of a tightly twisted sliver assembly.
The diameter reduction is more precisely expressed as a change in linear density measurement, since the fibres are not approximating circles in X-section anymore. Linear density is used more frequently in competing fibre industries and is expressed as decitex (g/10km).

## Slide 10: Fibre Appearance
Gary O’Loughlin
Notes: Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
This slide shows the appearance of fibres before and after the Optim™ treatment. The increase in fibre length caused by stretching is apparent. Less obvious, of course is the reduction in fibre diameter.

## Slide 11: Fibre Structure
Wool
OPTIMTMfine
alpha- Keratin X-Ray Pattern
beta-Keratin X-Ray Pattern
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
The characteristic x-ray diffraction pattern of wool is classified as of an alpha-crystallite form, shown on the left of the slide.
The OPTIMTMfine wool fibre x-ray diffraction pattern contains the diagnostic reflections of a beta-sheet crystalline form similar to that found for silk.
This is characterised by meridional and equatorial reflections in the alpha form, and equatorial reflections in the beta form.

## Slide 12: Alpha Beta Transformation
Raman Units
0
.02
.04
.06
.08
.1
.12
1750
1700
1650
1600
1550
    Wavenumber (cm-1)
OPTIMTMfine
Wool
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
This slide shows the results of structural investigations by ft-raman spectroscopy. A pronounced change in the amide 1 region of the wool spectra is shown that is indicative of a change from an alpha-helical conformation to an extended polypeptide backbone conformation.
This observation further supports the supposition that an alpha to beta transformation has taken place in the OPTIMTMfine modified wool fibre.

## Slide 13: Fineness of OPTIMTMfine Fibre
Parent Fibre
Reduced Micron
Wool
Diameter
[micron]
Linear Density
[decitex]
Linear Density
[decitex]
19
3.7
2.3
23
5.4
3.3
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
Since the profile of the OPTIMTMfine modified wool is no longer near circular, and the usual measure of linear density for competing synthetic fibres is decitex (g/10km), it is better for comparison to show typical changes in fibre linear density that result from the fibre modification.
Two parent wools are shown in the table with the subsequent linear density reduction. The linear density of single fibres was measured using a vibroscope.
The decrease in linear density that occurs after OPTIMTMfine modification can be seen from the table. The 3-4 m decrease in diameter mentioned earlier is really an equivalent value based on air flow measurements.
A value of 2.3 decitex equates to a 15 m fibre, assuming a circular cross-section.

## Slide 14: OPTIMTMfine Fibre Properties
OPTIMTMfine
Wool
Viscose
Linear Density
[decitex]
2.3
3.7
1.7
1.2
Tenacity
[cN/tex]
14.5
11.5
22-26
39
Extensibility
[%]
19
38
20-25
18
Silk
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
This slide compares the tensile properties of OPTIMTMfine modified wool fibres compared with those of other mainstream apparel fibres.
Of particular note is the increased dry tenacity and decreased extensibility of the OPTIMTMfine fibre.
In general, the tensile properties fall within the acceptable range for apparel products.
However, results for the wet modulus, or stiffness of the fibre wet, have been found to be about 50% of normal, comparable to viscose.
This has implications for dyeing at the fibre and yarn stage. Systems designed and suited for handling of low wet modulus fibre are required.

## Slide 15: Fabric Properties
* RM=OPTIMTMfine
Abrasion
Resistance
[1000 rubs]
WOOL
RM 1
RM 2
RM 3
WOOL
“COOL WOOL”
SPECIFICATION
Fibres in
X-Section
38
61
51
61
38
Weight
[g/m2]
100
100
129
170
170
MAX. 220
Strength
[N]
135
176
252
341
240
>147
12
8.7
26
18
22
>15
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
Typical fabric performance properties of light weight woven fabrics are shown in this slide.
The lower linear density OPTIMTMfine wool fibre enables finer yarns and lighter than normal fabrics to be produced.
The fabrics made from OPTIMTMfine wool meet the specification for all categories of “Cool Wool” apparel products, with the exception of the 100g/m2 fabric which had a low abrasion resistance. This fabric is still suitable for accessories such as scarves, shawls and ties.
The OPTIMTMfine wool fabrics also display an increased surface lustre and increased surface smoothness.

## Slide 16: Yarn and Fabric Bulk
Yarn Count
[tex]
Yarn Bulk
[cm3/g]
Fabric Bulk
[cm3/g]
Fabric Weight
[g/m2]
Untreated
Wool
R 75/ 2
12
3.5
287
Relaxed
OPTIMTMmax
Blend
R 74/ 2
17
6.3
225
Untreated
Wool
R 478 /3/3
6
7.8
R 435 /3
12
10.5
Relaxed
OPTIMTMmax
Blend
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
The measured increase in the bulk of yarns and fabrics produced using OPTIMTMmax fibres are shown in this table. Bulk is defined as the volume occupied by a given mass of material under a 10g/cm2 pressure.
Typically for machine knitting yarns of equivalent count the bulk increases from 12 to 17 and the resultant fabric bulk from 5 to 7.
The pronounced increase in bulk of yarns and fabrics is also shown for typical hand knitting yarns.
This means that when knitting to the same cover, 20-30% less of the bulky yarn is required. This corresponds to a 20-30% weight saving and weight reduction in the knitted garment product.

## Slide 17: Thermal Properties of OPTIMTMmax
Machine
Knitting
Yarn
Thermal
Insulation
[Tog]
Fabric
Weight
[g/m2]
Warmth to
Weight Ratio
[Tog.m2/kg]
Tex
Twist
Alpha
Fabric
Bulk
[cc/g]
Untreated
Wool
0.3
286
1.3
R70/2
 84/71
3.6
Bulky Wool
[Relaxed]
0.5
224
2.3
R78/2
 85/72
6.6
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
The measured heat transfer values shown in this slide indicate that the bulky wool product has better insulating properties compared to unmodified wool.
This is associated with the increased volume of air trapped in the bulky yarn assembly.
With the 20% lighter product from the bulky wool yarn providing the same cover, the warmth to weight data indicate the garment would be significantly more comfortable than the conventional wool product.

## Slide 18: New Product Opportunities
OPTIMTMfine Fibre
  Light-weight “silk-like” trans-seasonal wear
OPTIMTMmax Fibre
  20 to 30% lighter garments
  “warmth without weight” knitwear
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
There are a number of new product opportunities that stem from these modified wool fibres.
Firstly, from the finer OPTIMTMfine wool, light-weight trans-seasonal wear fabrics are possible. These fabrics would be made from fibre reminiscent of silk, and would allow the wool industry to enter non- traditional wool markets.
Secondly, OPTIMTMmax wool fibres allow wool knitwear products of lighter weight to be produced through enhanced yarn bulk. Wool garments 20% lighter than those knitted from conventional yarns provide increased warmth without added weight. This meets consumer demand for “warmth without weight” knitwear products.

## Slide 19: Current Status
Test marketing of products taking place
Australian topmaker licensed to:
  produce fibre
  distribute globally
Second Generation OPTIM Fibres
Gary O’Loughlin
Notes: <number>
<footer>
Written by: Gary O’Loughlin, CSIRO Textile and Fibre Technology.
In summary, a technology has been developed to modify wool at the fibre level.
This technology allows wool fibres to be modified in terms of linear density, cross-sectional profile, surface lustre and to possess latent effects.
Two new fibre types have been produced, called OPTIMTMfine, and OPTIMTMmax. Test marketing of products made from the new fibres has commenced.
The technology has been licensed to an Australian topmaker, who will be responsible for producing the fibres on a commercial basis, and to distribute the fibres on a global basis by selling modified fibre tops.