## Slide 1: Fibre Properties & Final Products
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Notes: This module examines the influence of fibre properties on the performance and appeal of consumer products.
The content is mainly confined to apparel wool products, since this is the major market for Australian wool. However, some discussion of woollen products (Australian wool is a raw material) and carpet yarns is included.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.

## Slide 2: Contributors to Fabric Properties
Fibre properties
Yarn construction
  twist
  doubling
Fabric Construction
  woven / knitted
  weave / knit structure
Finishing
  milling
  setting
A. de Boos, G. Naylor, P. Auer
Notes: <number>
<footer>
Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
It is important to note that fibre properties are just one set of contributors to the performance and appeal of wool apparel products. Other contributors can be yarn, fabric and garment construction and fabric finishing procedures.
Factors such as the yarn twist, the number of singles yarns folded together to form the final yarns (doublings), whether the fabric is woven or knitted, and the actual weave or knit structure can have an influence far greater than the fibre properties themselves. Finally the fabric finisher can influence the final fabric appearance and performance to a marked degree by the application of various chemicals and finishing treatments.
It is very important that these factors are taken into consideration when the impact of fibre properties on product is evaluated.
For example the same 19m wool can be made into soft knitted pullover, a high quality men’s suit, a crisp high performance jacket, or a soft supple ladies dress fabric.
Similarly, quality woollen products are made from the trash cans of the worsted industry, and from the raw product of the rag-pulling industry.

## Slide 3: Classification of Fabric Characteristics
Aesthetic
  Fabric Handle
  Prickle
  Thermal Insulation
  Wrinkle Recovery
  Pilling
  Appearance in Wear
  Colour
Functional
  Fabric Strength
    Tear
    Tensile
  Shrink Resistance
  Abrasion Resistance
  Ease of Manufacture
  Flame Retardance
  Water Repellency
A. de Boos, G. Naylor, P. Auer
Notes: <number>
<footer>
Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Fabric characteristics can be loosely divided into two groups; Aesthetic and Functional. The list is not exhaustive, but it encompasses the most important product characteristics.
Functional characteristics measure the failure of the fabric in some form. The fabric may tear, shrink, or be abraded to form holes, or be difficult to make into garments. Ease of manufacture which would also be regarded in some sense as an aesthetic characteristic could include such things as pressing performance, sewability or seam pucker. Also the fabric may be expected to perform in the areas of flame retardancy (eg. airline and motor vehicle upholstery), and water repellancy (eg. outdoor wear).
Aesthetic characteristics do not involve failure of the fabric as such, but rather that the fabric fails to meet consumer expectations. This might involve how it feels to touch and wear (handle, prickle, thermal insulation), how it performs during wear (wrinkling, pilling), how it appears during wear (seam puckering), or even the how the colour of the fabric performs (dye fading, fabric yellowing). In such instances the garment is not unusable, merely unsightly.
Both sets of characteristics are important to the consumer. No-one will wear a garment that lasts forever if it feels like iron or prickles. Likewise there will be few repeat purchases if a garment has a soft luxurious handle but pills badly after a few wears.

## Slide 4: Contributing Factors
Mechanical
Surface
Dimensional
Thermal
Fabric
Handle
Physical
Ease of Manufacture
A. de Boos, G. Naylor, P. Auer
Notes: <number>
<footer>
Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Examples of how some important fabric characteristics are assessed and measured are dealt with in this slide.
The first fabric characteristic shown is Fabric Handle. Handle is a complex phenomenon involving the mechanical, physical, surface and thermal properties of the fabric. Instruments have been developed to objectively measure these properties.
It should be noted that fabric handle is often assessed subjectively by panels of judges. The judges may be experienced or quite inexperienced depending on the aim of the trial. Whichever is the case, they are able to rate and rank the handle of fabrics subjectively with some degree of repeatability. Sometimes, this subjective assessment is called Total Hand Value (THV - only in Japan)(subjective). The term THV is also used for objectively determined handle. THV described later in this module will be for the objective and subjective measurements of fabric handle.
The second example shown in this slide is Ease of Manufacture. This is another complex characteristic involving the mechanical, physical, surface and dimensional properties of the fabric.
It would be helpful at this stage to review just what these assessable and measurable fabric properties are, before proceeding further.

## Slide 5: Fabric Properties
Low Stress Mechanical
  Extensibility
  Bending Rigidity
  Shear Stiffness
  Lateral Compressibility
  Recovery from above deformations
Physical
  weight
  thickness
  fabric construction
A. de Boos, G. Naylor, P. Auer
Notes: <number>
<footer>
Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
In the evaluation of fabric aesthetics, the important fabric mechanical properties are those that are measured at very low stress levels. This is analogous to the the sort of stresses that an apparel fabric would undergo during manufacture and in wear.
The mechanical properties that are normally measured in a woven fabric are the extensibility of the fabric, its behaviour under applied load (eg bending), and its recovery from the deformation.
These measurements can be carried out on precisely engineered instruments that have been developed for this purpose (eg. KES-F, SIROFAST).
The physical properties of fabrics which can be measured are listed above. Several of these are covered by international standards. These include properties such as fabric weight and thickness, and construction.

## Slide 6: Fabric Properties
Surface
  surface friction
  surface geometry
Dimensional
  relaxation shrinkage
  hygral expansion
Thermal Insulation
  thermal flux
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Other fabric properties that can be directly measured are listed in this slide.
The coefficient of friction of the fabric surface can be measured, usually by rubbing the fabric against another surface and measuring the resistant force.
The surface geometry of a fabric measured using a suitable probe relates to the yarn and fabric construction.
Relaxation shrinkage is the irreversible change in dimensions that occur when a fabric is relaxed in water or steam. This can be measured by standard procedures which assess the dimensions of the fabric before and after relaxation.
Hygral expansion describes the REVERSIBLE change in fabric dimensions that occurs when FIBRES absorb and desorb moisture in response to a change in the environment. The appearance of structured garments manufactured from fabrics with high hygral expansion deteriorates in environments with high humidity.
The thermal insulating properties of a fabric can be assessed by measuring the amount of heat that a fabric allows through itself. This is called the thermal flux.

## Slide 7: Fibre Effect - Mechanisms
direct
  prickle
  pilling
modification of fabric structure
  fabric thickness
  weave crimp
modification of fabric mechanical properties
  bending rigidity
  shear properties
A. de Boos, G. Naylor, P. Auer
Notes: <number>
<footer>
Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
The mechanisms by which changes in fibre properties lead to perceived and measured changes in fabric performance can be classified in a number of ways.
The effect can be DIRECT, i.e. the fibre property change directly affects the fabric performance. For example, coarser fibres directly influence the amount of prickling experienced by a fabric wearer, while finer fibres tend to pill more.
The change in fabric performance may be INDIRECT. For example, changing fibre properties may be reflected in fabric properties such as fabric thickness or weave crimp, which in turn may change the way a wearer experiences the fabric. Also changing fibre properties may lead to changes in fabric mechanical properties, such as how easily it bends (bending rigidity) or how the fabric responds to forces at angles not aligned with yarn directions (shear properties).

## Slide 8: Objective Description of Fabric Handle
FUKURAMI soft, bulky vs. cold, hard
KOSHI stiff vs. limp
NUMERI soft, smooth vs. hard, rough
HARI anti-drape stiffness
SHARI crispness
Total Hand Value THV (objective)
  combines all the above
  regression equation
  specific fabric ranges
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Fabric Handle is a complex phenomenon. The Japanese textile industry has developed a number of ways of describing various aspects of fabric handle. These are listed above. The fabric that suits a particular application will exhibit these aspects to different degrees. For example, a fabric for an overcoat might require a fabric which has a high Fukurami (soft and bulky), but also a high Koshi (stiffer), and high Shari (crisper).
Intensive research into this phenomena has established that these aspects of fabric handle can be estimated objectively from low stress mechanical and surface properties (e.g. bending rigidity, staple fibre crimp etc.). The system of instruments developed to measure the required fabric properties is referred to as KES-F (Kawabata Evaluation System - Fabric).
Combinations of these physical measurements have been correlated to subjective handle evaluations using regression techniques. The single figure outcome of these regression equations is referred to as the Total Hand Value (objective).
In this way the low stress mechanical measurements can be used to obtain an objective measurement of fabric handle, that attempts to encompass many of the sensations felt when assessing handle subjectively. It should be noted that these regression equations are different for different fabric types and only appropriate for the type of fabrics for which they have been derived.

## Slide 9: Fabric Handle (subjective): Fibre Diameter
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1982)(eds)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.), Objective Evaluation of Fabric Quality, Mechanical Properties and Performance, The Textile Machinery Society of Japan, p165.
The study shown on this slide was conducted on fabrics made from NZ cross-bred wools. The subjective Total Hand Value rating was determined by experienced judges. A lower hand value was less acceptable. Please note that this is a subjective assessment of fabric handle.
The result indicates that over the wide range of fibre diameter evaluated, higher diameter leads to less acceptable fabric handle.

## Slide 10: Fabric Handle (objective): Fibre Diameter
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.), Objective Evaluation of Fabric Quality, Mechanical Properties and Performance, The Textile Machinery Society of Japan, p173.
Another study conducted using South African Merino wool, in which the Total Hand Value was evaluated objectively, returned a conflicting result for a narrower fibre diameter range. This evaluation was done on a series of fabrics suitable for summer men’s suiting.
It would appear that, measured objectively, the Total Hand Value (THV) improved slightly as the fibre diameter increases.
This can be explained by the fact that the objective measurement of Total Hand Value (THV) was based on equations developed for Japanese summer weight suiting in which both stiffness and crispness are desirable. In a European environment where smoothness and softness would be more important the reverse behaviour may have been found.
This rather different result illustrates the fact that the measurement of fabric handle is a very complex phenomenon, having cultural, social and economic dimensions as well as the technical. Care must be taken when evaluating the prediction of such regression equations.

## Slide 11: Bending Rigidity: Fibre Diameter
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.), Objective Evaluation of Fabric Quality, Mechanical Properties and Performance, The Textile Machinery Society of Japan, p174.
This slide simplifies the matter by just looking at one fabric mechanical property (bending rigidity). A change in bending rigidity is thought to be the major component affecting subjective fabric stiffness.
Fibre diameter is seen in this slide to have a marked effect on fabric bending rigidity for plain and twill weave fabrics. An increase in fibre diameter will lead to fabrics that are more difficult to bend.
A comparison of results for the different weave fabrics shows the effect of fabric construction on bending rigidity. This demonstrates that the fabric construction is generally a key parameter affecting fabric properties.

## Slide 12: Fabric Stiffness: Fibre Diameter & Crimp
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.), Objective Evaluation of Fabric Quality, Mechanical Properties and Performance, The Textile Machinery Society of Japan, p178.
This slide shows the effect of fibre diameter and staple fibre crimp on “KOSHI” (a primary handle value related to fabric stiffness or limpness). A higher KOSHI value means the fabric is stiffer.
This graph indicates that higher diameter fibres lead to stiffer fabrics and that higher crimp fibres lead to stiffer fabrics.

## Slide 13: Fabric Handle: Staple Crimp
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.), Objective Evaluation of Fabric Quality, Mechanical Properties and Performance, The Textile Machinery Society of Japan, p175.
Shear stiffness is a measure of the difficulty of deforming a fabric at an angle (usually 45o) to the warp and weft yarn directions. The effect of fibre crimp on fabric shear stiffness is shown in this slide.
It would appear that higher crimp fibres will produce fabrics which are harder to shear. This effect has been attributed to the indirect effect of fibre crimp leading to an increase in fabric thickness. Fabric thickness was also measured in this experiment.

## Slide 14: Fabric Handle (objective): Fibre Crimp
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.), Objective Evaluation of Apparel Fabrics, The Textile Machinery Society of Japan, p199.
This slide again demonstrates the complexity of the objective measurement of fabric handle.
It shows that as another expression of fibre crimp (crimp shrinkage) increases, so does the objective THV. That is, the fabric has a better handle for that particular fabric application.
While this may appear to conflict with the South African data the derivation for objective THV is based on correlating various aspects of handle (KOSHI, HARI etc.) to subjective handle ratings - in this case the summer weight correlations. Therefore the higher crimp fibres in this case produce a fabric more suited to the particular application (most likely a stiffer, livelier fabric is needed).

## Slide 15: Fabric Handle: Fibre Diameter
Subjective
  (increase)
  less supple (stiffer)
  less smooth
  lower preference
    THV (subjective) lower
    NZ X-bred wool
Objective
  (increase)
  THV (objective) higher
  bending rigidity increased
  fabric stiffness increased
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
In summary, a subjective evaluation of a range of fabrics made using a wide range of fibre diameter were judged to be less supple and less smooth as fibre diameter increased, and therefore were less preferable as far as subjective fabric handle was concerned. This study was conducted using NZ X-bred wool.
Conversely a study on a narrower fibre diameter range for fabrics designed for men’s suiting showed that increasing fibre diameter lead to more preferable fabrics as measured objectively for THv using summer weight correlations. The increase in fabric stiffness over this diameter range was preferred as far as this fabric application is concerned.
These contrasting findings demonstrate the care that must be taken when evaluating the effect of fibre diameter on fabric handle. Particularly when the impact of cultural differences in fabric preference can affect the results.

## Slide 16: Fabric Handle: Fibre Crimp
Subjective
  (increase)
  rougher fabrics
    low fibre crimp smoother
Objective
  (increase)
  better quality fabrics
    THV (objective) higher
    bulkier yarns
    more lively yarns
    more retained crimp
  stiffer fabrics
  shear stiffness increased
    thicker fabrics
    more resilient
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
As far as subjective assessment of fabric handle is concerned, more recently published works have judged fabric made from low fibre crimp as more preferable because of its smoothness.
However objective measurements of fabric handle shows an increase in preference for fabrics made from higher crimp fibres when men’s suiting fabrics are considered. The bulkier, more lively yarns are preferred. These yarn properties lead to thicker, stiffer fabrics which are preferred in this application.
These contradictions emphasis the fact that all wools do not fit all applications, and the desired characteristics of the product determine the optimum properties of the raw wool.

## Slide 17: Appearance in wear
Hygral expansion (dimensional)
  reversible
  change in humidity changes weave crimp
Crimp
  (increase)
  hygral expansion increased
  weave crimp increased
Fabric structure and finishing more important
A. de Boos, G. Naylor, P. Auer
Notes: <number>
<footer>
Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Another important aesthetic fabric characteristic is its Appearance (in garment form) in Wear. One of the most important fabric properties that affects garment appearance is hygral expansion. This is a measure of how much the dimensions of the fabric change due to environmental changes.
The mechanism is thought to be as follows. The wool fibre absorbs moisture, as the relative humidity of the environment increases. This leads to fibre swelling and a reduction in fibre crimp and ultimately yarn crimp. This is manifested in a lengthening of the yarn and fabric. If the fabric is constrained by seams, e.g. in a suit coat, the fabric lengthening finally shows up as “seam pucker”. This phenomena is particularly applicable when fabrics and garments are used in high humidity environments.
It has been found that higher crimp fibres will lead to higher hygral expansion. This is particularly relevant considering that in some tailored garments higher crimp fibres are preferred because of their contribution to preferred fabric handle.
However, to keep things in perspective, fabric structure and the finishing routine imposed on the fabric have a greater effect on hygral expansion than fibre properties.

## Slide 18: Fabric Comfort (woven)
Woven
2mm
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Fabric comfort next-to-skin is a particularly important aesthetic characteristic considering consumers’ increased preference for casual clothes.
The lack of fabric skin comfort, sometimes called “prickle” is caused by coarse fibre ends pressing on the skin. A coarse fibre end may be able to press hard enough before buckling to trigger nerve endings just below the surface of the skin. If too many nerves are triggered there can be a “prickle” sensation. For a given fabric, the threshold force for this effect corresponds to a critical fibre diameter. The sensation varies between individuals, and skin types. This phenomenon applies to any fibre type.
The threshold for wool fibre is about fibres of 30m diameter or more. This slide shows the surface fibres on a woven fabric that may cause prickle.
Fabric type has an effect on the threshold level. 30µm applies to normal knitted fabrics, while for typical woven trouser fabrics, where the fibres are constrained to a greater degree and the protruding ends are shorter, the threshold is about 27m.

## Slide 19: Fibre Diameter Distribution
0
50
100
150
200
250
300
350
400
450
500
0
3
6
9
12
15
18
21
24
27
30
33
36
39
42
45
48
51
54
Diameter (m)
Count
MFD = 23.4 CVD = 25.5
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
An illustration of fibre diameter distribution for wool fibres in this slide shows that there is a population of fibres >30µm for this wool sample. This is referred to as the “coarse edge” of the sample. The size of the coarse edge is important for fabric skin comfort.
It should be noted that this distribution isn’t completely symmetrical, however the well known Gaussian or Normal distribution is often a useful model.

## Slide 20: MFD vs. % fibres >30m
5%
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Assuming a Normal distribution, the %fibres >30m can be extrapolated. This slide shows the predicted %fibres >30m plotted against the values found experimentally over a wide range of mean or average fibre diameters. The prediction appears robust. It would also indicate that the normal distribution can be assumed over a wide range of diameters. This is reasonable since the range of CVD in commercial wool tops is generally small.
A useful rule-of-thumb is that if there are less than 5% of fibres >30m, then a typical plain knit sweater will be comfortable on the wearer. This graph shows that wools with an average fibre diameter of 21µm or less will be comfortable in this application.
Some applications can be more critical. For example, men’s wool shirting material may require a figure closer to 2% fibres >30m.

## Slide 21: Contribution to Prickle
relative effect
Fibre diameter (1m) 10
CV of diameter (1%) 3
Fibre length (5mm) -2
Yarn Count (60-100 tex) 0
Cover factor (0.15units) 4
Finishing (raising) -10
A. de Boos, G. Naylor, P. Auer
Source: Naylor, G.R. & Phillips, D.G., (1995)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
This slide indicates the effect of various fibre, yarn and fabric properties, on prickle, as well gives a relative effect rating for those properties. The relative effects of increasing the parameters to the indicated amount are shown in the right hand column.
For example, a 1% increase in CV of diameter is approximately equivalent to a 0.3m increase in average diameter. A change of 5mm in average fibre length would have a similar effect.
Here the effect of average diameter and the finishing operation of raising would have the same effect. Raising actually increases the length of the protuding fibre ends making them easier to buckle and thus the fabric more comfortable.

## Slide 22: Pilling
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.), Objective Evaluation of Apparel Fabrics, The Textile Machinery Society of Japan, p53.
Another aesthetic fabric characteristic that is affected by fibre properties is pilling. This slide illustrates the formation of tight balls of fibre on the surface of a woven fabric. Investigations have found that the average fibre diameter of the fibres in these pills is lower than would be expected from the fabric fibre population.

## Slide 23: Pilling
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.), Objective Evaluation of Apparel Fabrics, The Textile Machinery Society of Japan, p54.
The pills remain attached to the fabric because of so-called “anchor fibres”. When the anchor fibre is broken the pill falls off.
This is a potential problem with fibre blends of wool and synthetic fibres. If the anchor fibre is a synthetic fibre, the pill would be harder to remove than if it was a wool fibre. Therefore, while the formation of pills for pure wool and wool blend fabrics may be equivalent, the pilling of wool blend fabrics may appear worse because the pills aren’t removed during normal wear.

## Slide 24: Pilling: Diameter & Length
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.), Objective Evaluation of Apparel Fabrics, The Textile Machinery Society of Japan, p191.
This graph illustrates the effect of fibre diameter and fibre length on the pilling performance of knitted fabrics. A higher resistance to pilling is better.
From these results it would appear that fabrics made from finer fibres pill more. Finer fibres are more flexible and hence more likely to migrate to the fabric surface and cause pilling. There is only a slight effect of fibre length.

## Slide 25: Contribution to Pilling (knitwear)
relative effect
Fibre diameter 5
Yarn twist 5
Stitch length 10
Finishing (degradative) 10
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
This assessment of the relative contributions of fibre and fabric properties, and finishing indicates that the fabric property of stitch length, and any finishing operation that degrades the fibre has much more influence than fibre diameter. Reducing stitch length makes a tighter fabric. This slide is indicative only as the quantitative changes will depend on the product manufactured.
In general, pilling is worse in fabrics where the fibres are not strongly bound, e.g. in loose knitted fabrics made from low twist yarns.
Recent commercial investigations at Woolaby Australia Pty. Ltd. have indicated that fibre crimp has an effect on pilling performance. The specification of low curvature wool to go into their fine knitted fabrics has resulted in a commercially significant improvement in pilling performance.

## Slide 26: Abrasion: Fibre Diameter & Length
A. de Boos, G. Naylor, P. Auer
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.), Objective Evaluation of Apparel Fabrics, The Textile Machinery Society of Japan, p190.
Abrasion Resistance is another important functional fabric characteristic. This can be measured as mass loss (as in this graph) for knitted fabrics.
The graph shows that increasing fibre diameter and increasing fibre length tend to minimise fibre loss during abrasion. This could be related to the absolute fibre strength and the ease with which fibres could be withdrawn from the fibre assemblies.
It should be noted that abrasion is a complex phenomenon, and some other studies have not demonstrated such a marked effect.

## Slide 27: Contribution of Finishing
Finish
Pressure decatise
Chemical Set
Wet decatise
Piece dyeing
Polymer shrink resist
Effective micron shift
- 5
- 2.5
- 1
- 4.5
+ 4
A. de Boos, G. Naylor, P. Auer
Source: de Boos, A. & Kenin, P (unpubl.)
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Source: de Boos, A. and Kenin, P. CSIRO Textile & Fibre Technology, unpublished data.
The change in a subjective or objective characteristic from a particular finishing process can often be expressed as the “effective micron shift”. For example, a pressure decatised fabric returns an equivalent result to a fabric made from fibres that are 5m finer and minimally finished.
It is interesting to note that a polymer shrink resist process has a relative detrimental effect on fabric handle.

## Slide 28: Finishing Effects
Interaction of MFD and Finishing
0
5
10
15
20
25
18
20
22
24
26
Mean Fibre Diameter
Subjective suppleness
minimum
pressdec
polymer
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
This slide illustrates the effect that several finishing operations (minimal, pressure decatised and polymer shrink resist) have on subjective fabric suppleness. This work was done on equivalent fabrics constructed from 19, 23 and 25m wool fibres. A higher rating is better.
There is a general trend for finer fibres to make more supple fabrics. An interesting result is that a fabric made from 25m fibre that has been pressure decatised is more supple than a minimally finished 19m fabric.

## Slide 29: Wrinkle Recovery
Ability of fabric to recover from deformation (creasing) in wear
Depends on
  fibre stress relaxation
  proximity of Tg to usage temps
    moisture lowers Tg
Contribution of fibre properties is small
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
Wrinkling recovery is the ability of a fabric to resist or recover from creasing during wear. Esssentially, if fibres relax in a new (creased) configuration, they will retain wrinkles. The fibres will relax much more rapidly if their glass transition temperature (Tg) is exceeded in wear, and will recover more slowly if the usage temperature is then lowered below Tg.
The problem with wool fibres is that they absorb moisture so that their Tg can be lowered below the usage temperature in areas of high moisture. The fabric sets in the creased form when the fabric dries out and Tg is raised again above the usage temperature.
However, the contribution of fibre properties such as diameter, CVD and crimp to this phenomenon is small.

## Slide 30: Ease of Garment Manufacture
Depends on
  mechanical properties
  dimensional properties
  pressing performance
  fibre-needle friction
Little information on role of fibre properties in some areas
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
The Ease of Garment Manufacture is a complex characteristic involving the properties listed in this slide.
Unfortunately there appears to be little information on the role of fibre properties in some of these areas.

## Slide 31: Summary
Diameter
CVD
Coarse Edge
Crimp
Style
Fibre Strength
Colour
Contaminants
Aesthetic Functional
10 3
3 1
10 1
4 3
4 2
8
5
3
A. de Boos, G. Naylor, P. Auer
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.
This slide summarises the effects of fibre properties on Aesthetic and Functional fabric properties. It is indicative only since the impact of fibre properties will depend on the product into which the wool is made. The quality of next-to-skin garments are affected by different fibre properties in different ways to that of tweed jackets. It is therefore difficult to be prescriptive.
Fibre diameter and %fibres >30m have the greatest effect on aesthetic properties (fabric handle, prickle), while fibre strength has the greatest effect on Functional properties such as abrasion resistance.

## Slide 32: Further Reading
Postle, R., Kawabata, S., and Niwa, M. (1982) (eds.), Objective Evaluation of Fabric Quality, Mechanical Properties and Performance, The Textile Machinery Society of Japan
Postle, R., Kawabata, S., and Niwa, M. (1983) (eds.), Objective Evaluation of Apparel Fabrics, The Textile Machinery Society of Japan
Notes: Written by: Dr. Allan de Boos & Dr. Geoff Naylor, CSIRO Textile & Fibre Technology, and Dr. Peter Auer, The University of New South Wales.