## Slide 1: Fibre Breakage in Carding
Produced for the CRC for Premium Quality Wool undergraduate program by;
Gary Robinson, CSIRO Textile & Fibre Technology.
Notes: This module examines the cost benefit of less fibre breakage during carding.
The module also looks at the locations for fibre breakage in the card.
The effect of lubrication during carding is examined, as well as the effect of the moisture content of the fibres on fibre breakage.
Produced for the CRC for Premium Quality Wool undergraduate program by Gary Robinson, CSIRO Textile & Fibre Technology.

## Slide 2: Effect Of Top Length On Price
20
21
22
7
8
9
10
11
40
50
60
70
Mean Fibre Length in Top (mm)
PRICE
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
The value of a top is determined largely by fibre diameter and fibre length.
This diagram shows that the price paid for a top of a particular diameter increases as the mean fibre length (MFL) of the top increases.
The major increase in price is for tops between 60mm - 65mm in length. This length range is the predominant range requested by spinners. Price tends to plateau after about 65mm as the demand from spinners for this length top is reduced due to perceived technical complications. The demand for these wools may change in time as the results of current spinning trials using longer Hauteur wools becomes more widely known.
Therefore there is a price benefit in increasing the MFL of a top. This can be achieved by using longer raw wool, which is more expensive, or by reducing the amount of fibre breakage during early stage processing (ESP).
Carding is a major location for fibre breakage during ESP, and is an obvious place to try and achieve less fibre breakage.

## Slide 3: TEAM Formula
H = 0.52L + 0.47S + 0.95D - 0.19M* - 0.45V - 3.5
    where
    H = Hauteur (mm)
    L = Staple length (mm)
    S = Staple Strength (N/ktex)
    D = Fibre Diameter (µm)
    M* = Adjusted percentage of middle breaks
    V = Vegetable Matter base (%)
VALUE OF TOP
  EACH 1mm DECREASE IN HAUTEUR 10c/kg LOSS
  EACH 1% INCREASE IN NOIL 7c/kg LOSS
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
If the mean fibre length (MFL) in the top (also known as Hauteur), is determined by the amount of fibre breakage which occurs in processing, then an examination of the TEAM formula can tell us something about the quantitative advantage of increasing Hauteur. Some illustrative figures are included in this slide.
Another way that the value of the raw wool can be increased is by decreasing the amount of short fibre removed in combing, as measured by Noil%. Noil is sold as an input for woollen processing, but at lower price than top. It should be noted that the price relationship between noil and top varies depending on market fluctuations.
Both of these occurrences, decrease in H and increase in Noil, cost money. Therefore fibre breakage costs money.

## Slide 4: Cost Implications (21 m Top)
LOSS: 2mm Hauteur 20 c/kg
LOSS: 1 percent unit Romaine 7 c/kg
TOTAL 27 c/kg
Within MILL 2 tonne / hr
$540 / hr
50 Tonne Consignment
25hr mill time
$13,500
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
This slide demonstrates how much money in terms of mill efficiency can be caused by fibre breakage embodied as loss in H and increase in Noil.
Even very small changes in Hauteur or Romaine can have quite significant financial implications in the processing mill.
Some illustrative figures are given in this slide.
The mill manager needs to have a good understanding of fibre properties and fibre machinery interactions to successfully run a processing plant. The manager could also be helped by understanding how to achieve less fibre breakage.

## Slide 5: Fibre Breakage in Carding
Source: G. Robinson (1996)
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
Source: Robinson, G. (1996) Carding: Fibre Breakage, In: Seminar Proceedings of Top-Tech ‘96, p.30.
The majority of fibre breakage takes place on the card. On average at least 30% of wool fibres break at least once during the carding process.
Studies at CSIRO using polymer coated fibres have identified just where on the card that fibre breakage occurs. A profile of fibre breakage and damage along the carding machine can be seen in the above diagram. It would appear that fibres don’t break at an even rate throughout the card.
The elements which contribute to fibre breakage are
density of fibres being processed
frictional interactions between fibres in relative motion
frictional forces between fibres and metal pins
the physical properties of the fibres themselves such as strength and extension
the presence of entanglements and impurities, especially vegetable matter.

## Slide 6: The Effect of Lubrication at the Card
Hauteur
  increases
Noil
  decreases
less fibre breakage
78
76
74
72
70
68
66
7
6
4
OILED
NOT OILED
15
25
35
45
55
65
CARD PRODUCTION RATE kg/h
NOIL %
HAUTEUR mm
NOT OILED
OILED
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
When wool enters the card it undergoes fibre-fibre and fibre-metal frictional forces.
Studies at CSIRO have shown that fibre-metal forces are the important forces to affect fibre breakage. The use of carding lubricants lowers fibre-metal forces and reduces fibre breakage.
The diagram shows the influence on top length (Hauteur) and combing waste (%Noil) of the addition of a light mineral oil. Hauteur has been increased and %Noil has been reduced by using the lubricant.

## Slide 7: Hauteur and Coefficient of Friction
H mm
0
2
4
6
8
10
12
0.18
Wool
Micron
20
21
23.5
23.5
21
21.7
21.7
0.20
0.24
0.28
0.32
0.36
0.38

commercial
lubricants
No Oil
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
It would then follow that further reduction in fibre-metal friction would lead to further reduction in fibre breakage. The magnitude of this friction can be estimated by measuring the coefficient of friction () between the fibre and the metal.
The diagram shows the relationship between the fibre-to-metal friction for a range of different lubricants and the gain in Hauteur of the top. As the selection of different lubricants reduces the frictional forces, H is increased.
In a similar manner, reduced fibre-metal friction improves the yield of good fibre through reducing the amount of combing waste (%Noil).
The shaded area shows the range covered by commercial lubricants available at the time of these studies. There would appear to be benefits to topmaking through the development of new lubricants.
The use of new lubricants must be balanced against their effect on further processing. The lubricant may benefit top-making, for example, but be difficult to remove and therefore hinder the application of dyes.

## Slide 8: Moisture Content & Fibre Tensile Properties
Dry fibre
60% r.h.
(-14% regain)
Wet fibre
PERCENT EXTENSION
LOAD
0
10
20
30
40
50
60
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
The strength of wool fibres is strongly dependent on their diameter. Finer fibres are weaker.
The tensile properties (strength and elongation at break) are also influenced by the moisture content of the fibres. This diagram shows how altering the moisture content of the wool fibre changes its tensile properties.
Therefore increasing moisture content increases extension at break which is good for carding but reduces the strength of the fibre which is a poor result for carding.
Another factor that may also be important is the recovery from extension. This is how much a fibre returns to its original dimensions after having a load placed on it.. A wet fibre at 20ºC recovers completely from a 20% extension, while a fibre in an atmosphere of 20ºC and 65% RH will recover by only 40% of the extended length.

## Slide 9: Optimum Regain
Card
Production
Time Delay
Before
Processing
Hopper
Regain
Combing
Noil, %
Hauteur
“
“
“
“
“
“
“
“
15.7
18.4
20.5
26.7
Means
4.31
4.40
4.38
4.55
4.43
81.2
80.7
81.2
80.4
81.2
55
“
“
“
“
7 days
“
“
“
“
3.6
15.2
17.0
21.0
24.6
Means
4.40
4.39
4.37
4.35
4.54
4.41
81.4
81.6
82.0
80.8
80.4
81.2
55
None
3.0
4.52
82.3
G. Robinson
Notes: Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
The question of the optimum regain at which to card is a very important one for the topmaker. The considerations on moisture content and tensile properties of the fibre give no clear leads so one is thrown back onto experimental investigation.
Results of studies at CSIRO are given in this slide. These results indicate that neither the level, nor the difference in variation in regain, as a result of differing practices before carding, have any great effect on Hauteur and % Noil.
However, it should be noted that the level of Regain has been found to be important for VM removal in carding and to minimise static electricity. For more information see the “VM Removal in Carding” module.