## Slide 1: Yarn Twist
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module explains the important principle of twist. Twist characterises yarns, and aspects such as twist level, twist angle, twist factor, and twist levelling (drafting) are explained.
Twist is also applied to slubbings and rovings before spinning, but usually as false twist.
The author would like to thank Assoc. Prof. Xungai Wang from Deakin University for his valuable input into this module.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Twist Types
Z
S
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The concept of twist with respect to fibre assemblies, such as rovings and yarns will be discussed, but limited to yarns for the sake of simplicity.
Ideally fibres spiral around the yarn axis as represented in this diagram.
Twist direction is designated "Z" or "S" according to the direction of spiral of the fibres around the yarn axis. The direction of spiral corresponds to the downstroke of the letters “Z” or “S”.
Z twist is more usual in worsted ring spinning, since the yarn is usually being rotated clockwise during that process.

## Slide 3: Twist Level
numbers of turns per length
  turns per metre (tpm)
  turns per centimetre
  turns per inch (tpi)
increase twist level
    assume same Tex
  increase twist angle
  slower spindle production
  more expensive yarns
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The amount of twist in a fibre assembly is the twist level measured in turns per length (usually turns per metre (tpm), or turns per inch (tpi)).
In an ideal yarn with perfect evenness, an increase in twist level will result in an increase in twist angle, if the linear density (tex) of the yarn is the same.
In a real yarn, the linear density varies and while the average twist level will stay the same the localised twist level and twist angle vary according to the linear density. This leads to the phenomenon of twist variation and twist levelling (see the following 2 slides).
Twist Level (tpm) = Spindle Speed (rpm) / Yarn delivery speed (mpm)
This formula shows that as the twist level is increased, and the spindle speed is constant, the yarn delivery speed decreases. The higher the twist level that is applied to a yarn the slower it is produced. Therefore high twist yarns are more costly to produce.

## Slide 4: Twist Angle
spiral formation after twist
  twist angle ()
applied linear force
  outer fibres pulled to core
yarn compactness
fibre coherence
  increased yarn strength
    limited

Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Ideally twist results in a spiral configuration of fibres around the fibre assembly axis. The angle between the yarn axis and the fibre spiral is the Twist Angle ().
Twist achieves a compact structure, more twist achieves greater compactness. The coherence of the structure can be increased by further increases in the twist level, i.e. increased twist angle.
A low twist yarn will have a low twist angle, and low compactness.
This is a “self-locking” assembly. Providing the initial coherence of the assembly is sufficient, an applied lateral force (blue arrow) will pull the outer fibres to the core of the assembly. These induced transverse forces lead to higher inter-fibre friction and a greater degree of coherence in the assembly.
A low twist angle (lower) means that fibres are able to slide past each other while a high twist angle ( greater) leads to high transverse forces and fibres will break before sliding. Therefore, twist angle determines the yarn strength up to the point where slippage is eliminated. Past this point, increased twist will detrimentally affect yarn strength since the whole structure is locked up.

## Slide 5: Twist Levelling
twist angle () varies
  number of fibres in X-section
  same twist (turns / cm)
thin: > twist angle
thick: < twist angle
apply tension during twist insertion
  fibres slide in thick places
  twist levelling effect
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
If fibre assemblies of differing linear densities have the same fibre diameter, this means that the number of fibres in the cross-section of the yarn will vary.
A thin spot in a fibre assembly has less fibres in the cross section, consequently when twist is applied to that fibre assembly, the twist angle will be slightly greater at the thin spot, and slightly less at a thick spot. It is an axiom in spinning that "the twist runs to the thin spots". The average twist level over the whole yarn will be constant, but there will be localised variations in twist level and twist angle.
If a thin spot has enough twist whereby fibre slippage is just prevented by lateral forces, then it follows that an amount of drafting will occur at the thick spots when tension is applied, since the twist level and angle in the thick spot is insufficient to maintain cohesion of the fibres, i.e. the lateral forces are low.
This phenomenon is referred to as “twist levelling” and “drafting-against-twist”. The result is a re-distribution of twist and the localised drafting improves the yarn evenness since thick places draft more than thin places in the assembly.

## Slide 6: Twist Factor
Constant (K)
yarn comparison
  “yarn character”
  maintain same K
    lower Tex needs higher tpm
    lower tpm needs higher Tex
  higher K
    harder, tighter yarns
      cf. softer, looser yarns
Peter Auer
tpm x  Tex  Twist Factor (K)
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
”Twist Factor” is a difficult concept but important because it is a way of comparing yarns of different twists and different linear densities.
Twist factor is used to assess hardness and softness of yarns and defines yarn character. Yarns with similar character will have similar twist factors.
One formula for twist factor is shown in this slide, however a number of different formulae are used in the textile industry depending on spinning system, fibre type, the units of linear density and location. “Twist ” and “twist multiplier” are other terms that are used.
The formula shows that to achieve a yarn of similar character with a lower tex yarn, you must increase the twist level to keep the twist factor the same. If the twist level was maintained then yarn of a different character would be produced (softer and looser).

## Slide 7: False Twist
S
Z
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Alternating Z and S twist can be achieved in fibre assemblies, e.g. rovings, woollen slubbing. This is called “false twist”.
In the diagram above a twisting force is applied to the middle of a fibre assembly. S twist will form on the left-hand side of the position where the twisting force is applied, Z twist will form on the other side.
If the assembly is moving passed the twisting point, and the twisting force is reversed, then the opposite occurs, Z twist on the left hand side, and vice versa. This alternating twist is called “false” twist, since the net twist is zero.
There are regions of zero twist along the length of the assembly where the reversal of twisting force occurs. In contrast if the twisting force is one direction only, then real twist is the result.