## Slide 1: Combing Principles
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module introduces the concept of combing, gives some of its history, and allows a perspective of where combing sits in the worsted process.
The module will concentrate on the French comb and describe its sections and their part in the combing sequence.
It is recommended that the reader has an understanding of gilling and fibre assemblies (especially slivers) before using this module.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Introduction
Peter Auer
Aims
  remove short fibres
  remove VM
  remove neps
  fibre blending
    doubling
  fibre straightening
    combing action
    hooks removed
Glossary
  noil
  % noil
  % romaine
  tear ratio
  sliver
    gilled
    combed
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The primary aim of combing is to remove short fibres from gilled slivers. Other important aims are the removal of as much of the remaining VM as possible, and also to take any neps out of the slivers. Secondary actions are fibre alignment, since fibres are being combed, and blending, since slivers are being doubled and drawn.
The following are terms that are used regularly in combing.
Noil is the short fibre removed from the gilled sliver. There is usually a fair component of VM mixed with the noil. The noil is used as a raw material in woollen processing.
%noil is the %ratio of noil to top and noil as a percentage
%romaine is slightly different, being the %ratio of noil compared to the card input. This term is more commonly used in Europe
tear ratio is the ratio of top to noil (usually between 8 and 12)
Gilled sliver is the input for a comb, combed sliver is the output. The sliver is not technically a TOP until it has gone through the next process of finisher gilling.
Up to 32 gilled slivers can be fed into a comb, while the output is only one combed sliver. Therefore there is drafting and doubling occurring during combing with implications for improving evenness and blending.

## Slide 3: History
Noble Comb
1790
  Cartwright's Big Ben
1851
  Lister Comb
1846
  French Comb (rectilinear)
1853
  Noble Comb (circular)
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Combing is intended to remove short fibres from a gilled sliver, as well as neps (bundles of short fibres) and VM. It also acts to straighten and align the fibres in a sliver.
Short fibres generally exist as a result of fibre breakage in carding, while neps can be generated in either carding or gilling.
VM is generally in small particles, however longer fibre-like particles are a particular concern.
Hand combing prevailed until the end of the 18th Century. Hand-combing guilds were quite powerful in Europe, and the work was very specialised.
A machine called Big Ben was developed between 1790-92 but was a failure due to high maintenance, unreliability, and it was suitable for long staples English wool only. A similar fate awaited Lister’s invention of 1851 which was also only suitable for long English wool, mohair and alpaca.
The first commercial comb was the Noble comb developed in 1853 using a circular configuration. This competed commercially with the French comb until the 1950’s but is now out-dated for economic reasons.
In 1846 Heilmann developed the rectilinear comb for cotton. The French company Schlumberger, owners of the patent, adapted it and made it a commercial success. The rectilinear comb has succeeded by offering faster production, less fibre breakage, and better VM removal.
The Schlumberger company is still the major manufacturer of rectilinear combs. The other significant manufacturer is S'ant Andrea Novara (SAN).

## Slide 4: NSC PB32
Circ Comb
Funnel
Input Nip
Front Comb
Peter Auer
Picture courtesy of CSIRO
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
This slide shows a view of a modern comb, in this case an NSC PB32. It is possible to make out the fibre feed from the input nip, the front comb, the circular comb, the delivery apron, and finally, the trumpet delivery of the combed fibre into a can below (not shown).
Use this picture to visualise the diagram in the following slide.

## Slide 5: French (rectilinear) Comb
FEEDROLLERS
FRONT
COMB
CIRCULAR
COMB
SHOVEL PLATE
APRON
Peter Auer
Source: Brearley, A., (1964)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Brearley, A., 1964, Worsted, Pitman Press
This slide is a schematic of a French or rectilinear comb. Various parts of this diagram are expanded on the following slides to examine each section of the comb more closely.

## Slide 6: Feed Section
Creel
Feed Rollers
Feed Gill
Nip
Shovel Plate
FRONT COMB
SHOVEL PLATE
FEED ROLLERS
Peter Auer
Source: Brearley, A., (1964)
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source: Brearley, A., 1964, Worsted, Pitman Press
Up to 32 gilled slivers from a creel are fed into the feed gill by the feed rollers. The comb loading refers to the total linear density of the input slivers (420g/m for Xbreds, 340g/m short, fine wool). There is a positive feed on creel to prevent drafting during feeding.
The length of feed is controlled by the feed rollers usually by a ratchet mechanism. The feed length is less for shorter wool.
The feed gill consists 3 plates: a grooved plate below the wool, a slotted plate above wool, and an upper pinned plate. The action of the pins is to hold the wool when they are pushed through the slots and the wool. The entire feed gill (is able to move) moves back and forth as a unit, the pinned plate can be withdrawn.
The feed gill disengages by lifting the upper pinned plate during the feeding stage. It disengages when the fibres are held by the nip. It stays engaged during detaching to prevent the whole fibre mass being dragged forward. The tuft of fibres being detached each cycle is very small, so fibres can be withdrawn even if they are held.
A "beard" (fringe) of fibres protrudes from the feed gill after wool is fed through the feed gill (pins raised). This fringe is held by the nip, consisting of upper and lower nipper jaws.
The shovel plate is located below the feed gill and supports the beard as it is presented to the drawing off rollers. This shovel plate device is unique to the worsted system due to the longer wool fibres. It isn’t found in a cotton comb.

## Slide 7: Circular Comb Section
Circular Comb
  comb sections
Nipper Brush
Noil Brush
Waste Collection
  Fillet Roller
  Doffing Comb
  Noil Boxes
  Dust Box
FILLET ROLLER
Peter Auer
Source: Brearley, A., (1964)
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source: Brearley, A., 1964, Worsted, Pitman Press
The Circular comb has two segments. The first segment presented to the beard is coarse (4-17 pins/cm) and contains about 10 rows of pins. The second segment is finer.
The pin density increases for finer wool types. The following figures are for the Schlumberger comb.
19-24pins/cm Xbred
19-30pins/cm 64's quality and finer
The beard is pushed into the pins on the Circular Comb by the Nipper brush, which is attached to the upper nipper jaws. This make combing the beard more efficient. The beard is only about 30mm long, compared to a total fibre length of up to 180 mm.
The fibre removed by the circular comb is called noil. The circular comb is kept clear of noil by a circular brush in order to maintain combing efficiency.
The nipper brush is attached to the upper nipper jaw and pushes the beard into the pins of the circular comb, ensuring effective removal of short fibres, neps and VM.
Waste collection is achieved below the Circular Comb. The noil is stripped off the Noil Brush by the Fillet roller. The Doffing Comb oscillates to clean the Fillet roller and the noil is collected and baled for sale. The action of the Fillet roller stripping the Noil Brush may lead to a heavier type of noil called 2nd noil. This depends on the type of VM present in the wool.

## Slide 8: Drawing-Off Section
Front Comb (separate)
Drawing-off Rollers
Apron
Sword
  redundant
Sliver Collection
  Funnel
  Calender Rollers
  Can
FRONT COMB
Peter Auer
Source: Brearley, A., (1964)
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source: Brearley, A., 1964, Worsted, Pitman Press
The Front Comb (or Top Comb) is an extremely important element of the drawing-off section, mainly because it provides the ultimate control of the quality. The pin density of the Front Comb can be between 22- 28 pins/cm.
The Drawing-off rollers are fluted and barrel-shaped to maximise the grip on fibres in the beard. There is a leather Apron between the Drawing-off rollers which acts as endless support for the combed fibres that are laid on it. The leather gives an even grip which is essential for finer fibres.
The apron winds backwards and forwards while the apron carriage moves in and out.
The swords, which are not shown, are curved metal plates which ensure the combed fibres are laid flat onto the Apron. In later combs, swords are now only used for long fibres such as flax, and are no longer used for wool.
The whole detaching unit described above (except for the front comb) oscillates back and forth during combing. It should be noted that the front comb moves forwards with the feed and is independent of the drawing-off section.
Combed Sliver is collected by being taken off the Apron by exit (calender) rollers. The sliver is condensed as it is drawn through the Sliver Funnel. The sliver is finally coiled in a Can.
Modern combs pass the sliver through a crimper box to enhance sliver tenacity before the sliver is collected in the can.

## Slide 9: Combing Sequence: Part 1
Feed direction
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
This is the combing sequence starting from just after the last tuft of fibres has been detached:
1. Feed Gill disengaged
2. Detaching unit at maximum distance from nip.
3. Gilled sliver bed fed forward by the feed rollers (not shown)
4. Feed Gill engages and moves sliver bed forward to nip position
5. Upper nipper jaw lowered to nip beard of fibres
6. Feed Gill disengages and moves backwards
7. Circular comb combs beard (nipper brush pushes fibres down into comb)

## Slide 10: Combing Sequence: Part 2
Feed direction
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
8. Circular comb moves out of the way
9. Feed Gill engages
10. Nip disengages
11. Detaching unit moves towards nip
12. Apron rotates backwards to provide overlap for detached tuft of fibres
13. Front comb engages beard
14. Detaching rollers start detaching while moving forward to closest position possible
15. Deatched tuft is laid on Apron while Detaching unit is moving away from nip
16. Detaching unit reaches maximum travel

## Slide 11: Fibre Breakage
Hooked Fibre
Neps
Pin Slicing
Nip point
Leading hook
(nipped)
Circular comb
pin
Feed direction
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Fibre breakage is not the problem that it is during carding, however it still occurs.
The main cause of fibre breakage is when a leading hook is nipped. The diagram shows this occurrence. If a leading hook is nipped then it will always be broken during circular combing. The broken end of the fibre is likely to end up in the noil, depending on its length.
Neps, or fibre conglomerates may cause fibre breakage as they are drawn through the front comb.
If the density of fibres is too great then fibres may be jammed into the space between the front comb pins and be either damaged slightly or sliced.

## Slide 12: Noil Selection
(nip 1)
C
B
A
D
sliver
detachment
setting
combed
length
L
T
L
T
Fibre 1
Fibre 2
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
This diagram and the one following explain how the length of fibre and machine settings determine which fibres are selected for noil and which are selected for the sliver. The green striped triangle represents a sliver beard during combing.
The length CD is called the detachment setting (the closest distance possible between drawing-off rollers and the nip). This is also commonly called the nip or gauge setting.
Line C is the nip, line A is the end of the beard. Length AC is the length combed by the Circular Comb. Therefore all fibres shorter than AC are removed in the first part of the combing sequence. This includes short fibres, neps and VM trapped by the Front Comb in the previous sequence.
During drawing-off, the drawing-off rollers eat into the beard and all fibres with leading ends in between line A and line D will be detached to combed sliver. The nip is open during this operation.
Therefore, the shortest fibre in combed sliver must be > CD, i.e. just longer than the detachment setting since fibres longer than this will be held in the nip during combing.
There are two fibres represented in the diagram with leading (L) and trailing ends (T) marked.
Fibre 1 would have been combed out to the noil.
Fibre 2 would have been retained for this cycle since the trailing end was held by the nip during combing.

## Slide 13: Noil Selection
(nip 2)
C
B
A
D
sliver
detachment
setting
combed
length
E
feed
T
L
Fibre 2
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The diagram above represents the next Circular combing cycle. The nip is now at a line E. The sliver mass has been fed forward by a length CE, called the feed length. Therefore ED is length to be combed in this cycle.
All fibres with trailing ends between C and E will be removed to the noil in this cycle l. This would happen to Fibre 2 this cycle. These trailing ends were nipped during the last cycle but not this cycle.
Therefore the longest fibre in noil possible will be CD + CE (the detachment setting plus the feed length).
Now, since AD must equal CE (the machine must be feeding at the same rate it is detaching), the longest fibre in noil can also be expressed as CD + AD.
Thus the detachment setting (CD) determines the shortest fibre in combed sliver.
The detachment setting plus the feed length (CD + CE/AD) determine longest fibre in noil.
Therefore the shortest fibres possible in the combed sliver are determined by how close the drawing off rollers can approach the nip, i.e. you can control the short fibres in the sliver by adjusting the detachment setting.
The longest fibre in the noil depends on this setting PLUS how much sliver is fed into the comb, i.e. feeding more sliver length into the comb at each cycle will increase the noil (waste) from the comb if the detachment setting stays the same.
N.B. fibres may be poorly aligned between DE and fibres longer than CD + CE may be found in the noil.