## Slide 1: High Speed Carding
Produced for the CRC for Premium Quality Wool undergraduate program by;
Gary Robinson, CSIRO Textile & Fibre Technology.
Notes: This module examines how the productivity of worsted carding has been significantly improved by increasing the speed of carding.
The usual measure of carding speed is the speed of the main cylinder or swift. Other card components are usually locked in set speed ratios.
Produced for the CRC for Premium Quality Wool undergraduate program by Gary Robinson, CSIRO Textile & Fibre Technology.

## Slide 2: Increasing card productivity
wool < other fibres
$1M per card
  lowest productivity in topmaking
increase productivity
  increase width
  limit reached
  3.5m
Is there another way?
  increase rate of feed
  INCREASE SPEED
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
Prior to the introduction of high speed cards, the productivity of worsted carding had fallen well behind the carding productivity for other fibres. Typically for 21m wool, carding production rate was 40kg/m/h whilst for cotton, card production rates were 60-80 kg/m/h.
The cost of worsted carding is relatively high, and so its productivity must be raised to compete on a more even basis with other fibres.
Worsted cards, with a capital cost of about A$1.0 million are extremely expensive machines with the lowest production per unit of invested capital of any machine in topmaking.
Card production can be increased by:
(i) Increasing the rate at which fibre is processed through the card.
(ii) Leaving the amount of fibre being carded constant, and increasing the width of the card.
(iii) Increase the speed of carding.
The only response from manufacturers of cards to increase card production had been to increase card width which has now reached 3.5m. This width is considered the maximum, as engineering limits have been reached and maintenance problems are encountered with wider cards.

## Slide 3: The effect of increased feed
CARD PRODUCTION RATE kg/h
74
72
70
68
66
7
6
5
4
15
25
35
45
65
HAUTEUR mm
NOIL %
55
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
Simply increasing the rate at which fibre is being processed by the card has a detrimental effect on the two major determinants of carding efficiency, Noil% and Hauteur (average fibre length as measured at the top stage). This is seen in this slide which are results from work conducted at CSIRO.
These results mean that this method of increasing card productivity results in more wastage in combing and shorter fibres in the top. This is due to increased fibre breakage.

## Slide 4: Fibre flow on the Worsted Swift
WORKER
WFD
TFD
DOFFER
STRIPPER
working
zone
SWIFT
RFD
FFD
ANGLE STRIPPER
RFD
FFD+RFD=TFD
VW
VS

G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
Fibre movement throughout the card is a complex matter.
The probability of fibres transferring or not transferring at any point is dependent on fibre properties, speed ratios, distance between various elements, wire geometry, fibre density at that point and the general condition of the wire.
A term dealing with the amount of fresh fibre being fed onto the swift can be defined thus:
Fresh Fibre Density (g/m2) = Production Rate (kg/h) x 1000
Card width (m) x Cylinder speed (m/min) x 60
FFD is the difference between the total fibre density (TFD) on the swift and the amount of fibre being recycled on the swift (recycled fibre density or RFD). Obviously the fibre making up RFD is not transferred to the doffer.

## Slide 5: Effect of FFD & Card speed (design)
Experimental
Condition
I
II
III
IV
Card
Rate
(kg/m/h)
17
30
30
53
Production
Card
Speed
(Swift
m/min)
450
450
800
800
Fresh
Fibre
Density
(g/m )
2
0.6
1.1
0.6
1.1
G. Robinson
Notes: Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
CSIRO studied the role of card speed in 1985.
When the swift speed is altered, the complete machine changes speed.
The experimental design for these studies is shown in the table above.
Condition II was considered a "standard" condition for carding 21 µm wool in 1985.
Condition III card speed was increased to 800 m/min and normal production was achieved at the low value of Fresh Fibre Density (FFD) of 0.6 g/m2.
Condition IV used elevated speed with normal FFD of 1.1 g/m2 to give very high production rates.
Condition I completes the comparison.

## Slide 6: Effects of FFD and speed
HAUTEUR mm
NOIL %
I
II
III
IV
69
68
67
5.0
4.5
4.0
Carding Conditions
0.6 1.06 0.6 1.06 Fresh Fibre Density (g/m2)
30 52 52 90 Card Production Rate (kg/h)
450 450 800 800 Swift Surface Speed (m/min)
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
Results for H and Noil% produced in this study are shown in this slide.
Compare condition I to condition II and condition III to condition IV.
In both cases, Noil% increases and Hauteur reduces with increasing production rate.
Now compare I with condition III and condition II with condition IV.
No penalty of Noil% or Hauteur is incurred while production rate has increased.
Conclusions: There is no significant effect of card speed on fibre breakage even though traditional speeds have nearly doubled. Noil% and Hauteur are determined by FFD.
Increasing card speeds can be used in TWO ways:
1. There has been a gain in product quality and waste control at constant production rate- Condition II to condition III.
2. In passing from condition II to condition IV, a large gain in production rate has been achieved without any deterioration in top length or increase in noil.
However, if a mill didn’t wish to increase carding production rate because of processing constraints further down the processing line (e.g. production capacity limits in combing), an increase in card speed associated with a decrease in FFD would give a product with higher Hauteur and lower combing noil. This is the desired benefit that mills strive to achieve.

## Slide 7: Problems with increased speed
Feeding
  better control needed
VM removal
  burr beater design
Delivery
  doffer design
Air Control
  more movement of air
  more fly
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
Increasing card speed can lead to significant gains in card productivity. However, CSIRO studies showed that the increased speed (beyond 900 m/min) can in itself lead to further difficulties in carding such as:
feeding, where better control was needed
VM removal was reduced due to inefficient burr-beaters
delivery, or removal of web from the doffer
plant pollution from more air movement and increased fibre fly.
Further studies have overcome these difficulties, as discussed below and on the following slides.
Adapted off-the-shelf technologies such as electronic sensors and radio isotope absorption techniques have been employed to better control the feeding of the wool into the card.
Plant pollution can be overcome with the enclosure of the card. Some cards are now totally enclosed and have dust extraction equipment connected with the capabilities of introducing fresh air which is moisture controlled into the system. This has the added advantage of doing away with water sprays to control static electricity.

## Slide 8: Effect of Card speed on VM content of Tops
VM Content - Points
Card (Swift) Speed (m/min)
Conventional Burr
Removal System
“New” Burr
Removal System
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
The mechanism of burr-beaters can be likened to a golf-club hitting a golf ball. The large VM particles are flicked out of the fibre mass.
The operation of the burr-beaters at high speed requires them to rotate at a speed such that the natural vibrational frequency of the material from which they are manufactured is reached. The burr-beaters resonate and lose efficiency beyond this speed.
A new burr-beater design overcame this problem, as evidenced by the reduction in the number of VM particles in the card web. It is also significant that this design leads to reductions in VM at “normal” speeds.

## Slide 9: New Doffing System: Noil% improvement
Noil %
Production (kg/h)
New System
Single doffer
800
135
210
4.5
7.5
6.0
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
At high card speeds the single doffer employed on “conventional” cards was unable to cope with the increased fibre load. This resulted in increased fibre breakage as measured by Noil% at combing.
A double doffer system proved to be the answer to this problem, whereby a second doffer is added in tandem to cope with the increased fibre load. The two webs coming off the doffers are combined in the condenser funnel at the end of the card.

## Slide 10: High Speed Carding Results
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
After overcoming these difficulties, CSIRO, in 1990, formed a collaborative agreement with the major worsted card manufacturer, Thibeau, France and a local topmaker G.H. Michell & Sons.
Studies have been undertaken on this new experimental card and a typical set of results is given in the above table.
The results indicate that only at the very highest card (swift) speed of 1444 m/min has there been any deterioration in card performance, and this only in the combing Romaine and perhaps the VM content of the tops.
The outcome of these studies is the industrial proving of a new generation of worsted carding machinery. Due to the increased flexibility of this machine compared with previous wool cards, this new generation will revolutionise the way in which carding technologists approach the processing of wool.

## Slide 11: CARD production rates (Thibeau Cards)
+50%
+80%
+85%
+110%
G. Robinson
Notes: <number>
<footer>
Written by: Gary Robinson, CSIRO Textile & Fibre Technology.
Further trials have shown that the productivity increases for the new generation of Thibeau cards can be translated into results for various types of wool as shown on this slide.
Since the release of the high speed card more has been learned and higher production rates have been achieved. Although the card production rates for cotton have also increased in recent years the difference between wool and cotton card production has decreased. Wool is now on more competitive terms with cotton in terms of carding technology.