## Slide 1: Evenness (of Fibre Assemblies)
Produced for the CRC for Premium Quality Wool undergraduate program by;
Assoc. Prof. Xungai Wang, Deakin University, and
Dr. Peter Auer, The University of New South Wales.
Notes: Evenness or low irregularity is vitally important in both the processing and subsequent usage of fibre assemblies like slivers and yarns. This module examines the significance of evenness and how it is measured.
It is recommended that the modules “Fibre Assemblies” and “Drafting Principles” are viewed in conjunction with this module.
Produced for the CRC for Premium Quality Wool undergraduate program by Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.

## Slide 2: Definition of Evenness
Evenness of Fibre Assemblies
  e.g. colour, twist, hairiness
commonly linear density changes
  mass per unit length (e.g. g/km or tex)
Assessed by
    CV of linear density (CV%)
    deviation from mean linear density (U%)
    Mass Diagrams
    Spectrograms
Xungai Wang & Peter Auer
Notes: <number>
<footer>
15
Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
Fibre assemblies such as slivers, tops, rovings and yarns may exhibit irregularity in a number of parameters such as their colour, the level of twist, or yarn hairiness. However, the most common and important evenness parameter is that of linear density. This is because the evenness in linear density affects the evenness in other parameters such as twist and strength.
Evenness refers to how the mass of the assembly changes over the length of the assembly. Considering that such things as fibre length and fibre density will not have significant effects over long lengths, this change in linear density has been attributed to the change in the number of fibres in the cross-section of the fibre assembly.
This common evenness parameter can be measured by such parameters as the CV of linear density (CV%), or the deviation from the mean linear density (U%). Alternatively, some further analysis of the results may return information on how the mass changes over length (Mass Diagrams), or the frequency of these mass changes (Spectrogram).
Many of these measurements relate to the industry standard machine used in mass evenness testing, the Uster Evenness tester.

## Slide 3: Significance
slivers and rovings
  less even products
  material wastage
yarns
  strength variation (thin places)
  production efficiency
    more ends down (spinning, winding)
  number of fibres in yarn cross-section is critical
fabric
  production efficiency
    more yarn breaks in weaving & knitting
  uneven appearance
    barre (woven)
    weft knitted
Xungai Wang & Peter Auer
Notes: <number>
<footer>
16
Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
The significance of changes in linear density of fibre assemblies is manifested at various stages of processing.
Slivers and rovings may be uneven and cause machine breakdowns with subsequent material wastage. Uneven slivers and rovings will also produce uneven products. The Law of Doubling and the Law of Addition in drafting (refer to the “Drafting Principles” module) show that the evenness of fibre assemblies can’t be fixed, only ameliorated during processing. If an uneven sliver is produced in the card this will carry through to the yarn stage.
Uneven rovings will produce uneven yarns which will exhibit strength variation due to the presence of thin places in the fibre assembly. Uneven yarns may also be produced by the spinning machinery.
The change in the number of fibres in the cross-section (thin place) can also lead to lower production efficiency in spinning and winding/clearing. A certain number of fibres is required to support the forces applied in these processes. This occurrence is referred to as an “ends-down”.
Similarly the production efficiency in fabric manufacture can be affected due to yarns breaking during weft insertion or during the formation of knitted loops.
Another very significant effect, especially for periodic variations in evenness is the formation of unwanted visual effects such as “barre” in weaving, where the periodic variation manifests as a diagonal pattern. Similar effects are also noted in weft knitted fabrics.

## Slide 4: Standards for Evenness
IWTO-18-67(E)
  Uster Evenness Tester
  Capacitance Principle
Xungai Wang & Peter Auer
Notes: <number>
<footer>
Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
The Uster Evenness Tester is the most popular and versatile machine available for evenness measurement. It is interesting to note that before this machine became available the need for evenness measurement was not thought critical by the textile industry. It is now considered essential.
The principle of capacitance mass measurement is employed. This means that changes in mass cause a change in charge as the fibre assembly is fed through charged ceramic plates. The instrument is sensitive to moisture, and so the testing should be conducted in a standard atmosphere.
The measuring apparatus is displayed in the picture. The white ceramic sensors are half-way down the apparatus. This particular picture shows yarns being measured.
The signal is amplified and analysed with proprietary software, and can be displayed on the monitor on the right, or printed out in hard copy.
This machine can measure everything from slivers to fine yarns. Different linear density is catered for by using different size sensors.

## Slide 5: Describing Evenness
Xungai Wang & Peter Auer
Single Value methods
  CV%
  U% (proprietary method)
  limiting irregularity CV(lim.)
  index of irregularity (I)
Other methods
  diagram
    charted deviations
  spectrogram
    frequency of deviations
Notes: <number>
<footer>
17
Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
There are various methods of measuring evenness, which can be classified into Single Value methods, and Other methods.
These will be discussed in the following slides.

## Slide 6: U% and CV%
Mass Diagram
CV% = s.d. x 100%
mean
U% = mean deviation x 100%
mean
Xungai Wang & Peter Auer
Notes: <number>
<footer>
18
Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
The diagram above represents a Mass Diagram that might appear on the monitor or be printed out. The central line is the mean linear density, with the variation from this mean plotted as the fibre assembly moves through the sensor.
From this Mass diagram, some Single Value measurements of evenness can be derived as shown by the formulas for CV% and U%.
While single values may be adequate in some applications, especially to satisfy customer specifications for process control, a deeper analysis of the signal may yield more information.

## Slide 7: Spectrogram
  typical read-out
  Chimney
  Hump
Xungai Wang & Peter Auer
Notes: <number>
<footer>
Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
One way of doing this is to change the linear density signal into a wavelength signal. This is called a Spectrogram. A typical Spectrogram is shown at the top of the slide.
The wavelength () of the periodic fluctuation in linear density can be read from the horizontal axis. The top Spectrogram shows a periodic fluctuation occurring every 3 metres for this particular assembly.
Each fibre assembly has a characteristic Spectrogram, influenced by things such as fibre types and machinery type. However, some stand-out features of the Spectrogram are indications that something is awry.
The stylised Spectrogram shown at the bottom of the slide, illustrates two unusual features that may show up.
Firstly a “chimney” which is a periodic fluctuation restricted to a specific wavelength may be related to machine parameters such as roller circumference. This may indicate a drafting breakdown such as an eccentric roller.
Secondly a “hump” shows that unusual fluctuations occurring over several close frequencies. This is more likely to be related to the presence of short fibres and poor fibre control in drafting, i.e. DRAFTING WAVES.
Relating the wavelength of unusual periodic fluctuations to the processing machinery configuration can be helpful in isolating machinery faults which could lead to appearance faults in the fabric.

## Slide 8: Limiting Irregularity
a completely random fibre array will be this even
this converts to
finer fibres are better
f
CV (lim.) = 3.58 d
tex
y
y
CV (lim.) = 100 ( 1 + 0.0004 CVd )
2
n
Xungai Wang & Peter Auer
Notes: <number>
<footer>
20
Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
Randomness is a desirable feature of any fibre assembly since a completely random array will achieve the maximum evenness.
The Martindale theory worked out the minimum possible irregularity of a yarn arising from a random array of its constituent fibres. This is shown in the first formula on this slide. This is referred to as the Limiting Irregularity of the fibre assembly, in this case for yarns (CVy).
This formula shows that the minimum irregularity (maximum evenness) is mainly a function of the number of fibres in the cross-section. There is a small effect of the fibre diameter variability (CVd).
This formula can be transposed using some assumptions about the fibres (constant fibre density (1.31g/cm3), and an approximation of 25% for CVd) to the second formula on this slide. This formula essentially says that for a given yarn linear density the maximum evenness will be determined by the diameter of the fibres.
This is very important because it means that if finer fibres are used to produce a yarn of a given tex, the yarn will be more even.
This means that fine fibres are more desirable as far as the evenness of product goes. Fine fibres make more even yarns. This theory can be applied to any fibre assembly, e.g. slivers and rovings.
Reference: Martindale, J.G. (1945), Journal of the Textile Institute, March, T35 - 47

## Slide 9: Index of Irregularity (I)
I
= CV (eff) (always > 1)
CV (lim.)
where CV (eff.) = measured (effective) irregularity
CV (lim.) = calculated limiting irregularity
how close is machinery to achieving the ideal randomness?
I gradually reduces through the sliver-roving-yarn processing
Xungai Wang & Peter Auer
Notes: <number>
<footer>
21
Written by: Assoc. Prof. Xungai Wang, Deakin University, and Dr. Peter Auer, The University of New South Wales.
The index of Irregularity is a dimensionless parameter which indicates the degree to which the mass variations of a fibre assembly deviate from the ideal fibre distribution. Remember that the ideal is a completely random distribution.
This parameter is used to assess just how closely machinery is achieving the desired randomness. The closer the I is to 1.0 the better. However, I is always greater than 1.0 since fibre arrays are never completely random in practice. For more information see “Fibre Assemblies” module.
Now, CV(lim) will decrease as the number of fibres being processed increases (see previous slide), but what happens to I?
During sliver-roving-yarn processing, the I value gradually decreases from sliver to yarn. This is because with further processing, the fibre assembly becomes more randomised in fibre ends distribution and more closely approaches an ideal fibre assembly. But the CV of a yarn is always greater than that of a sliver, because a yarn has much fewer fibres in its cross section than a sliver.