## Slide 1: Competing Fibres
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module examines the wool fibre against some competing fibres, and also looks at developments in fibre technology. “Shingosen” fibres from Japan are used as an example of a very recent development. See module Competing fibres”Shingosen”.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Fibre Classification
Natural
  wool
  cotton
  jute
  silk, cashmere (very small markets)
Regenerated, Cellulosic
  cellulose raw material
  rayons
    ~1900
Synthetic
  polyester
    1940
  polyamide
    “nylon”
    1939
  plyacrylonitrile
    “acrylic”
    1942
  polypropylene
    1960
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Fibres in significant commercial use today are classified as natural, regenerated cellulosic (also known as man-made), and synthetic fibres.
The natural fibres have been in use as apparel fibres for millenia. Rayon, the most popular regenerated cellulosic, was developed about 1900. Regenerated protein fibres have also been developed but these have proved to be unpopular over the years.
The most popular synthetic fibres are listed, along with the approximate dates of their development. The marketing of these fibres expanded in the 1960’s. The last major commercial development was polypropylene in about 1960, after the development of novel catalysis procedures.

## Slide 3: Comparison of Wool & other Apparel Fibres
Peter Auer
Source: Morton, W.E. & Hearle, J.W.S. (1962)
Property
Wool
Cotton
Polyester
Polyamide
(Nylon)
Poly-
acrylonitrile
(Acrylic)
Fibre Length (mm)
Fibre Length Variation
(CV%)
Fibre Density (g/cm)
(@ 65% R.H.)
Fibre Strength
(N/dtex)
Elongation at Break
(%)
Moisture Regain (%)
(@ room temp)
Diameter m
decitex
~13-30
~3 - 6
>27
50-60
1.31
1-1.5
30-40
13
N/A
~9
~1-3
20-35
to order
~40
(natural)
1.52
1.39
2 - 5
6 - 7
~40
7
1.5
down to 1
down to 1
~9
~10
(to order)
to order
to order
~10
~10
1.14
1.19
~5
(staple)
(staple)
~4
~3
~40
~25
4.5
1.5
N/A
~3
(worsted)
(short staple)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Morton, W.E. & Hearle, J.W.S. (1962) Physical Properties of Textile Fibres, Butterworth & Co. Ltd. and the Textile Institute.
The next two slides list some of the properties of fibres that have been compared. The tables are indicative only since the single values are based on variable populations.
Referring to these two slides, the questions may be asked:
How does the wool fibre compare to other fibres in terms of fibre properties?
How would the wool fibre compete with other fibres in terms of desirable properties in the apparel market? (fashion, performance, cost, versatility, environmental impact)

## Slide 4: Comparison of Wool & other Apparel Fibres
Peter Auer
Source: Morton, W.E. & Hearle, J.W.S. (1962)
Property
Wool
Cotton
Polyester
Polyamide
(Nylon)
Poly-
acrylonitrile
(Acrylic)
Elastic Recovery (%)
Features Surface
Heat Evolved (cal/g)
(40-70r.h.) (20°C)
Dyeing Behaviour
Setting Behaviour
Felting Behaviour
Initial Tensile Modulus (N/dtex)
~25
69
~50
52
~90
~10
~60
(from 5% extension 60%r.h.)
65
89
50
Longitudinal
X - section
scales
smooth
variable
smooth
smooth
crimped
convoluted
textured
textured
textured
ovoid
flat,tubular
variable
variable
dog-bone
38
20
1
10
1
easy
easy
easy
easy
difficult
Yes
Yes
Yes
Yes
Yes
No
No
No
No
marginal
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Morton, W.E. & Hearle, J.W.S. (1962) Physical Properties of Textile Fibres, Butterworth & Co. Ltd. and the Textile Institute

## Slide 5: Fibre Properties
Peter Auer
wool is:
  relatively coarse
  relatively weak but good elongation
  relatively pliable
  absorbs moisture well
  gives off heat when absorbing moisture
  finishes well (can be set)
  subject to shrinkage (can be rectified)
ALSO
  lustrous
  unique handle properties
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
In answer to these questions, it could be inferred from the information provided that wool has the listed comparative properties.
Less obvious, and not listed, are the outstanding lustre of the wool fibre, and also the unique handle (tactile) properties of articles made from the wool fibre.

## Slide 6: Desirable Properties
Peter Auer
fashion
  drape, handle, lustre (second to none)
performance
  ease of production, ease of processing, durability, strength
versatility
  linear density range, fibre characteristics, product development
environmental impact
  energy consumption, impact of production, use of raw materials, animal husbandry
relative cost?
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
It is the properties of drape, handle and lustre which make wool clothing such a fashion favourite. These properties are not obvious from the properties listed in the preceding tables, and more information can be found in the module, “Fibre Effects in Processing”.
The performance property of durability can be correlated to the fibre strength, perhaps as measured by abrasion resistance. Wool fibre suffers in comparison in this case. Other less obvious performance characteristics of the fibre relate to ease of production and processing, factors which have an impact on the marketing of the fibre.
The versatility of wool as a fibre can be related to the range of fibre linear densities available, the range of fibre characteristics, and the amount of fibre development that occurs. When comparing fibres it is usual to refer to the term linear density rather than diameter, because not all fibres are approximately round. Fibres which are manufactured products are more versatile in this respect.
As far as the environmental impact of the fibres is concerned, the energy consumption to make the fibre, the impact on the environment of fibre production (compare the footprint of synthetic fibre plants (including raw material manufacture), the conversion of waste products from the petroleum and coal industries into safe consumer products would also be a factor.
The cost of fibre, which is a raw material for the textile industry, might also affect the desirability of the fibre depending on the application. The relative costs are always changing due to climatic considerations, technological advances, demand and supply imbalances.

## Slide 7: Fibre Costs - 1995
Peter Auer
Source: World Textile Demand (Oct 1996)
* CRC for PQW Wool Marketing, Lecture 8, Ross Griffith (1996)
Fibre
Price
($US per kg)
Wool, greasy
$ 3.96
Wool, scoured
$ 5.80*
Wool, top
$ 8.40* (21µm)
Polyester, staple
$ 1.80
Polyester, filament
$ 2.10
Acrylic
$ 2.20
Rayon, staple
$ 2.60
Cotton
$ 1.70
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source: World Textile Demand (Oct 1996) Int. Cotton Advisory Committee ICAC & CRC for PQW Wool Marketing, Lecture 8, Ross Griffith (1996).
This is a “snapshot” of relative fibre prices in 1995. An oft-quoted figure is that a ratio of wool / synthetic and wool / cotton prices of 3 - 4 is sustainable due to the desirable properties of the wool fibre, and its relative scarcity.
However, this “price premium” is not guaranteed, and over time will blow out due to on-going technological advances in the cotton and synthetic fibre industries leading to lower cotton and synthetic fibre unit costs.

## Slide 8: Fibre Production
wool
cotton
synthetic
regenerated
Raw material
amino acids
carbohydrates
petroleum
by-products
Natural
cellulose
Polymer
production
biosynthesis
biosynthesis
Synthetic
polymerisation
N/A
(some
modification)
Production
unit
skin
follicle
plant
boll
factory
spinneret
factory
spinneret
Usable form
staple
staple
filament
staple
tow
filament
staple
tow
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
This table shows the production units for each fibre, from which can be inferred the scope for technological advances in fibre production. For synthetic fibres, the spinneret in the factory, is the production unit. Synthetic raw material manufactures, and plastic converters (fibre spinners) are always working to make the fibre come out of the spinneret faster, but with a higher quality.
The diversity of product is also highlighted in this table. Synthetic fibres can either be continuous filament, staple or tow. Natural fibres are always discontinuous staple fibres. However, synthetic fibres used in apparel applications is usually staple or tow (which are both converted forms of continuous filament).

## Slide 9: Nylon Fibre Manufacture
Peter Auer
Source: Von Bergen, W. (1963)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Von Bergen, Werner (1963), von Bergen’s Wool Handbook, Vol. I, 3rd Edition, John Wiley & Sons, pp512.
This slide is self-explanatory, and details the manufacture of the intermediate polymer in the production of the polyamide, Nylon 6.6, fibre.
Once manufactured the polymer is converted to continuous filament by a process called “fibre spinning”, not to be confused with the process of converting a combed sliver to a yarn, called “yarn spinning”.
The next two slides show the fibre spinning and staple / tow conversion routes for polyester and polyacrylonitrile.

## Slide 10: Polyester Fibre Manufacture
Peter Auer
Source: Von Bergen, W. (1963)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Von Bergen, Werner (1963), von Bergen’s Wool Handbook, Vol. I, 3rd Edition, John Wiley & Sons, pp516
This slide shows the raw material manufacture, and polymer conversion route for polyester polymer. Both continuous filament and staple fibre production are shown.

## Slide 11: Acrylic Fibre Manufacture
Peter Auer
Source: Von Bergen, W. (1963)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Von Bergen, Werner (1963), von Bergen’s Wool Handbook, Vol. I, 3rd Edition, John Wiley & Sons, pp517
This slide shows the manufacture of the acrylic polymer from raw materials, and its conversion to staple fibre. Notice the inclusion of crimping machinery in this process. This also features in the production of staple nylon and polyester staple.

## Slide 12: Synthetic Fibre Technology
DRY Spinning
MELT Spinning
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Shown in more detail in this slide are the spinning and drawing sections of synthetic fibre manufacture.
Some fibres are DRY spun (e.g. acrylic). This means that the polymer is dissolved in a suitable solvent so that the solution can be metered out of the spinneret. Once the liquid polymer leaves the spinneret it is stretched because it is being pulled away faster than it is delivered. It is also dried because the solvent evaporates in the chimney.
Other fibres are MELT spun (e.g. nylon, polyester, polypropylene). This means the polymer is heated until it melts and the molten polymer is pushed out of the spinneret where it solidifies. The undrawn fibre is then passed through a drawing section consisting of firstly slow back rollers, and then fast front rollers. This means that the fibre is stretched to impart the desired tensile properties.
The spinnerets are barriers at the end of the polymer streams which have many holes through which the dissolved or molten polymer can pass, forming a discrete undrawn fibre.

## Slide 13: Synthetic Fibre Development
Peter Auer
linear density
  microfibres
profiles
  CoolmaxTM
surface effects
  delustered
latent effects
  heat shrink acrylic
crimp
  bicomponent fibre
    TactelTM
  texturing
new chemistry
  PP
  1960
re-launch old chemistry
  TencelTM
length
  continuous filament
  tow cutting
  stretch breaking
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The implementation of new fibre technology a key strategy among competing fibre producers. The developments have been in the form of:
linear density modification (e.g. microfibres),
fibre X-sectional profiles (e.g. CoolmaxTM),
surface effects to change the surface lustre of fibres (e.g. addition of TiO2 to polymers, enzyme treatment of cotton),
the development of fibres with latent effects (e.g. heat-shrink acrylic fibre),
the development of fibres with a new chemical basis (e.g. the successful manufacture of polypropylene (PP) for fibre usage),
the re-launch of fibres with the same chemistry, but improved performance (e.g. TencelTM, which is rayon re-launched).
The importance of crimp for staple fibre processing and apparel fibre performance has long been recognised by synthetic fibre manufacturers. A recent development has been a bicomponent nylon fibre called Tactel ™, which crimps without being crimped.
The length variable has also long been available to synthetic fibre makers. The processes of tow cutting and stretch breaking can be controlled to give variable average fibre lengths. Each process also gives a characteristic fibre length distribution.
Some recent examples of synthetic fibre developments can be seen in the modules, “Competing Fibre on the Internet” and “Competing Fibres: Shingosen”.

## Slide 14: Cotton Fibre Technology
Peter Auer
metrology
  HVI
  every lot is tested
    linear density
    length
    strength
    trash
  main price determinants
  market confidence
crop types
  GM crops
  higher yields
ginning
  process control
    Intelligin ™
  trash content can be adjusted to suit market
processing developments
  U.S.
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Cotton fibre manufacturers have invested heavily in metrology, or fibre measurement. This reflects the variable nature of the fibres. Every lot traded is tested by High Volume Instrumentation (HVI) for the attributes listed. These are the main price determinants, and the market has confidence in the tests.
New crop types are always being developed, with higher yields being a research priority. Fibre diameter, and fibre length are also variables that can be controlled by crop type. The cotton industry has also been quick to adopt genetically modified crops to minimise pesticide usage.
At the processing end, the gins (which strip the fibre from the cotton seed after harvesting) have been subject to systems control (e.g. Intelligin ™), whereby the trash content of the output can be monitored and trash settings can be controlled.
Much of the developments in textile processing of cotton have been carried out in the U.S., which is also the major funding source for the cotton industry.

## Slide 15: Wool Fibre Technology
Wool
  finishing
    shrink-resist fibres
      machine washable
    insect-proof fibres
    flame-proof fibres
      safety
    enzyme treatment
      prickle
  blending
    new specs
      fibre diameter
      length
      crimp
OptimTM fine
  linear density
  profiles
  surface effects
OptimTM max
  latent effects
processing
  spinning
  easy care
  fibre blends
    wool/microfibre
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The wool industry has been able to develop new fibre technologies over the years based on the areas of finishing and blending. The development of shrink, insect and flame-resist fibres is well known. Perhaps less well known is the application of enzymatic finishing to improve the comfort factor of wool fabrics.
The development of new customer specifications for wool products containing wool with differing fibre properties has been a possibility since wool metrology has developed to a point where these properties can be specified in the market-place. The recent involvement of groups selling wool fibre on this basis is illustrated by the SRSTM and Egelabra groups.
However, until recently the wool industry hasn’t been able to modify wool at the fibre level. It is now possible, using technology developed in collaboration between CSIRO Textile & Fibre Technology (CSIRO TFT) and The WoolMark Company (WMC). See the module “Modified Wool Fibre Technology (Optim fibre)” for further details.
A further benefit of the technology is that it can be used to also produce a fibre that has the potential to provide light, warm garments by inducing latent effects in the modified fibre.