## Slide 1: Fibre Assemblies: Slivers, Rovings, Yarns
Produced for the CRC for Premium Quality Wool undergraduate program by;
Assoc. Prof. Xungai Wang, Deakin University, and
Dr. Peter Auer, The University of New South Wales.
Notes: This module defines fibre assemblies and examines which fibre distribution is the most desirable in any fibre assembly of staple fibres.
Produced for the CRC for Premium Quality Wool undergraduate program by Assoc. Prof. Xungai Wang, Deakin University and Dr. Peter Auer, The University of New South Wales.

## Slide 2: Definition
Fibre Assembly
  sliver (top)
  roving
  yarn
Important Fibre Features
  Fibre Leading Ends (FLE)
  Fibre Trailing Ends (FTE)
  Length variation
    affects drafting
  Diameter
    affects number of fibres in cross-section
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University and Dr. Peter Auer, The University of New South Wales.
Fibre assembly is a general term used to describe many of the products of various textile processes, ie slivers, rovings and yarns.
In general, a fibre assembly of staple fibres consists of discrete fibres aligned in the direction of the assembly axis. Each fibre in the assembly has a fibre leading end (FLE) and a fibre trailing end (FTE).
Other important fibre features are the length variation of the fibres, which can affect drafting performance and evenness of the drafted fibre assembly, and the fibre diameter which influences the number of fibres in the cross-section of any comparable fibre assembly. The number of fibres in the cross section of a fibre assembly has the greatest effect on the evenness of the assembly.
For more information on these effects see the modules, “Drafting Principles” and “Evenness”.

## Slide 3: Perfect sliver
FTE always joins FLE
  perfect fibres
    same diameter & length
  always the same number of fibres in cross section
  IMPOSSIBLE to achieve
  USELESS in practice
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University and Dr. Peter Auer, The University of New South Wales.
The concept of the Perfect sliver needs to be expxlored. In this fibre assembly, a FLE always meets a FTE. The fibres are also perfect fibres, each having the same diameter and length. As a consequence of this arrangement and these fibre properties there are always the same number of fibres in the cross-section.
This situation is impossible to achieve, since fibres can’t be arranged end to end, and fibre properties vary in reality. More importantly, it is not even desirable to achieve this arrangement; the fibre assembly has no coherence. If this assembly was drafted it would fall apart.
Although this concept is useful to picture what a perfect fibre assembly looks like, it is useless in practice.

## Slide 4: Ideal Sliver
RANDOM FLE
  NOT always the same number of fibres in cross section
  distribution of FLE
    laws of probability
    random distribution
  IMPOSSIBLE to achieve with current technology
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University and Dr. Peter Auer, The University of New South Wales.
The fibre assembly being striven for is characterised by a RANDOM arrangement of fibres (FLE or FTE are randomised throughout the assembly).
Fibres overlap and give the structure coherence, and there is not always the same number of fibres in the cross-section.
In fact the distribution of FLE’s is characterised by a normal distribution according to the laws of probability. This means that 50% of the time there are less fibres than average in the cross section, and more fibres than average in the cross-section for the other 50% of the time.
Whilst this is the ideal sliver, it is not achievable with any current drafting technology.

## Slide 5: Real sliver
random FLE (sometimes)
non-random groups of FLE
  DRAFTING WAVES
real fibres
  uneven diameter
  uneven length
Xungai Wang & Peter Auer
Notes: Written by: Assoc. Prof. Xungai Wang, Deakin University and Dr. Peter Auer, The University of New South Wales.
A realistic fibre assembly is illustrated above.
Mechanical factors such as imperfect drafting systems, and faulty machinery lead to the fibre distribution being random sometimes, but often the distribution is non-random along the assembly length. These non-random groups of fibres are referred to as drafting waves.
The presence of too many short fibres in a fibre assembly often leads to drafting waves when the assembly is drafted, since the short fibres are difficult to control during drafting.
This type of arrangement has implications for drafting and the evenness of textile products. For more information see the modules, “Drafting Principles” and “Evenness”.