## Slide 1: Combing: Latest Developments & Future Trends
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Notes: This module will inform you of the developments in combing that have taken place over the last 15 years or so.
In the context of Wool Science this discussion is limited to the developments in worsted combing. The module will also give an insight into the expected future trends in combing.
Users are urged to review the modules on ‘Gilling’ and ‘Combing Principles’ before using this module.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.

## Slide 2: Trends in Comb Speed
Year Comb Speed
(cycles/min)
NSC SAN Leisnig
1996 240 280 250
1981 210 210 230 (1992)
1974 185
1971 165
1967 160
1956 125
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
The first rectilinear comb was patented by Heilmann around 1843, but development began at least 12 years earlier. It was originally designed for combing cotton.
A long staple version was operating by about 1850 at a speed of about 80 cycles/min and a production rate of 2 -3 kg/hour, which compares with 10 - 12 kg/h for the Noble comb (which the rectilinear comb has since superseded).
The above table shows the progressive increase in comb speed since that time. At ITMA 95 (International Textile Machinery Association exhibition held in 1995) NSC released the PB32, which operates at a speed of 240 cycles/min and a production rate of about 40 kg/h for 21 µm.
The speeds of two other makes of comb are also shown. The SAN comb operated at a lower speed (210 cycles/min) but the latest model, the P2000, released at ITMA 95, operates at 280 cycles/min. Leisnig had been operating at 230 cycles/min for some years, but their new comb operates at 250 c/min.
These increments in speed are good news for the combing industry because production rates of the comb are very low compared with gills and cards. The combing process is a bit of a “bottleneck”. This means that relatively more combs are needed to service the other parts of the process, such as scours, cards etc.

## Slide 3: Future Trends: Speed
Physical process a barrier
  Combing the original open-end process
Sources of incremental advances
  exotic materials
  altered working cycles
Economic Restraints
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
This slide discusses the future trends in comb speed.
Combing is an “open end” process, which imposes significant constraints on the design and operation of the machine. It was of course the original “open-end” process, i.e. the sliver of fibres is “broken” during the process to allow combing.
The most likely increases in speed will come from wider use of exotic materials, basically a lightening of the construction.
Altered working cycles, e.g. new cam profiles and altered timings, will also play a part. The latter option may involve compromising the functioning of the machine.
Both options will involve increased cost. Therefore economics will constrain and control the nature and type of these developments.

## Slide 4: VM Removal
Ken Atkinson
VM Particle
Size (mm)
Removal
Efficiency (%)
0 to 3
3 to 10
10 to 20
96
98
98
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
One of the main reasons for combing is to remove VM (the others are to remove short fibre and nep).
The table shows measured efficiencies for removing VM according to particle size. There is some uncertainty in these figures mainly because of the errors associated with counting VM particles, which is a difficult and somewhat subjective task. Nevertheless, over many trials the efficiencies have been consistently measured at these levels.
The physical principle underlying VM removal, and indeed the removal of short fibre, is that any material that is not held by the nipper jaws will be removed by the circular comb.
The circular comb removes VM particles from a beard of fibre some 30 mm long. By this process, the contamination is removed from the leading ends of the fibre. VM contamination in the trailing ends is prevented from transferring into the output sliver by a secondary comb (the top or front comb) that is inserted from above. The contamination that is prevented from transferring to the output is removed by the circular comb on the next cycle.
The efficiency of the process is very dependent on the length of the particles and any material with a length less than about 30 mm is almost certain to be removed from the sliver.
Nevertheless about 4% of particles <3mm will get through the combing.

## Slide 5: Future Trends: VM Removal
Machine Efficiency already high at more than 96%
Reduced scope for improvement
Possibilities
Finer & longer pinning on Front Comb
Further increase in the pinned arc of the circular comb
Improved nipper brush design and operation
On-line monitoring
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
The already high efficiencies of combs mitigates against further large increases in efficiency.
Nevertheless, incremental change will occur over the foreseeable future. Most of this development will be in pin design and systems to maintain comb efficiencies at high levels.
Other developments that may help are to further increase the pinned arc of the circular comb, although this may be difficult because currently it is already relatively large at about 210 º. Improved nipper brush design may also eventuate.
Development of an intelligent comb may also be a possibility. This means that some kind of sensor attached to the comb could monitor VM contamination in the combed sliver. The benefit is that by monitoring the combs it may be possible to maintain plant efficiency at maximum levels.
As an example, if the efficiency of one comb in a bank of 30 dropped to 84%, the number of particles in the top from the group would increase from 20 particles /kg to 30 particles/kg, decreasing the top grade from AA to A.
More worrying perhaps, a similar decrease in quality is equivalent to 5 combs in 40 running at 95% efficiency or 10 combs running at 97% efficiency.

## Slide 6: Future Trends: Noil
Extremely desirable to reduce noil.
0.5% noil reduction
Savings of $12.5k / comb / year
Possible? How?
Reducing the entanglement in the scoured wool
  Reduce fibre breakage during carding and gilling
  Improve fibre alignment in the prepared sliver
Research required
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Noil is effectively lost top production. The price of noil is typically about $2 - 3 per kg compared with about $8 - 10 per kg for top (approximate prices for Jan 99). NB: These figures are very variable depending on the price of the greasy wool and the relative strengths of the worsted and woollen industries.
A 0.5% reduction in noil can increase returns to topmakers of the order of $12,500 /comb/year. This calculation was made by assuming that each comb operated all week (168 hours) for about 48 weeks per year with the above prices for top and noil.
Whether noil can be reduced is a moot point and will obviously require further research. Noil can only be reduced by reducing fibre breakage, either during carding or combing, which in turn is influenced by the degree of entanglement in scouring and carding performance.
Further research is required into the interactions between these processes before a definitive answer can be given in the case of the reduction in noil.

## Slide 7: Materials Handling
Input Output
Bobbins Cans
Cans Rail-Road
Laps
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Materials handling is a very important part of the textile industry. The processes that can be used for materials handling depend very much upon the physical properties of the material being handled and the process involved.
Combing is a discontinuous process producing a low tenacity sliver at low speed. Compare this to gilling which is a continuous process producing a relatively higher tenacity sliver at high speed.
This means that the feed to the comb can be in a greater variety of forms than the output from the comb. In particular, feeds to combs can be from bobbins, cans, or laps. In contrast, the output from a comb is generally collected in a can or, in a few cases, fed directly to the subsequent finisher gill.
The physical origin for this sliver tenacity difference is discussed later, but the next few slides shows some of the forms that the materials handling systems can take.
One form of materials handling in limited usage is called rail-roading, where all slivers from a number of machines are run together into the next machine. This certainly may reduce labour and associated costs, however, since there is no reversal of sliver taking place, the leading hooks are not removed, by straightening or reversal. It is probably for this reason that this form of sliver transference has not been universally accepted in worsted processing.

## Slide 8: SAN P90 Comb: Bobbin-Feed
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
The slide shows a SAN P90 comb arranged to take large bobbins as the feed.
The comb is generally designed to take 24 bobbins, the normal size of which is 20 kg. The SAN comb in this photo, however, has been fitted with a creel that takes 50 kg bobbins. In this configuration there is 1200 kg loaded onto the back of the comb, which could enable the comb to operate for up to about 34 hours with a fine wool before having to be reloaded. This arrangement can clearly reduce the labour required to process the fibre through the mill. The downside, of course, is that the capital cost of the larger capacity creel is higher.
An important aspect of combing is that it offers an excellent opportunity for further blending of the wool, significantly improving quality. The procedures of the mill must be organised to ensure that the wool is loaded randomly onto the backs of the combs for high levels of blending to be achieved.
Notice that the output of the comb is being collected in a can.

## Slide 9: NSC PB32: Can Feed
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
This slide shows an arrangement for an NSC PB32 comb on which the feed comes from cans.
Each can contains two slivers and since there are 12 cans, the number of input slivers is 24, the same as for the previous comb.
The creel shown is referred to as a Table Top; the previous type is a Central Frame. The main difference between them is that Table Tops come in a larger sizes and is therefore capable of taking larger cans. In particular, the maximum can diameters for Table Tops are 800 mm, which compares with 700 mm for the Central Frame.
If only single ends are to be used in the cans, the diameter is only 400 mm but in this case four rows of cans need to be used and the total number of cans is 24.

## Slide 10: Osaka Kiko: Lap Feed
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Lap feeding is a unique characteristic of the Japanese wool combing industry. The claims made for this method of feeding is that it reduces the noil and increases the mean fibre length (Hauteur) of the top.
The belief underlying these claims is that the density of the fibres in the lap is more uniform than for sliver feeds, and that the fibres are held more positively and are more aligned in the direction of the feed. There is the implication that there is less fibre breakage when combing laps than for combing sliver.
Laps are formed by using a special gill for the final preparation for combing. An advantage of the lap feeding system is that automatic feeding systems are relatively easy to implement because only one unit needs to be fitted to a comb compared with many units in the case of bobbins or cans.
This method of feeding has not caught on in worsted processing in Europe or Australia.
There is a lack of data in English language textile journals dealing with lap feeding, and therefore it is difficult to comment on the validity of the claims regarding the advantages of lap feeding. However, given the high compression of slivers during feed into a comb, the advantages may not be significant.

## Slide 11: SAN: LINEA (Gilling Development)
rail-road
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Although this development is not strictly combing, it is an important part of the processing line, and it shows a direction that combers may adopt in the future.
The LINEA consists of 3 stages of gilling, with the sliver collecting in cans after the 1st and 2nd stages of gilling. The sliver is delivered from the machine as either a ball or a bump.
The figure shows two views of the input to the LINEA. At this stage of development the idea was to feed the card sliver directly into the the first gilling via rail-roading. Clearly with this method there is a loss of reversal from the card to the gill. A later version of the LINEA employed can feed into the first stage.
The LINEA is not yet in commercial operation, not because of the performance of the machine, but more the high capital cost (approx. $1M). Combers would like such a machine but at much lower cost. This is a “chicken and egg” situation as clearly the cost is related to the number of units sold.
SAN have taken up this development to explore issues surrounding automation and it is a good example of the innovation displayed by this company. Some of the developments that went into the gill boxes have now been incorporated into their latest gill box, the SN21.

## Slide 12: New S&U Feed Comb
Ken Atkinson
Notes: <number>
<footer>
Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
Staedtler & Uhl (S&U) displayed at ITMA 95, a continuous feed comb as shown in the diagram. It operates on the “chain gill” principle in which the bars are driven continuously around a path.
The orientation of the pins (bar) is controlled by an arm at the end of each bar (see diagram) that moves in its own track.
The possible benefits of this development are:
  reduced noil, through reduced felting of the fibre in the feed section of the comb. The conventional feed comb operates on a reciprocal process in which it is inserted and withdrawn from the fibre feed once per cycle;
  higher operating speed, because of the smoother operation (high gilling speeds of 400 m/min are attributable to the development of chain gills);
  lower noil, because the pins remain in the fibre during detaching.
One possible disadvantage of the method is that the pins are pulled out of the wool further back than for the normal feed comb. This could mean some loss of control of the fibre during detaching, which could cause problems for the operation of the comb.
The unit has undergone trials with all of the major comb manufacturers. The major mills have decided that at the present moment they are not going to use the continuous feed comb to replace the feed gill now being used. Questions have arisen about the mechanical robustness of the device.

## Slide 13: SAN P100
Appeared at ITMA99
Speed to 260 cycles / min
Ken Atkinson
Notes: Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
SAN released their new comb the P100, which is radically different to previous SAN combs and possibly to any other comb currently on the market. In terms of production performance, the P100 operates at 260 cycles/min, which is well above the speed of the P90. A detailed view of the comb is shown in the slide.
SAN have also engineered the comb to provide for rapid removal and replacement of the circular brush, which can now be replaced in 5 to7 seconds.
The front comb moves up and down only, the forwards and backwards motions have been eliminated. Note also that the incremental motion of the feed rollers has been replaced by continuous rotation, although the feed gill retains its classic intermittent action. It is these changes that enable the simpler changing of the ratch, the details of which are shown in the next figure.

## Slide 14: SAN P100
Close-up of new Noil setting technology on the P100
Ken Atkinson
Notes: Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
The ratch can be changed by the ‘turn of a knob’ instead of the more usual series of interdependent setting changes. This should significantly improve the convenience in mill operations as well as ensuring that the ratch is indeed set at the chosen value.
In reconfiguring the comb, SAN have maintained, however, the relative motion between detaching rollers and nipper jaws at 90 mm. This reduces apron motion, extending the lifetime of the apron although potentially increasing vibration at higher speeds. Vibrations have been minimised by other design changes such as locating the epicyclic gear box, which provides the oscillating motion of the apron, low down on the frame of the comb.
The top brush is in its own mounting, which makes replacement relatively easy. Oiling points are collected together at the rear of the machine giving ready access to operators.
This comb has rewritten the combing design handbook and it will be fascinating to see how the machine performs industrially as it is taken up by the combing industry.

## Slide 15: NSC PB33
Appeared at ITMA99
Ken Atkinson
Notes: Written by: Dr. Ken Atkinson, CSIRO Textile & Fibre Technology.
NSC has denoted their new comb the PB33, which continues the development of the ground breaking PB32. There are some major new features of this comb that should appeal to users of worsted combs:
    the maximum speed of operation has been increased to 260 cycles/min;
    the circular brush can be removed and replaced without major disassembly of the comb, an operation that now takes only 10 to 20 seconds;
    the nipper brush is continuously adjusted during running to maintain optimum pressure on the beard during the circular combing phase; and,
    visual readout devices have been fitted that provide instant feedback on all settings on the comb and on status of safety switches etc.
The PB33 ran quietly at its maximum speed and with very little evidence of vibration. A further strength is the overall refinement of the machine that will ensure efficient operation in demanding mill environments.