## Slide 1: Microscopy in Wool Biology
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr Janelle Hocking Edwards, The University of Western Australia.
Notes: To actually ascertain whether factors are affecting wool production and quality it is essential that something can be measured to determine the degree of change. Likewise to study the structure of the wool fibre, the skin and its follicles it is important that we can see these microscopic features. This module describes the microscopes that are routinely used to examine wool growth and quality and the wool follicle. Images from the light microscope, transmission and electron scanning microscopes are supplied.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr Janelle Hocking Edwards, The University of Western Australia.

## Slide 2: Microscopes
Light Electron
  Transmission (TEM) Scanning (SEM)
Condenser lens
Objective lens
Specimen
Eyepiece lens
View of image
Projector
lens
Projector
lens
Beam
deflector
Detector
Specimen
Janelle Hocking Edwards
Notes: Written by: Dr Janelle Hocking Edwards, The University of Western Australia.
Adapted from Curtis, H. (1983) Biology. Fourth Edition. Worth Publishers, New York.
These diagrams depict the three main types of microscopes used in wool biology. The light microscope (LM) is shown upside down to emphasise its similarities to the two electron microscopes - the transmission electron microscope (TEM) and the scanning electron microscope (SEM).
  LM - resolving power of 0.2µm (200nm) = can not distinguish smaller than this. The limiting factor is the wavelength of light.
  TEM- resolving power of 0.5nm (200 000greater than eyes) = 5x Hydrogen atom diameter. This is achieved by using shorter wavelengths of electrons.
  SEM - resolving power of 10nm. An electron beam is focussed into a fine probe which is rapidly passed back and forward across the specimen. The specimen emits electrons as well as those from the illuminating beam. These interact to form a pattern of dark holes and light ridges. This provides a 3D image which is viewed on a TV screen.
Cells are fragile so they need to be “fixed”. This binds the cell structures in place usually via covalent bonds. As it is also necessary to make the tissue thin, a support such as wax, plastic resin or freezing is used.
In order to see anything under a microscope, different parts of the cell have to differ in their transparency to illumination. Cells are mainly water therefore they are transparent to light and small electrons do not emit as well as larger electrons such as heavy metals. Therefore tissues to be examined with LM are treated with dyes, and tissues to be examined with EM are pre-treated with heavy metals.
SEM may have organic matter removed with solvents leaving a metal replica which is reinforced with a carbon film.
EM needs water dehydrated from the samples as a vacuum is needed because the electron beam will scatter with anything with which it interacts.

## Slide 3: Human hair follicles
Light microscope
Scanning electron
microscope (SEM)
Janelle Hocking Edwards
Source: Holbrook & Minami (1991)
Notes: Written by: Dr Janelle Hocking Edwards, The University of Western Australia.
Source: Holbrook & Minami (1991) Ann. N.Y. Acad. Sci. 642;167
These are photomicrographs showing human hair follicles viewed using light microscope (inset) and the 3-D image generated with the scanning electron microscope.

## Slide 4: SEM and TEM of exclamation mark hair
500x
10 000 x
Janelle Hocking Edwards
Source: Tobin et al. (1991)
Notes: Written by: Dr Janelle Hocking Edwards, The University of Western Australia.
Source: Tobin et al. (1991) Ann. N.Y. Acad. Sci. 642;483
These are photomicrographs showing the 3D image of a hair fibre using SEM and the highly magnified, cross-sectional view of the fibre with TEM. Note that individual cells can be seen with the TEM and it is usual to examine the ultrastructure of individual cells with TEM.