## Slide 1: Detailed Fibre Cuticle Structure
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Les Jones, CSIRO Textile & Fibre Technology.
Notes: <number>
<footer>
Fibre cuticle cells are composed of a series of layers (laminations) varying in thickness and staining characteristics. This module describes the structure of the cuticle using transmission electron microscope (TEM) images to illustrate the cuticle structure and diagrams showing the location of each of the intercellular components of the fibre cuticle cell.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Les Jones, CSIRO Textile & Fibre Technology.

## Slide 2: Fibre cuticle cell
Fibre cuticle surface membrane
(epicuticle); contains lipids & proteins
a
exocuticle
endocuticle
cell membrane complex (CMC)



Cortex
c.r.
100nm
i
Les Jones
Notes: <number>
<footer>
Written by: Dr. Les Jones, CSIRO Textile & Fibre Technology.
The laminations or layers of the fibre cuticle cell are shown diagrammatically, and their main features summarised in this module.
Order of layers:
  Fibre cuticle surface membrane
  exocuticle (with an a-layer)
  endocuticle
    with cell remnants (c.r.)
    intracellular band (I-layer)
  Cell membrane complex
     -layer between two -layers

## Slide 3: Fibre cuticle cell surface
Fibre cuticle
surface membrane
a-layer
exocuticle
Les Jones
Notes: <number>
<footer>
Written by: Dr. Les Jones, CSIRO Textile & Fibre Technology.
The outermost layer of the fibre is the fibre cuticle surface membrane (FCUSM). It is seen as a non-staining thin band (6nm) on outer surface of mature fibres in this transmission scanning electron micrograph. It lies adjacent to the densely stained a-layer which is part of the exocuticle.

## Slide 4: Fibre cuticle surface membrane (FCUSM)
O
S
O
S
O
S
O
S
O
S
O
S
O
S
O
S
O
S
O
S
interior of cuticle cell
fatty acid
cross-linked
protein matrix
a-layer
Les Jones
composed of lipids and protein matrix
  major fatty acid - 18-methyl eicosanoic acid (C21a)
  protein associated with C21a contains citrulline
    iso-peptide bonds contributes to high stability of membrane
Notes: <number>
<footer>
Written by: Dr. Les Jones, CSIRO Textile & Fibre Technology.
The externally exposed cuticle surface membrane (FCUSM) performs the initial vital barrier functions of the mammalian fibre surface.
The model of this surface layer contains lipids (fatty acids) as a monolayer to form a hydrophobic surface. The polar (head group) end of the fatty acid form a presumed thioester bond with thiol groups (cysteine) in the underlying protein matrix. The lipid layer is approximately 3.0 nm thick and the protein matrix is similarly about 3.0 nm thick.
The major constituent fatty acid on the surface of the FCU is uncommon in nature, and has been identified as 18-methyl eicosanoic acid (MEA). MEA is an anteiso 21Carbon fatty acid which is methyl branched at C18 and is derived from isoleucine. It is usually designated as C21a.
The protein associated with the C21a is also unusual in that it contains citrulline and is crosslinked with isopeptide bonds (e.g. -(j-glutamyl)lysyl) which contribute to the unusual stability of this thin membrane. The protein-layer is often called the epicuticle.

## Slide 5: Proteinaceous barriers
a-layer (30-40nm) forms outer band
  intensely stained laminations beneath the surface lipid/protein bands
  high content of cystine residues
  network of disulfide bonds to produce barrier
remaining exocuticle less well stained
Les Jones
Notes: Written by: Dr. Les Jones, CSIRO Textile & Fibre Technology.
Referring back to the electron micrograph in slide 3 it is possible to see further laminations comprising the exocuticle beneath the surface lipid/protein bands. This heavy staining is referred to the a-layer which stains intensely due to the high content of cystine residues. This network of disulfide bonds produces a proteinaceous barrier. The remainder of the exocuticle has fewer cystine residues, therefore is less intensely stained.

## Slide 6: Endocuticle
contains cellular remnants
low cross-linking
derived from cuticle cytoplasm organelles
Les Jones
Notes: Written by: Dr. Les Jones, CSIRO Textile & Fibre Technology.
The regions comprising the inner cuticle contain cellular remnants and its characteristic low uptake of heavy metal stain indicates a low cross-link density. The endocuticle appears to be derived from the developing FCU cytoplasm organelles. This region differs from exocuticle in being more susceptible to attack by proteolytic enzymes.

## Slide 7: Cell membrane complex (CMC)
between overlapping fibre cuticle cells
consists of 3 layers
  two  layers
    (5nm; non staining)
  one  layer
    (15nm; dark staining)
sometimes an intracellular layer (i) is considered part of the CMC
Les Jones
Notes: Written by: Dr. Les Jones, CSIRO Textile & Fibre Technology.
Between overlapping FCU cells an intercellular moderately dark staining band (15 nm thick) known as the  layer lies between two non-staining (5 nm thick) membranous bands referred to as  layers.
By definition the CMC consists of two layers and the layer but an intracellular (I-band) is sometimes considered as part of the CMC.