## Slide 1: General Fibre Structure
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Janelle Hocking Edwards, The University of Western Australia.
Notes: This module contains a schematic diagram and a photomicrograph of the general structure of the fibre. The outermost layer of the fibre is called the cuticle, which surrounds the major component of the fibre, the cortex. In broad fibres (>30 µm) a medulla is present in the centre of the fibre.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Janelle Hocking Edwards, The University of Western Australia.

## Slide 2: Fibre structure
Cuticle
Cortex
Medulla
Orthocortex
Paracortex
Janelle Hocking Edwards
Notes: <number>
<footer>
Written by: Dr. Janelle Hocking Edwards, The University of Western Australia.
The fibre consists of two and sometimes three components.
Cuticle is the outermost layer that surrounds the fibre.
Cortex is the major component of the fibre in Merino sheep. The cortex can be further divided into:
  paracortex that has a high sulfur content and tends to be present on the inner side of the crimp
  orthocortex has a lower sulfur content than the paracortex.
The medulla is present in fibres that have large diameters.

## Slide 3: Different fibre structures
Sheep
Echidna
Mouse
Janelle Hocking Edwards
Source: Bereiter-Hahn et al., (1986)
Notes: Written by: Dr. Janelle Hocking Edwards, The University of Western Australia.
Source: Bereiter-Hahn, J., Matoltsy, A.G. & Richards, K.S. (1986) Biology of the Integument Vol 2. Vertebrates. Springer-Verlag, Berlin.
Transmission electron microscope images show the similarities and differences in fibre structure between species.
  Mouse fibres have a multi-layered Cuticle (Cu), a cortex (C) that fills most of the fibre and a medulla (M).
  Merino wool has a thin cuticle, and the cortex is divided into the orthocortex (OC), mesocortex (MC) and the paracortex (PC).
  Echidna quills have a thin cuticle, thin cortex and the majority of the fibre is filled by the medulla.