## Slide 1: Cuticle Structure
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Janelle Hocking Edwards, The University of Western Australia.
Notes: This module describes the structure of the fibre cuticle and includes photographs of cuticle scale patterns and a diagram of cuticle cell structure. For more detailed descriptions of the cuticle see the modules “Detailed Cuticle Structure” and “Cuticle Formation”.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Janelle Hocking Edwards, The University of Western Australia.

## Slide 2: Fibre cuticle
Janelle Hocking Edwards
layers of overlapping, flattened cells
generally single-layered in wool
involved in scale patterns
Notes: <number>
<footer>
Written by: Dr. Janelle Hocking Edwards, The University of Western Australia.
In sheep, the cuticle consists of flattened cells, one cell thick but overlapping. Cuticle cells overlap longitudinally and circumferentially. This produces a scale pattern with the edges pointing towards the tip of the fibre.
Cuticle cells are approximately rectangular (20-40µm long x 20-30µm wide) and are non-pigmented.
The number of layers of cuticle cells differs between species:
  1 in kangaroo, platypus, seals and wool
  6-10 in humans
  14 in whiskers of possum
  35 in pig bristles
Useful reference: Chapman, R.E. (1986) In Bereiter-Hahn, J., Matoltsy, A.G. & Richards, K.S. Biology of the Integument Vol 2. Vertebrates. Springer-Verlag, Berlin. Ch 17.

## Slide 3: Cuticle scale patterns
Cape
hunting
dog
Kincajou
Red fox
Sloth
bear
Janelle Hocking Edwards
Source: Montagna, W. and Parakkal, P.F.,(1974)
Notes: Written by: Dr. Janelle Hocking Edwards, The University of Western Australia.
Source: Montagna, W. and Parakkal, P.F. (1974), The structure and function of skin. Academic Press, NY p181
The edges of the cuticle cells form a pattern depending on the relationship of one cell to another. In broad fibres, the edges are reasonably flat, thus the fibres can not be interlocked and woven into yarn as well as finer fibres that have higher cuticle edges. Scale pattern varies between species and along the fibre (e.g. in seasonal animals). Scale edges do not always correspond to the edge of the cells, and there may be 2 or more scale edges per cell in some species.
Scale patterns can be used for fibre identification (longwools have long, thin scales with little overlap; finewools have ridged serrated surface; cashmere fibres have no scales). These patterns influence fibre properties. For example, fibres with smooth cuticle are very translucent as the unbroken surface reflects the light. This is one of the characteristics that gives cashmere its shine.

## Slide 4: Cuticle cell structure
Exocuticle
Epicuticle
very high S layer
Endocuticle
S-rich layer
Cell membrane
complex
Cortex
Janelle Hocking Edwards
Notes: <number>
<footer>
Written by: Dr. Janelle Hocking Edwards, The University of Western Australia.
The fibre cuticle is composed of 4 main layers (as demonstrated above);
1. Epicuticle which consists of a thin membrane on the outer surface.
2. Exocuticle which is further divided into 2 regions:
  the outer part has an extremely high S content
  the remainder has a high sulphur content
3. Endocuticle is also divided into 2 regions:
  the majority of the endocuticle has a low sulphur content
  the innermost surface of the endocuticle has a S rich layer
4. Cell membrane complex
  between overlapping cuticle cells