## Slide 1: Detailed Structure of the Cortex
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Les Jones, CSIRO Textile & Fibre Technology,
Dr Barry Powell & Dr. C. Simon Bawden, The University of Adelaide.
Notes: <number>
<footer>
Cortical cells normally account for the bulk of the fibre and are responsible for most of its mechanical properties. Cortex ultrastructure differs markedly in appearance from the cuticle. Numerous microscopic studies, mainly using tranmission electron microscopy (TEM), on sections of mammalian hair follicles have provided an abundance of morphological data to explain the cellular composition and ultrastructural details of the processes involved in hair formation. This module contains a transmission electron micrograph of the structure of the cortex.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Les Jones, CSIRO Textile & Fibre Technology and Dr Barry Powell & Dr. C. Simon Bawden, The University of Adelaide.

## Slide 2: Diagram of an electron micrograph of a wool cortical cell in cross-section
Keratin IF proteins
Cysteine-rich proteins
Glycine/tyrosine-rich proteins
Intermediate
Filament
Matrix
Keratin associated proteins
Type I & Type II IF
Dr Barry Powell & Dr. C. Simon Bawden
Notes: Written by: Dr Barry Powell & Dr. C. Simon Bawden, The University of Adelaide.
This is a diagrammatic representation of a X-section through the fibre. The small yellow dots are the IF’s and the red surrounding layer is the matrix. The IF’s are composed of Type I and Type II IF’s and the matrix (otherwise known as the intermediate filament associated proteins - IFAP’s; or keratin associated proteins - KAP’s) consists of cysteine-rich proteins (high sulfur proteins) and glycine/tyrosine rich proteins. This provides an introduction to the next slide of an actual electron micrograph of the fibre.

## Slide 3: TEM of cortex ultrastructure
Intermediate
filaments
Matrix
Ortho-
cortex
Para
-cortex
Dr. Les Jones
Notes: Written by: Dr. Les Jones, CSIRO Textile & Fibre Technology .
In stained sections of mammalian fibres observed with the transmission electron microscope (TEM), cortical cells demonstrate a filament/matrix texture. In modern terminology the filaments are classified as hard keratin intermediate filaments and are abbreviated as IFs. In transverse sections IFs are typically 7.5nm circular structures and consist of an unstained outer ring, a stained annular region and an unstained central core. The matrix generally shows high stain uptake with no apparent ultrastructural texture.
  In cross sections of the orthocortex, the intermediate filaments (IF’s) are in a whorl like pattern as if coiled around each other.
  The IF’s are arranged in a hexagonal pattern as if straight and lying parallel to each other in the paracortex.
Other structural components observed in cortical cells (although not seen in the above micrograph) include the remnants of cell nuclear material, cell membranes and associated structures. These latter structures form the so-called cell membrane complex which, like the fibre cuticle consists of paired unstained thin membranous bands about 5 nm thick ( layers) surrounding a densely stained intercellular substance ( layer). An intracellular densely stained irregular band is often associated with this CMC. The CMC of the fibre cortex differs in many respects to the CMC found in the fibre cuticle.