## Slide 1: Wool Metrology & Technology in Context
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module places wool technology and wool metrology in an industry context.
This module is designed to introduce wool technology. The differing processes of worsted and woollen manufacture are outlined, and an overview is given of the different products of these processes.
An understanding of the context of wool metrology is then possible, with some knowledge of wool technology established.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Wool Technology Overview
Growing
Shearing
Lotting
Blending
Scouring
Carbonising
Carding
Gilling
Combing
Finishing
Drafting
Spinning
Folding
Weaving / Knitting
Dyeing / Finishing
Garment Manufacture
Retailing
Recycling
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
There are many technological processes involved in converting greasy wool to a product that retail customers can use. The processes are listed above.
The non-textile but important processes such as growing, shearing, lotting are listed. The technology of retailing is evolving constantly, with information technology becoming increasingly important in the ways that retailers respond to consumers needs. This has implications for Wool Marketing which are covered in other modules. Recycling of clothing and fibre waste is an important source of raw material in the woollen and non-woven industries.
The processes of fabric and garment manufacture are covered briefly in the module “Textile Processes and Products”.
It is important to understand the impact of these processes on fibre properties in the final products covered in the module “Fibre Effects on Final Products”.

## Slide 3: Worsted or Woollen?
Scouring
Carding
Gilling
Combing
Drawing
Scouring
Carbonising
Carding
Spinning
Spinning
Condensing
CLEANING PROCESS
INTERMEDIATE PROCESS
TOP
Slubbing
Twisting
Twisting
YARN
YARN MANUFACTURE
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The differentiation between the WORSTED and WOOLLEN process is shown above.
In essence less time is spent straightening and aligning the fibres in the woollen process, hence the absence of gilling and combing from this processing route. The lack of straightening and presence of many short fibres has implications for the sorts of products that each process produces.
Recycled raw material can be used in the woollen process. The virgin fibre that is used is generally shorter and more contaminated with VM, hence the carbonising process. The intermediate product called slubbing is displayed for comparison purposes only. Slubbing is not a traded product, unlike wool top which is sold commercially by top-makers.
The worsted and woollen processes are covered in more detail in other modules.

## Slide 4: WORSTED
Yarns - fine, smooth & strong
Fabrics - expensive, smooth & strong
Garments - suits, garments worn close to skin
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Wool of sufficient length and strength is processed in the worsted system. Worsted yarns are fine smooth and strong.
Typical end uses for these light and durable fabrics are suits and garments worn close to the skin.
These fine, luxurious garments command a high regard and hence a price premium in the market-place.

## Slide 5: WOOLLEN
Yarns - thicker and relatively weak
Fabrics - often harsher handling
Garments - outer garments, blankets
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Shorter and weaker wools are more likely to be processed in the woollen system.
The yarn produced by this system is thicker and relatively weak.
The fabrics produced are used in outer garments, blankets, upholstery and other products which suit this type of input material.

## Slide 6: Wool Metrology
sale lots (baled fleeces)
  greasy colour, style, length, strength
  SUBJECTIVE APPRAISAL
staples
  length, strength, style
  OBJECTIVE MEASUREMENT
fibres
  diameter, yield, VM content, curvature, scoured colour, processed length
  OBJECTIVE MEASUREMENT
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
With a brief understanding of wool technology, the properties of the wool fibre, whether in fibre, staple or fleece form can be investigated. Wool Metrology is the study of the measurement of wool and the forthcoming slides aim to place metrology in an industry context.
The trend in the measurement of any raw material is for objective measurement, i.e. against a calibration standard, using some form of instrumentation. However, some fleece measurements are still performed subjectively, i.e. using an experienced mind and eye. Generally subjective measurements are less reliable and repeatable. However, due to various factors some subjective measurements are still valued by some sections of the industry.
The fleeces baled for sale are sampled by processes called GRAB SAMPLING (taking whole staples) and CORE SAMPLING (taking fibre cores). For more information see the “Grab Sampling” and Core Sampling” modules.
Most of the grab sample ends up as a display sample, which can be accessed by buyers who may subjectively assess the wool for greasy colour, style, length and strength before auction.
The grab sample also provides whole staples (collections of fibres growing on the animal). This form of the raw wool is used to ESTIMATE fibre length and strength before processing. The same staples can be used to measure the style of the fleece objectively.
The fibres from core sampling are used to measure diameter, scoured colour and estimate the amount of usable fibre (yield, vegetable matter or VM). The average processed length (also called Hauteur) and the amount of short fibres in the processed wool or top (this is highly correlated to CVH, or the spread of the length measurements) is important to topmakers’ customers, the spinners. Processed fibre length is measured on the intermediate product called the TOP.
Current research work is examining the importance of curvature in both processing and final products. This property is measured on fibre obtained in core sampling.

## Slide 7: Context of Metrology
Marketing
  specifications for sale
  marketing advantage
Process Control
  QA (certainty)
  Efficiency ($$)
  Optimisation ($$)
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Having established an understanding of wool technology and also wool metrology, the context of metrology can be seen to be two-fold.
Wool Metrology is important in the trading of wool in terms of specifications for sale. Buyers can be sure of what they are buying. The trading of raw wool is regulated by the International Wool Trading Organisation (IWTO) which involves agreements between the various countries involved in wool trading in the world. A point of interest is that P.R. China remained apart from the IWTO until 1998.
Australia and New Zealand have the highest adoption rate of raw wool measurement which can be a significant raw wool marketing advantage. This is because the specifications of raw wool have been related to the performance of the wool in processing. Therefore if the raw wool measurements are known, it is possible to PREDICT the outcome of the topmaking process. The research behind this innovation was sponsored by the Australian woolgrower, in conjunction with topmaking mills worldwide. For more information refer to the modules dealing with PREDICTION.
Therefore there are obvious implications in process control for wool metrology. Topmakers can be more certain of their product, they can gain greater efficiencies in their processes, and they can also optimise their raw wool purchases to deliver the specified top to their customer the spinner at least cost.
An on-going concern in the marketing of raw wool is the completeness of the description of the product. It is essential that Wool Metrology continues to advance to the stage where these concerns are unnecessary in the market place. Competing fibres like cotton are sold with assured description based on grading and objective measurement.