## Slide 1: Optical Fibre Diameter Analyser: Measurement of Fibre Diameter
Produced for the CRC for Premium Quality Wool undergraduate program by;
Mark Brims, BSC Electronics Pty Ltd., and
Dr. Peter Auer, The University of New South Wales.
Notes: This modules examines the measurement of fibre diameter by the Optical Fibre Diameter Analyser (OFDA).
The components of the OFDA measurement system are explained and the measurement of fibre diameter discussed.
Produced for the CRC for Premium Quality Wool undergraduate program by Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.

## Slide 2: Introduction to OFDA
History
  introduced 1991
  used in 22 countries
Capabilities
  raw wool to fabric measurement
  cashmere, mohair, alpaca, synthetics
Measurement
  diameter
  medullation
  curvature
  ALONG fibre diameter
  fibre cleanliness
Mark Brims & Peter Auer
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
OFDA 100 was introduced in 1991 and is now in use across 22 countries.
It is used at all stages in the wool processing chain, from raw wool to fabric. It can also be used to measure other fibres, including cashmere, mohair, alpaca and some synthetic fibres.
OFDA also has several measurement options in addition to mean fibre diameter and fibre diameter distribution. An opacity measurement option is used to estimate medullation and flat fibres. A curvature measurement option measures snippet curvature in degrees per mm.
The most recent option measures fibre diameter along the fibre and fibre cleanliness.

## Slide 3: OFDA measurement system
Microscope & video
Spreader
Guillotine
Monochrome video monitor
Computer &
printer
Mark Brims & Peter Auer
Source: http://www.ofda.com/products.htm
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
The OFDA measurement system, shown in this slide, consists of a microscope with an electronically controlled stage and video image circuit board. Part of the apparatus is a guillotine to cut top into 2mm snippets.
A minicore machine (not shown above) is used to make fibre snippets from scoured greasy wool.
An automatic spreader is used to spread the snippets onto hinged glass slides. A monochrome video monitor displays the images of the fibres being measured. The system is computer controlled, and the output is stored electronically and/or printed out.
A graticule calibration slide is provided as a direct calibration reference. Calibration has been verified as linear from 5 to 100 microns. The diameter range is from 4 to 300 micron.
Calibration for measuring wool and mohair are carried out using standard wool samples from Interwoollabs.

## Slide 4: Standard
Mark Brims & Peter Auer
IWTO-47-95
  Measurement of the mean and distribution of fibre diameter of wool using an Optical Fibre Diameter Analyser (OFDA)
Accepted as full standard at IWTO in 1995
  certified and applied in wool trading contracts.
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
In June 1995 at the Harrogate meeting of IWTO Standardisation Committee, the OFDA Test Method 47 was accepted as a full test method after having undergone extensive international Round Trials.
These Round Trials were completed over a period of 3 years. In the final trial, 11 OFDAs were compared against Airflow, projection microscope and Laserscan on a group of 30 wool tops. On 40 greasy wool core samples, 4 OFDAs were compared against Airflow and Laserscan.
Following the adoption of this Test Method, fibre diameter and distribution results generated on OFDA may be certified and applied in wool trading contracts.

## Slide 5: Operating principles
Measurement points
are shown as lines crossing fibre
Mark Brims & Peter Auer
Source: http://www.ofda.com/Operating Principles.htm
cut sample into 2mm snippets
spread fibre snippets onto open glass slide
load slide onto OFDA microscope stage
follow computer software instructions
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
Source: http://www.ofda.com/Operating Principles.htm
OFDA is an image analysis measurement system where an automatic microscope is positioned above a moving sample of fibres. Magnified images of individual fibres are captured by a video camera and then identified and measured. The fibres and measurement points are seen on the video screen, as shown above. A complete measurement cycle on a clean, conditioned sample takes less than 2 minutes.
The width of each identified fibre image is measured with a resolution of 1 micron whilst the combined diameter and standard deviation are calculated to a resolution of 0.01 micron. After completing the measurement of the requested number of fibres, a histogram of fibre diameter distribution is produced.

## Slide 6: OFDA histogram
Mark Brims & Peter Auer
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.
The histogram data includes mean fibre diameter, standard deviation of diameter, coefficient of variation of fibre diameter, prickle factor and spinning fineness. If the opacity and curvature options are enabled, these will be measured and reported at the same time.

## Slide 7: Further Information
http://www.ofda.com
Mark Brims
Notes: Written by: Mark Brims, BSC Electronics Pty Ltd. and Dr. Peter Auer, The University of New South Wales.