## Slide 1: Using Multiple Regression Analysis in Processing Prediction
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
Notes: This module uses some specific results from sale lot processing to demonstrate the application of multiple linear regression analysis to the derivation of formulae whereby the processed fibre length (Actual Hauteur) is predicted from the raw wool properties of the sale lots.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.

## Slide 2: Using staple length only
110
Staple Length (mm)
R= 0.67
40
50
60
70
80
90
100
110
40
50
60
70
80
90
100
Actual Hauteur (mm)
Peter Auer & Lorraine Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
First, the range of staple length characteristics of the sale lots is plotted against the actual Hauteur (H). The X-axis could also be labelled Predicted Hauteur (mm).
A correlation coefficient (R) of 0.67 indicates that 45% (R2=0.45) of the variation in H is explained by the Predicted H. In this case mean staple length has been used as the predictor of H. A correlation coefficient of 1.0 is the maximum expected.
The unbroken line on these graphs represent the 1:1 line and the broken lines indicate the width of the spread of results.

## Slide 3: Using SL & Fibre Diameter
Predicted Hauteur (mm)
( SL & Fibre Diameter)
Actual Hauteur (mm)
R = 0.67
40
50
60
70
80
90
100
110
40
50
60
70
80
90
100
110
Peter Auer & Lorraine Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
This graph has included the range of fibre diameter results for the lots in the calculation of Predicted H.
Unlike the TEAM formula, which was based on many more lots over a wide range of properties, fibre diameter doesn’t have any significant effect on the prediction of Actual H, for these sale lots, based on the correlation coefficient. These sale lots covered only a limited range of fibre diameters.

## Slide 4: Using SL, FD and Staple Strength
Predicted Hauteur (mm)
( SL, Fibre Diameter, Staple Strength)
40
50
60
70
80
90
100
110
R = 0.80
40
50
60
70
80
90
100
110
Actual Hauteur (mm)
Peter Auer & Lorraine Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
This graph includes staple strength (SS) in the calculation of Predicted H.
The inclusion of a SS term in the formula to predict Actual H sees an improvement in prediction as judged by the correlation coefficient.

## Slide 5: Using SL, FD, SS and Mid Breaks
R= 0.85
40
50
60
70
80
90
100
110
40
50
60
70
80
90
100
110
Predicted Hauteur (mm)
( SL, Fibre Diameter, SS, Mid Breaks)
Actual Hauteur (mm)
Peter Auer & Lorraine Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
This graph includes Mid Breaks (M) in the formula used to predict Actual H.
Again, judging from the correlation coefficient, the inclusion of Mid Breaks in the formula improves the prediction.

## Slide 6: Using SL, FD, SS, M and VM
R = 0.86
40
50
60
70
80
90
100
110
40
50
60
70
80
90
100
Predicted Hauteur
( SL, Fibre Diameter, SS, Mid breaks, VM)
Actual Hauteur (mm)
110
Peter Auer & Lorraine Osborne
Notes: Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
Finally, the inclusion of a term for Vegetable Matter (VM) in the formula used to predict Actual H sees a further slight improvement in prediction.
The prediction formulae calculated haven’t been included in this module to avoid confusion with the formulae derived from the TEAM trials.
However, the final formulae resemble the TEAM equation, but would be different in terms of the coefficients represented by x, y, z, a, b & C in the following example:
H = x SL + y SS + z D - a M - b VM + C