## Slide 1: Latest Developments in Prediction
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Notes: This module examines developments in processing prediction after the adoption of the TEAM formula into the commercial environment.
The adoption of TEAM by industry is assessed.
The development of sale lot processing prediction formulae and the accuracy of the resulting predictions are discussed.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.

## Slide 2: TEAM Survey - 1996/1997
Trevor Mahar
Results
28 mills
14 exporters
75% use prediction
Level of satisfaction with TEAM
  Mills - 91%
  Exporters - 54%
Conclusions
TEAM:
  simple, robust formula
  provides benchmark
Future research & improvement
  by individual organisations
  should “add-on” to TEAM
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
By 1996 80% of combing wools had objective additional measurements pre-sale and the TEAM general formula was being used as the benchmark for the prediction of Hauteur.
Woolbrokers in Australia were making the predicted Hauteur available with their sale catalogues, and AWTA Ltd was automatically transmitting the calculated Hauteur electronically to all clients who had conducted both core and staple tests and was providing the Hauteur on certificates when requested.
But changes in technologies since 1988 stimulated a re-assessment of the relevance and use of TEAM by the wool industry.
A survey was conducted in which mills and exporters were asked a series of questions about TEAM. 28 mills and 14 exporters responded to this survey - a 40% response rate. 75% of the respondents used prediction and the level of satisfaction with TEAM was 91% for the mills and 54% for the exporters. They all agreed that there was a general acceptance of TEAM within the industry and were all aware of the mill factor part of the equation.
They also were aware of, and allowed for the differences in results given by TEAM for different wool types. This was an issue that had been raised at IWTO by WA woolgrowers, concerned about penalties for tenderness.
The overall conclusions from this survey were that TEAM was simple with a robust formula that provided a benchmark to industry. Recommendations were made that any future research & improvement to TEAM should be made by individual organisations, and that any improvements should be “add-ons” to TEAM, rather than the adoption of entirely different approaches.
Reference: Douglas, SAS and Couchman, R.C. (1997), ‘Industry Review of the TEAM Prediction Formula’, Growers, Traders & Early Processors C’tees, IWTO, Nice.

## Slide 3
Mob units
Consignment
Sale lots
Trevor Mahar
Notes: Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Sale lots are the initial trading unit of wool. Woolgrowers, brokers and wool buyers or exporters trade in sale lots. Wool characteristics for sale lots can be more extreme than for processing consignments. For example, sale lots can reflect the characteristics a particular environment has on one mob of sheep. A processing consignment, on the other hand, typically contains wool from many sale lots and therefore is characterised by the average of the environments of the many mobs of sheep represented in the consignment. The effect of the average will always be less extreme than that of its individual components.
With this in mind the TEAM management committee noted that, “Application of these (TEAM) formulae to sale lots could lead to unusual results …..”
The accurate prediction of the processing potential of sale lots might have a number of benefits:
Sale lot prediction would stimulate an “engineering” approach to the assembling of sale lots to meet the specifications of a processing consignment.
It would also:
* enable alterations to be made to the make-up of the consignment;
* improve the predictability of the resulting mill consignments;
* provide feedback to the grower from the marketplace; and,
* enable the growers to maintain equity in their product output.

## Slide 4
* Raw wool properties specific
to one lot
Mob units
Sale lots
*Common
genetic
husbandry
environmental
factors
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Sale lots are not routinely processed to top as individual units, although some growers have adopted this procedure recently as an alternative form of marketing their clip.
From a processing viewpoint individual sale lots differ from consignments since they typically consist of wool from a single mob of sheep. Wool from one mob may have combinations of characteristics specific to the genetic, environmental and husbandry factors which affect the mob during wool growth.
These factors are averaged in a processing consignment because of the blending together of different sale lots. Due to the averaging effect of blending, consignments do not have the extremes of raw wool properties exhibited by sale lots.
The following slide illustrates this point.

## Slide 5: Sale Lot Variability
Sale Lots Consignments
Processing: CSIRO Commercial mills
number 326 505
Staple Length:
mean (mm) 56 - 136 65 - 108
CV (%) 10 - 32 13 - 30
Staple Strength 13 - 63 26 - 56
(N/Ktex)
Mid - breaks (%) 3 - 95 14 - 88
Trevor Mahar
Source: Mahar, T.J. et al 1994
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Source: Mahar, T.J., Brown, G.H., Osborne, L.J. and Burke, A.J., (1994), Prediction of Processing Performance for Sale Lots and Consignments, In: seminar Proceedings ‘Specification of Australian Wool & Its Implications for Marketing and Processing’, Woolspec 94.
This table shows the variations in raw wool properties for 326 sale lots and 505 consignments from the ASMAP and second TEAM trials, respectively.
For each of the the raw wool properties, the sale lots have more extreme values. It would also be highly unusual for a consignment to be processed consisting of only one type of wool, eg. tender wool or belly wool. However, sale lots with these characteristics are processed as components of consignments and predictions of their processing performance are required.
Since some sale lots have raw wool measurements that lie outside those used in the TEAM database their processing performance may not be well predicted by the TEAM equation. Also, the TEAM equations were not developed to predict the processing performance of sale lots. The TEAM equations use only linear relationships between raw wool characteristics which may, in fact, be an over-simplification.

## Slide 6: Sale Lot Hauteur and CVH
H : 65mm
cvH : 36%
H: 55mm
cvH: 50%
H : 72mm
cvH : 46%
H : 58mm
cvH : 56%
Fleece
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Researchers at CSIRO Division of Wool Technology, using a mini-processing facility which is capable of processing small quantities of wool have been able to show the range and shape of fibre length distributions of individual sale lots within a consignment.
In one case samples from each of the 16 individual sale lot components of a commercial consignment of fleece wool were processed to top. The slide features distributions of Hauteur for 4 of these 16 sale lots. Note the different shapes of the distributions and the different average fibre lengths of the component lots.

## Slide 7: CSIRO 1 Formula
H* = 1.17L / (1 + P)
1 - P : PROBABILITY FIBRE will NOT BREAK
P = 0, H* = 1.17L ( no breaks)
P = 1, H* = 1.17L / 2 (all fibres break)
P = ey / (1 + ey)
where y = f(RAW WOOL PROPERTIES)
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
In order to be able to predict the processing performance of sale lots, a series of 166 sale lots were ‘mini-processed’ to top. The results from this processing formed a database for the development of sale lot prediction formulae. Two formulae were initially developed based on a modified regression approaches.
The modified regression method of prediction uses a 2-stage approach.
Firstly, an estimate is made of the probability of a fibre breaking during processing. This estimate is based on the same measured raw wool variables as used in TEAM (with the inclusion of the Coefficient of Staple Length, CVSL). The variable, ‘P’, with the interpretation that ‘1-P’ is the probability that a fibre will NOT break during processing, is calculated as follows:
P = ey / (1+ey) ……………………………………………….. (1)
where ‘y’ is determined from a regression equation based on raw wool variables.
Secondly, the predicted Hauteur is then determined based on an estimate of the unbroken fibre length of the lot, modified by the probability of fibres breaking during processing. The prediction of Hauteur is calculated as:
H* = 1.17 x L / (1+P)
where ‘L’ is the mean Staple Length of the lot and ‘P’ is obtained from equation (1). The factor 1.17 is the average Fibre Length to Staple Length ratio. This ratio indicates that the mean fibre length of greasy wool is approximately 17% longer than the mean staple length.
This method of prediction assumes that the removal of short fibre during processing has negligible effect on Hauteur and that fibres do not break more than once.

## Slide 8: SiroHauteur
Actual Distribution
Predicted Distribution
Trevor Mahar
predicts fibre length distribution
9 quantiles from almeter output
fits smooth curve to fibre length distribution
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
A second sale lot technique has the added advantage of predicting the distribution of fibre length in top as well as Hauteur.
When a top is measured on an Almeter, or similar instrument, a printout of the fibre length distribution can be obtained as well as Hauteur and other parameters of the distribution. A typical Almeter Hauteur distribution is shown in the top graph in this slide. The column of statistics in the top right hand corner of the actual distribution gives the length of fibres at nine percentage points of the distribution, ranging from 95% to 1%. These points as referred to as quantiles.
Fibre length distributions can be considered simply as a curve which may be expressed as an equation and may be predicted. A simple way of fitting a curve was found by regression of nine quantiles on functions of their associated probabilities within each lot. An example of this is shown in the lower graph on this slide.
The algorithms required to generate predictions using this method necessitate a computer program. This program has been produced commercially and is marketed as ‘SiroHauteur’.
SiroHauteur incorporates both the TEAM formula and what was then called “CSIRO2” prediction formulae. The program will predict the processing performance of individual sale lots and any combination of sale lots entered into the data set. This program therefore allows for more accurate “engineering” of blends for consignments.

## Slide 9: Effect of Staple Strength
Staple Strength (N/ktex)
Hauteur (mm)
20 34 43 47 63
55
59
63
67
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
This figure shows the empirical relationship between Staple Strength and top Hauteur when all other variables are held constant.
As expected, an increase in Staple Strength is associated with an increase in top Hauteur. However, there is a change in the relationship at approximately 45 - 50 N/ktex. At high values of Staple Strength (>43 N/ktex) an increase in Staple Strength is associated with a relatively small increase in top Hauteur.

## Slide 10: Effect of Staple Strength on Predicted Hauteur
20
40
60
TEAM
SiroHauteur
Predicted Hauteur (mm)
Staple Strength (N/ktex)
56
64
68
Trevor Mahar
Source: Mahar, T.J. et al 1994
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Source: Mahar, T.J., Brown, G.H., Osborne, L.J. and Burke, A.J., (1994), Prediction of Processing Performance for Sale Lots and Consignments, In: seminar Proceedings ‘Specification of Australian Wool & Its Implications for Marketing and Processing’, Woolspec 94.
The above graph shows the predicted effect of changes in Staple Strength on Hauteur using both the SiroHauteur formula and the linear TEAM prediction.
The lessening of the effect of Staple Strength at higher values as predicted by SiroHauteur agrees with controlled trials conducted by CSIRO on the effect of Staple Strength on Hauteur, as shown on the previous slide.

## Slide 11: CSIRO Sale Lot formula (2nd generation)
Trevor Mahar
SIROLAN TOPSPEC
  LOTSpec
  FLCSpec
LOTSpec
  Uses higher order terms (eg. SL2, SSxSL)
  non-linear relationships between predicted H and raw wool measurements
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
CSIRO Division of Wool Technology used its expanded database of raw wool measurements and processing outcomes for sale lots to update and improve their prediction formulae for sale lots.
A PC-based prediction program was developed called Sirolan-TOPSpec. This program consists of two separate prediction models, LOTSpec for predicting the processing performance of individual sale lots and their combinations, and FLCSpec which predicts the processing potential of individual fleeces.
The statistical detail behind the Sirolan-TOPSpec technologies is quite complex with new knowledge resulting in improved prediction. Non-linear relationships between predicted Hauteur and raw wool measurements are used.
Reference: Hansford, K.A., Humphries, W., Brown, G.H., Mahar, T.J. and Charlton, D., (1997) Sirolan-Topspec Part1: Topmaking Prediction for Sale Lots and Consignments, IWTO Boston, May 1997, Report No. 4.

## Slide 12: Prediction Accuracy (mm) [SD of (Actual - Predicted) Hauteur]
Sale lots predicted less accurately than consignments
CSIRO formulae slightly better than TEAM for sale lots
400 500
sale lots consignments
TEAM: 5.0 - 5.6 3.4
SiroHauteur: 4.5
LOTSpec: 4.5
Trevor Mahar
Notes: Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
The above table evaluates the results obtained for sale lots from the three prediction formulae now available commercially.
The figures quoted are the Standard Deviation of actual minus predicted Hauteur. A higher figure means that the distribution of actual minus predicted H was broader.
The table shows that the processing prediction of sale lots improved with the use of specifically developed sale lot formulae compared to TEAM (i.e., Standard Deviation of differences between Actual and Predicted Hauteur reduced from 5.4mm to 4.5mm).
The more individual nature of sale lots contributes to their less accurate prediction compared to consignments. The Standard Deviation of differences between Actual and Predicted Hauteur for consignments is 3.4mm compared to 4.5mm for sale lots.

## Slide 13: Effect of Wool Category
80
40
50
110
Staple Length (mm)
Predicted Hauteur (mm)
Fleece
Skirtings
Trevor Mahar
Source: Mahar, T.J. et al 1994
Notes: Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Source: Mahar, T.J., Brown, G.H., Osborne, L.J. and Burke, A.J., (1994), Prediction of Processing Performance for Sale Lots and Consignments, In: seminar Proceedings ‘Specification of Australian Wool & Its Implications for Marketing and Processing’, Woolspec 94.
Prior to the development of Sirolan-TOPSpec, research was conducted on how sale lot prediction might be improved. It was found that further improvements could be gained by considering wool category, style grade and breed.
Separate formulae were developed for fleece and skirting Merino wool sale lots. The graph on this slide shows how Hauteur predicted from these two relationships varies with Staple Length for lots. The raw wool properties of the lots were close to the average of the sale lot database ie. 21.5µm, 35 N/ktex, 18% SLCV and 62% mid breaks.
The Hauteur for fleece prediction is greater than that for the skirting prediction for all values of Staple Length. This relationship implies that for any value of Staple Length, with other raw wool properties remaining constant, fleece wool will process between 1mm to 4mm longer in Hauteur than skirtings wool.
Having separate prediction formulae for wool categories takes into consideration the different prediction relationships for these different wool categories.

## Slide 14: Improvement in Prediction
Standard Deviation (mm)
One Formula Individual Group
for all Formulae
Merino 4.1 4.1
Crossbred 5.4 4.5
Fleece 4.1 4.1
Skirtings 3.2 2.9
Best 4.5 4.2
Good 4.0 3.9
Trevor Mahar
Source: Mahar, T.J. et al 1994
Notes: Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Source: Mahar, T.J., Brown, G.H., Osborne, L.J. and Burke, A.J., (1994), Prediction of Processing Performance for Sale Lots and Consignments, In: seminar Proceedings ‘Specification of Australian Wool & Its Implications for Marketing and Processing’, Woolspec 94.
This table shows the improvements achieved when individual prediction formulae were developed for breed, wool category and style grade.
There was a definite improvement in prediction accuracy (lower Standard Deviation of differences between Predicted and Actual Hauteur) when individual formulae were applied compared to applying one formula for all wools.
In this analysis the groups which showed little or no measurable improvement, viz. ‘Merino’, ‘Fleece’ and ‘Good Topmaking’, were the most popular contributors to the overall database. These groups had more influence on the overall results, i.e. for the single formula prediction, than the other, less well represented groups in the database. However, there was a minimum of at least 20 lots in each of the groups.