## Slide 1: The Processing Performance of Raw Wool: Introduction to Prediction
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Notes: This module introduces the concept of processing prediction. The formulas developed from the Trials Evaluating Additional Measurement (TEAM) project are discussed and explained.
The recommendations arising from the TEAM project are also discussed.
It is recommended that an understanding of regression analysis is gained before using this module, see the module, “Using regression analysis in processing prediction”. The understanding of Hauteur and its measurement is also recommended, see the module, “The Measurement of Hauteur and CVH”.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.

## Slide 2: Fibre length in Top
Dependent on:
  Greasy wool Fibre length
  Amount of Fibre breakage
  Location of breakage along Fibre
    short fibre is combed out
Can be estimated (predicted) by raw wool properties
  Staple Length (SL)
  Staple Strength (SS)
  Position of break (POB)
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
The development of objective measurements for greasy wool has enabled the prediction of top characteristics to be placed on an objective basis for the first time. Prior to this, evaluation of processing performance was a matter of experience and judgement.
One of the most important customer requirements that a topmaker is trying to meet is Hauteur, or average fibre length. The topmaker also has to fulfil specifications for the distribution of fibre length, coefficient of variation of Hauteur (CVH), and also the short fibre content of the top. Each of these characteristics is considered important by the spinner. The length properties are second in importance to diameter in determining the value of a top.
Top fibre length properties depend on:
the original fibre length of the greasy wool;
the amount of fibre breakage (dependent on, e.g. fibre length, fibre strength, fibre entanglement and fibre crimp);
the location of fibre breakage along the length of the fibre
Due to the nature and complexity of raw wool consignments compiled to produce tops, it is a difficult matter to measure average FIBRE properties. In an ideal world this would be done.
However in each case listed there is a a measure which can be used to ESTIMATE the fibre properties listed.
Wool Staple Length can be used to estimate fibre length. The amount by which the average fibre length is greater than staple length is termed the fibre length to staple length ratio. This ratio commonly varies from 1.0 to 1.35 with an average of 1.17.
Similarly Staple Strength and Position of Break (POB) in a staple can be used to estimate fibre strength and fibre “point of break”.

## Slide 3: TEAM
Trials Evaluating Additional Measurement
  PREDICTION based on Objective Measurements
used simple regression techniques
603 consignments (88,000 bales)
28 mills in 12 countries
managed by industry committee
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
A series of trials was initiated in the early 1980’s to examine the predictability of top fibre length for commercial processing consignments based on raw wool specifications.
The trial were organised by the Australian Wool Corporation (AWC), now known as The Woolmark Company, the Australian Wool Testing Authority Ltd (AWTA Ltd) and CSIRO Division of Wool Technology.
The trials were officially known as the Trials Evaluating Additional Measurement (TEAM) in reference to the industry term “Additional Measurements”. This covered the recently introduced tests for Staple Length (SL), Staple Strength (SS) and POB.
TEAM was conducted in 2 stages. The first stage saw the TEAM 1 report issued in 1985 to coincide with the commercial release of the ATLAS instrument which measured SL, SS and POB. A formula was developed from this stage of the trial.
In 1988 a TEAM 2 report was issued after more processing was conducted and a larger database of consignments was available. The formula issued in this report is the one recommended as a starting point for mills today.
In total, TEAM involved trials with 28 mills in 12 countries and encompassed 603 commercial consignments.
Simple, multiple regression techniques were used to analyse the data collected.

## Slide 4: TEAM formula for Hauteur
H = 0.52L + 0.47S + 0.95D - 0.19M* - 0.45V - 3.5
H = Hauteur (mm)
L = Staple Length (mm)
S = Staple Strength (N/ktex)
D = Fibre Diameter (µm)
M*= Adjusted % mid breaks (%)
V = Vegetable Matter Base (%)
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
The aim of TEAM was to introduce a new concept within the wool trading and early stage processing industries. This concept was to use a mathematical formula based on objective specifications of raw wool properties to predict top fibre length.
The decision was taken to use a simple approach, multiple linear regression, which would be relatively easy to explain. It was also considered important for subsequent adoption of the technology that one general formula be obtained, rather than a series of formulas.
TEAM predictions are valid only if the raw wool & top properties of the consignment to be predicted fall within the range of properties included in the original data used to derive the regression equation. The TEAM equation is shown in this slide.
The wools in the TEAM consignments covered a wide range of wool properties and were composed of 70% fleece, 20% skirting and 10% mixed wools. The mean value and range of values for the raw wool characteristics of the original consignments were:
range mean
Mean Fibre Diameter (µm) 17 - 31 22
Vegetable Matter Base (%) 0 - 10 2.1
Staple Length (mm) 59 - 123 86
CV of Staple Length (%) 12 - 30 19
Staple Strength (N/ktex) 23 - 60 39
The final term in the equation is called the mill adjustment factor (Mill Factor). This factor is variable depending on how a particular mill performs in relation to the TEAM average. If a figure of 3.5 was found, the mill’s machinery would be performing to the average performance of mills used in the TEAM trial. A figure greater than 3.5 would mean that a mill performs below that average.

## Slide 5: Relative Importance of Properties
STAPLE LENGTH 100
STAPLE STRENGTH 88
DIAMETER 46
M* 40
VM 19
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
This table lists the relative importance of the raw wool terms in the TEAM equation as judged by the statistical significance of the regression terms. The values correspond to the relative influence each term in the TEAM formula has on determining the Hauteur (H) of the top.
The most important term Staple Length has been assigned the value 100 for comparative purposes. The other terms are rated relative to 100.
This table shows the overwhelming importance of Staple Length and Staple Strength in influencing the average fibre length (H) in the top.
This makes sense, in that a long, strong wool will end up longer after processing compared to a short weak wool, all other factors being equal.
The positive influence of fibre diameter on average fibre length is also important but not as significant. This is NOT related to the fact that broader wool tends to be longer because the length factor is already accounted for by Staple Length. It may be due to the amount of entanglement the wool undergoes during processing. Fine wool entangles more and is subject to more fibre breakage during processing than coarse wool.
Mid-breaks have a negative influence on H. A greater percentage of mid-breaks means that more fibres which are about half the length of the original fibre will be retained in processing because they are too long to be combed out. On the other hand, the short fibres formed from a tip or base break are more likely to be removed in combing. Once a fibre is removed it can’t influence the average fibre length.
The amount of VM also has a slight negative influence. This makes sense in that it would be expected that the presence of VM would lead to a slight increase in fibre breakage thus lowering the average fibre length.

## Slide 6: Further TEAM formulas
Noil% (N%)
N = - 0.11L - 0.14S - 0.35D + 0.94V + 27.7
Coefficient of Variation of Hauteur (CVH)
CVH = 0.12L - 0.41S - 0.35D + 0.2M* + 49.3
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
The TEAM trial in 1988 also led to the calculation of formulae for the amount of short fibre generated during combing (Noil% of clean (top & noil) weight) and the distribution of mean fibre length (CVH).
The TEAM management committee caution that the CVH and Noil% prediction are for guidance purposes only. This is because the precision of these figures is generally quite poor.

## Slide 7: Accuracy of TEAM predictions
(Actual - Predicted) Hauteur (mm)
0
20
40
60
80
100
120
-10
-8
-6
-4
-2
0
2
4
6
8
10
Frequency
Standard
Deviation: 3.4mm
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
This slide shows the accuracy of the TEAM prediction for H in the TEAM trials.
If the formula predicted perfectly then there would only be one column shown since measured or Actual Hauteur - Predicted Hauteur would always be zero.
However, that is not the case since the formula relies on a simple regression technique, and is really the average performance of the consignments used in the trial. The formula over-predicts and under-predicts.
From this histogram it can be seen that about 67% of the results fall in the range 3.4mm (i.e. one standard deviation either side of zero).
The precision of the prediction would be around 7mm according to this histogram. This means that 95 times out of 100, the Actual - Predicted Hauteur will be less than 7mm.

## Slide 8: Objective vs Subjective
-10
S.D. = 3.2mm
Accuracy of TEAM
- 4 mills
-8
-6
-4
-2
0
2
4
6
8
10
-10
-8
-6
-4
-2
0
2
4
6
8
10
Accuracy of Topmakers
- 4 Mills
S.D. = 2.8mm
(Actual - Predicted) Hauteur (mm)
Trevor Mahar
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Traditionally, the fibre length properties of the top have been gauged by experienced topmakers understanding how raw wool will process in their machinery.
The above slide shows the results from part of the TEAM trial where the accuracy of the predictions from experienced topmakers at 4 mills were evaluated against the accuracy of predictions using the TEAM formula for the same consignments at those mills.
The results show the TEAM formula performed at least as well as the experienced topmakers, considering the standard deviation figures derived from these histograms.
The closeness of these figures could explain why a proportion of topmakers don’t use the TEAM formula despite its availability and proven performance. However, as the level of experienced personnel declines in the industry, this situation is likely to change over time.

## Slide 9: Recommendations
Trevor Mahar
Formulas
Mill specific activities
Encourage additional measurements
Improve wool metrology
Improve processing knowledge
Harmonise testing
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
The TEAM management committee recommended that the formulas as they stand are reliable and robust for the range of wool processed in the trials. However, individual mills were encouraged to determine their own Mill Factor. This would prove a benchmark for mill performance as well.
Mills were further encouraged to develop their own formulas for specific processing lines, and also to fine tune the formulas for wool categories and types.
The industry as a whole was encouraged to adopt Additional Measurement. This is currently about 80% nation-wide.
The influence of other factors such as Style was recognised in that improvements in wool metrology in this area were called for, as well as an improvement in the level of knowledge of processing itself, e.g. where and how do fibres break in processing.
The need to harmonise testing was recognised, and the activities of Interwoollabs in this process were considered beneficial.

## Slide 10: TEAM - the balance sheet
Trevor Mahar
Positives
Introduced concept
Simple to understand
Simple to use
Based on wide variety of wools & mills
Based on processing consignments
Negatives
One general formula
May be oversimplified
Not most suited to grower lots
No inclusion of fibre behaviour
Notes: <number>
<footer>
Written by: Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
This trial was certainly the biggest and one of the costliest in the history of the wool industry. The benefits of the introduction of TEAM to the wool processing industry include introduction of a concept to the industry which is simple to use and understand, and which should be robust in that it encompassed a wide range of raw wool from Australia, and also the gamut of processing lines used world-wide.
A significant proportion of topmakers world-wide have adopted this technology which relies on objectively specified raw wool.
However, there is room for improvement in the approach which has seen further work done in this field. Further reading should include the Latest Developments in Prediction, where work looking at grower lot behaviour, and the consideration of fibre behaviour is discussed.