## Slide 1: Top Testing
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module covers information about some of the tests performed on tops to ensure they conform to customer’s specifications.
Spinners’ specifications vary, and only a selection of these tests may be necessary to fulfil the orders. Some tests have been covered in other modules, such as “Hauteur”, “Evenness” and “Regain”.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Top Specification (example)
Specification
Diameter (m)
Length (mm)
CV Length (%)
Oil Content (%)
Moisture (%)
Sliver Wt. (ktex)
Top Wt. (kg)
Top size
Evenness (% Uster)
Neps large
Neps small
Slubs
Vegetable Matter (VM) Seed
VM Burr
Coloured Fibre
Other Fibres
Colour
Standard Allowance
21.0 +/- 0.6
68 AH +/- 2
50
0.8
18.25
20
10
360mm x 400mm
3 +/- 1
1 per 10g Max
10 per 10g Max
1 per kg Max
15 per 250g Max
1 per 250g Max
1 per 10g Max
1 per 250g Max
as per sample
Peter Auer
Source: Ascough, S. (1994)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Ascough, S. (1994), Practical Hints to Improve the Quality and Performance of Australian Wool during ESP, AWRAP, Melbourne
The slide displays an abridged example of what a top buyer might specify to a topmaker with respect to the product they want. There is usually more specification involved with fibre length such as % fibres < 25mm and L 5% etc.
This would obviously vary according to which customers were involved, but provides a good example of the stringent requirements that a topmaker must meet.
Other modules cover Diameter, Evenness and Regain, so this module will concentrate on those not covered elsewhere.

## Slide 3: Regain & Invoice Mass
Regain
  standards applied
  18.25%
    (65% r.h., 20 oC)
    IWTO dry combed standard
  16-17%
    IWTO scoured wool
Invoice Mass
  scoured / carbonised
    IWTO- 33- 88(E)
  tops
    IWTO- 34- 85(E)
  capacitance
    IWTO- 41- 92(E)
  Near Infra-Red
    NIRS sensors
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Regain has been measured for many years with such apparatus as the CSIRO Rapid Dryer, which provides a direct readout of regain from a sample of wool. This particular method requires samples to be selected and measured during processing. The sample weight required is about 250g and the test takes about 10 minutes.
A newer method involves the use of the principle of conductivity, or capacitance. A similar principle is employed in the measurement of Hauteur and Evenness, whereby changes in mass can be detected by passing wool between electrically charged plates.
Both of these principles are sensitive to fibre diameter and chemical treatments, such as shrink-proofing. The methods must be calibrated to overcome this sensitivity.
The latest method of regain analysis involves the use of near infra-red sensors which can detect the actual amount of water in a sample by exciting the water molecules to a higher energy state. This excitation level can be measured and translated into regain by a calibration equation. This method is claimed to use less sample weight, and be less sensitive to fibre diameter and the treatments the wool may have undergone. The test time is about 5 minutes and requires about 10g of sample. The machines used still require calibration and routine checking.
The regain of the top can be adjusted during Finisher Gilling, usually by spraying water onto the sliver.

## Slide 4: Diameter of Top
Peter Auer
slight increase (1%)
  raw wool to top
    fine, short fibres combed out
diameter
  m
    mean
    variation
  % fibres >30m
    comfort factor
    prickle factor
measurement
  Projection Microscope
  Airflow
  SIROLAN-Laserscan
  OFDA
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The mean diameter of top is slightly higher, compared to the mean diameter of the raw wool in the consignment. The difference is significant but not great, about 1% coarser in tops. This is thought to be due to the fact that the noil removed during combing is from a part of the fibre population which is shorter and finer, about 10% finer.
As far as customer specifications are concerned the mean fibre diameter is paramount in present trading environments, while the distribution of fibre diameter in tops is becoming a feature of specifications, but adoption of these measurements is low.
Another diameter property which is gaining increasingly in importance is the % of fibres greater than 30m. This figure has been variously referred to as the comfort factor or prickle factor. A greater percentage of fibres above this diameter has been correlated to the level of discomfort felt by wearers of wool products. This figure can be derived from measurements of the diameter distribution.
As with raw wool, fibre diameter in tops can be measured in a number of ways. For further detail see the “Instruments to Measure Fibre Diameter” module. Of those listed above, only the Airflow method doesn’t return a value for diameter distribution.

## Slide 5: Linear Density
top
  weigh bobbins
  length counted during finisher gilling
sliver
  interim product
    “in-house”
  ruler
  tensioned sliver
roving
  wrap roller
yarn
  wrap reel
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The linear density of the finished top is also included in spinners’ specifications. Linear density of sliver and tops is usually expressed as kilotex (g/m). This can be determined by counting the length of top during packaging and weighing the package after they are full.
Sliver is an intermediate product and its linear density is important “in-house” to monitor processing performance.
Roving is another intermediate product which is monitored for quality control (QC) purposes. A wrap roller is used to measure 10m of roving wrapped around the roller of 1m circumference. The length is then weighed and the result may be expressed as kilotex (g/m) or decitex (g/10m).
The slide shows a wrap reel which is used to measure yarn. Usually 100m of yarn is wrapped at constant tension, and then weighed to return a result expressed as tex (g/km).

## Slide 6: Colour
Peter Auer
Standard
  IWTO- 35- 87(E)
  Degree of Whiteness
  whole spectrum (X,Y and Z used)
Measurement
  visual standards
  Instruments
    Colorimeter
    Spectrophotometer
    calibration
      reference wool & cream tile
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The colour of a top is important since this will determine the colour of the substrate that is dyed. The best substrate for colour matching during dyeing is pure white, although this is rarely achievable. The property measured is Whiteness, as opposed to Yellowness which is the measurement used for raw wool sales. See “The Measurement of Wool Colour” module for more information on yellowness measurement.
The colour of top can be determined by matching the finished product to visual standards. This is a subjective measurement, but may be all that some customers require.
Objective measurements may be made using a colorimeter or a spectrophotometer. These return CIE tristimulus values of the sample, expressed as X,Y,Z, or as L*(brightness), a*(green-red), b*(blue-yellow).
The Degree of Whiteness (W) is derived from the equation:
W = [(100-0.94Y)2 + (2.84X - 2.35Z)2 ]1/2
Whiteness refers to the whole visible colour spectrum, hence the use of X, Y and Z.
A reference wool is used to calibrate a cream reference tile, rather than a white tile which is common in the colour matching industry.

## Slide 7: Fault Content (VM & Nep)
Standard
  IWTO- 24- 73(E)
definition
diversity
variable frequency
Peter Auer
Source; ASTM-D-1770
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source of diagrams: ASTM-D-1770, Fig 11 & 12.
The difficulty in the determination of the fault content of tops is in their definition. They are very diverse, and they also occur with variable frequency. Therefore their measurement is fraught with inherent difficulties. Nevertheless, top buyers require that the level of these faults is controlled in the final product, so methods have been developed to define and measure them.
Some faults are listed as:
straws and bast fibres (various lengths)
burrs
coloured fibres
slubs
neps
foreign fibres
The diversity of VM faults and the various sizes of nep faults are illustrated above.

## Slide 8: Top Fault Measurement
mechanical opening device
  manual counting
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Several mechanical opening devices have been developed to aid the difficult task of measuring top faults. Generally these devices consist of a drafting zone which thins the top and also spreads it out to be displayed over a background field. The length of top opened is usually 1m long.
The background field may be illuminated, or black depending on the fault being measured. For example a balanced light field consists of lighting from above and below which allows dark fibres to be easily identified and counted.
This method is manual and the web density may have an effect on the count of faults. The results tend to be variable and operator dependant.

## Slide 9: pH
Standard
  IWTO- 2- 86(E)
isoelectric point
  pH 4.8
processing history
  affects pH
  alkaline scouring
  suint content
pH limits vary
  important for dyeing & Superwash
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The pH of the top can be a part of top specifications.
Whilst there is some literature which suggests that the control of static electricity plays a part in the specification of pH, the use of humidity and anti-static applications should take care of this problem.
The main usage of tops with a specified pH is for treatments such as Superwash which are affected by the pH of the emulsion solution. The pH of the top will also affect the dyeing properties of the wool (especially where top dyeing is employed).
The top pH is determined by measuring aqueous extractions of top samples as described in the listed standard.

## Slide 10: Oil Content
spinning oils added
measurement
  residual fatty matter content
    base level
  Soxhlet extraction
Delivery Configuration
Bobbins
Bumps
Hanks
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Spinning oils can be added to control static electricity during spinning and may be part of the top buyers specifications.
The %oil and residual fatty matter content are usually determined using Soxhlet extraction and a suitable solvent.
In the determination of %oil added, the level of residual fatty matter must be known, otherwise only the total solvent extractables can be determined.
Finally the delivery configuration of the tops may be specified. This can be in the form of bobbins, bumps or hanks. The final agreement is tied to the needs of the customer. For further information see “Gilling” module, and the formation of these top forms.

## Slide 11: References
Barker, S.G.(1931), "Wool Quality", WIRA, HM Stationery Office, London
Morton, W.E. and Hearle, J.W.S., (1962), "Physical Properties of Textile Fibres", The Textile Institute, Butterworths, London
Ascough, S., (1994), "Practical Hints to Improve the Quality and Performance of Australian Wool during Early Stage Processing", AWRAP, Melbourne
Peter Auer