## Slide 1: Style Effects in Processing
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. W. Humphries, CSIRO Textile & Fibre Technology and
Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Notes: <number>
<footer>
This module considers the ramifications of wool style in terms of its effects on processing performance, particularly topmaking.
The material is largely drawn from the CSIRO Division of Wool Technology’s seminar Woolspec 94. Copies of the proceedings are available from CSIRO Textile & Fibre Technology, formerly Division of Wool Technology.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. W. Humphries, CSIRO Textile & Fibre Technology and Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.

## Slide 2: Specific Style Effects in Topmaking
crimp
  frequency
  definition
fibre damage
staple tip structure
W. Humphries & T. Mahar
Notes: <number>
<footer>
Written by: Dr. W. Humphries, CSIRO Textile & Fibre Technology and Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
During topmaking many fibres are broken. Therefore while mean diameter changes very little, mean fibre length can change dramatically. So, topmaking performance is measured primarily as effects on fibre length (Hauteur) and on yields such as card yield and Romaine or noil. Colour and faults such as neps, vegetable matter and dark fibres are also measured.
Currently, appraised style does not necessarily imply expected processing capabilities, however, as part of its style research project, CSIRO is investigating the relationships between measured style components and processing performance. The following describes this work as it applies to topmaking.
In evaluating specific style effects in topmaking, it should again be emphasised that mean diameter, staple length, staple strength, position of break and vegetable matter content together account for 80% of the variation in Hauteur. The effects of style in processing should be seen in this light (i.e. it is expected that the contribution of style effects to topmaking performance will be small).
This module will summarise some specific style effects (crimp, fibre damage and staple tip structure) on processing performance in terms of Hauteur.

## Slide 3: Crimp
H predicted without crimp (frequency & definition)
70
70
80
60
60
80
R2 = 0.79
70
70
80
60
60
80
H predicted with crimp (frequency & definition)
R2 = 0.94
Measured Hauteur (mm)
W. Humphries & T. Mahar
Notes: Written by: Dr. W. Humphries, CSIRO Textile & Fibre Technology and Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
The graph above demonstrates the effect that the inclusion of crimp factors of frequency and definition can have on predicting Hauteur. In this case the inclusion of crimp parameters greatly improved the correlation coefficient between the actual Hauteur and the predicted Hauteur.
In a maximum crimp effect topmaking trial conducted by CSIRO and reported in Woolspec94, Style and Processing Effects, it was found that Hauteur increases as crimp frequency decreases and as crimp definition improves. In this carefully controlled trial it was seen that;
+1 crimp definition grade = -1 crimp frequency grade = +4mm Hauteur
(steps of ~1crimp/cm)

## Slide 4: Fibre Damage
environmental factors
  staple crimp definition
  ultraviolet light
  dust contamination
position of damage
  problems with detection
W. Humphries & T. Mahar
Source: Stevens, D. and Crowe, D.W., 1994
Notes: Written by: Dr. W. Humphries, CSIRO Textile & Fibre Technology and Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Source: Stevens, D. and Crowe, D.W. (1994), Style and Processing Effects, In: seminar Proceedings ‘Specification of Australian Wool & Its Implications for Marketing and Processing’, Woolspec 94.
Any damage to the staple will weaken the fibres within the staple and thus affect the processing performance of that wool by increased fibre breakage, and also increased fibre loss.
Major environmental effects which damage the staple are UV rays from the sun and contamination due to dust. Researchers have found that staples’ crimp definition is adversely affected through the action of dust and weathering. Also staples with a long tip are more likely to be effected by weathering and water and dust penetration than those staples with a blocky tip.
Damage in the staple tip, such as weathering presents potential problems for its detection by staple strength measurements. Unless it extends beyond the jaws of the ATLAS instrument and is weaker than other areas in the staple it may not be detected in the measurement of length and strength. The potential impact that weathering may have on processing performance and processing prediction would remain unknown.
Trials have shown that fibre damage caused by environmental factors has a detrimental effect on Hauteur, increases card waste and romaine.

## Slide 5: Staple Tip Structure
120
100
Mean Fibre
length (mm)
Staple length
Fibres
Fibre length to staple length ratio: 120/100 = 1.20
W. Humphries & T. Mahar
Notes: Written by: Dr. W. Humphries, CSIRO Textile & Fibre Technology and Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Tip structure is thought to correlate to the degree of variation in fibre length within a staple.
The fibres within a Merino wool staple are on average longer than the staple length. The relationship between the average fibre length and staple length is termed the fibre length to staple length ratio. This ratio usually varies from 1.0 to 1.35 with an average value of 1.17. It is this 1.17 value which is assumed in sale lot prediction formulae.
This slide shows a representation of fibre length to staple length ratio.

## Slide 6: Staple Tip Structure
Lot A Lot B
Diameter (µm) 20.6 20.7
Staple Length (mm) 77 73
CV Staple Length (%) 18 16
Staple Strength (N//kt) 33 42
% Mid Breaks 55 58
Fibre Length
* Predicted 61 61
* Actual 62 51
* Actual - Predicted 1 -10
Ratio of fibre length to 1.20 0.97
staple length (FL/SL)
Incorporate actual FL/SL
* Predicted 62 51
* Actual - Predicted 0 0
W. Humphries & T. Mahar
Source: Mahar, T.J. et al 1994
Notes: <number>
<footer>
Written by: Dr. W. Humphries, CSIRO Textile & Fibre Technology and Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Source: Mahar, T.J., Brown, G.H., Osborne, L.J. and Burke, A.J., (1994), Prediction of Processing Performance for Sale Lots and Consignments, In: seminar Proceedings ‘Specification of Australian Wool & Its Implications for Marketing and Processing’, Woolspec 94.
The slide above demonstrates the effect that the fibre length to staple length ratio can have on predicting processing performance. The effect of changing the FL/SL ratio within the formula to the actual figure for that lot is clearly demonstrated in the above examples where lot B prediction changed from a difference of actual minus predicted of -10 to 0.
Other trials have also found a trend for Hauteur to decrease with increasing tip length, although the effect was not large.

## Slide 7: Summary of STYLE effects
crimp frequency: 4mm H per 1-1.5 crimps/cm
definition: 8mm H between extremes
fibre damage: up to 10% card waste
(weathering) up to 7mm H (depending on
severity)
tip shape: 8mm H adult / hogget
W. Humphries & T. Mahar
Source: Stevens, D. and Crowe, D.W., 1994
Notes: <number>
<footer>
Written by: Dr. W. Humphries, CSIRO Textile & Fibre Technology and Dr. Trevor Mahar, Australian Wool Testing Authority Ltd.
Source: Stevens, D. and Crowe, D.W. (1994), Style and Processing Effects, In: seminar Proceedings ‘Specification of Australian Wool & Its Implications for Marketing and Processing’, Woolspec 94.
These are the current best estimates of the effects of the various style parameters on processing performance.
Each of the components can be shown to affect Hauteur and other processing parameters due to their relationship to the amount of fibre breakage during carding and combing.
However, appraised style grade effects are less clear, mainly because they result from the interaction of several aspects of style. These results are now being confirmed for many different wool types with a wide variety of style attributes.