## Slide 1: The Implications of Raw Wool Properties to a Top-maker
Produced for the CRC for Premium Quality Wool undergraduate program by;
Ms. J. Turk, G.H. Michell & Sons Pty Ltd.
Notes: This module outlines the implications of raw wool properties to a commercial top-maker, and as a consequence, to the customers of the top-maker.
An example of how a particular raw wool property can affect a batch of tops is provided.
Produced for the CRC for Premium Quality Wool undergraduate program by Ms. J. Turk, G.H. Michell & Sons Pty Ltd.

## Slide 2: Raw Wool Parameters
staple length
staple strength
POB
  equally important for H
  included in TEAM
Judy Turk
Notes: Written by: Ms. J. Turk, G.H. Michell & Sons Pty Ltd.
The raw wool characteristics which play the major role in determining the final length of the top are staple length, staple strength and position of break.
Weak wool with a high percentage of mid breaks always causes problems. Such wool would produce a top with a lower Hauteur, higher CVH and greater percentage (%) of short fibres. It wouldn’t be used in a good spinning blend. However it can be used in the type of blend that compares with a Fleece/Pieces blend.
Each mill knows the approximate strength of wool it needs to achieve a required mean fibre length in the top. There is no exact cut-off between weak and strong wool, but once the strength of wool is above 40 N/ktex it would be universally accepted as sound.
The inclusion of POB into TEAM II was readily accepted by mills. Position of break gives a very good indication as to where the wool fibre has the greastest potential for breakage. Base and tip breaks mean that the ends will likely be lost to noil during combing, without having a significant effect on Hauteur, while high mid-breaks means that both broken ends are retained past combing, but will have some effect on the subsequent average fibre length in the top.

## Slide 3: Raw Wool Parameters
Mean Diameter
  higher in tops
    ~0.2m
  greatest price effect
  effect on H
  included in TEAM
CV Diameter
  8% in top
  not in customer specs yet
  no raw wool information yet
    niche markets only
  can’t assess effect on H
Judy Turk
Notes: Written by: Ms. J. Turk, G.H. Michell & Sons Pty Ltd.
Mean fibre diameter has the greastest influence on the price of both raw wool and top. Tops produced from finer diameter wools are able to be spun into finer yarns and hence made into garments which are lighter, softer and have a higher comfort factor. For more information in this area see module “Developments in Yarn Technology”.
Fibre diameter is the easiest parameter to predict and relate to the final product. Airflow measurement has been universally accepted for attaining the mean fibre diameter and is used for all pre-sale testing and most top trading. The development in more recent years of Sirolan-Laserscan and OFDA now allows for the measurement of CVD as well as mean fibre diameter. It is envisaged that in early 2000 Laserscan measurement will be introduced into the testing houses and replace the more traditional Airflow method. For more information see the module “Instruments to measure Fibre Diameter”.
The prediction of top diameter is slightly different for each mill because of the different machine settings and processing parameters used. If comb gauge settings are “wide”, a large number of short, and therefore fine, fibres will be removed. Conversely, if the gauge settings are narrow, the finer fibres will remain in the top. The usual effect is for the top to be slightly coarser than the greasy wool.
Now that CVD is more readily available, buyers and sellers are on a learning curve with this parameter. Michell laboratories have been measuring CVD in tops with the projection microscope for many years and haven’t seen a huge shift in CVD. The range in tops is not large (about 8% CVD, from 20 - 28%), over the general diameter range. So there doesn’t seem to be a lot of room for improvement.
CVD of greasy wool is as not yet routinely reported, and therefore a mill factor to predict how it behaves and how it affects the final product has yet to be determined. It will be a few years before this parameter can be introduced as a specification.

## Slide 4: Raw Wool Parameters
VM
  effect on yield
  effect on plant settings
  VM types
  effect on H
    fibre breakage
Style
  possible effect on H
  refine TEAM II?
    more info needed
    fine tuning only
Crimp effects
  mills interested
Judy Turk
Notes: Written by: Ms. J. Turk, G.H. Michell & Sons Pty Ltd.
The vegetable matter base (VMB) has a direct effect on mill production yield. The mill needs to know how much VM is in a batch to get their machinery setting right. It is used in the TEAM formulas as it is known that VM causes fibre breakage and fibre loss.
The type of VM has a large effect on plant settings. Some types are easy to remove and others like shive behave like wool fibres and may end up in the final product. Bathurst and Nagorra burr can stick to the card clothing, requiring the card to be fettled (teeth cleaned).
Objective style is a parameter still being developed and trialled but the results could help to refine prediction formulas. It should be noted however that 80% of the variation in mean fibre length in top is accounted for in the existing parameters of staple length, staple strength, fibre diameter, POB and VM, so the introduction of style parameters into any prediction would be fine tuning.
The measurement of crimp is of interest to topmaking mills, and Michells looks forward to its introduction.
For more information on style effects in processing see the module “Style Effects in Processing”.

## Slide 5: Other Parameters
Yield
  Wool Base
  Top & Noil Yield
    affects price paid
    affects costs incurred
Colour
  important to end-users
    blends
    dyeing
Judy Turk
Notes: Written by: Ms. J. Turk, G.H. Michell & Sons Pty Ltd.
Wool Base and estimated Top and Noil Yield have been extremely valuable to mills to calculate prices paid, costs incurred and for batch formation. Mills cannot imagine now trading without a raw wool yield measurement. For more information on yield and its measurement see modules “Wool Base and Vegetable Base” and “Yield Determination”.
The greasy wool colour is a poor indicator of top colour. Greasy wool must be scoured and measured for colour. Scoured colour is a good indicator of top colour. The module “Measurement of Wool Colour” is of interest here.
The objective measure of scoured wool colour gives what is known as ‘base colour’. This is important to the processor, because to produce a wool that will dye to bright clear colours and mix with synthetics it must be as white as possible. Spinners are starting to specify this characteristic.
However, not all wool is required to be white. If the mill knows the end market for the wool, then a cheaper blend containing yellower wools could be assembled for the spinner. In the extreme, which is an end use which is black or a very dark colour, a top can be made using stained wool.
The price of a top is also reliant on colour. A stains tops will be much cheaper than a white top.

## Slide 6: Processing Example
Two tops produced for Japan - 2 X 48’s Weaving Yarn
TOP A TOP B
H 72 67
CVH 45 49
<40mm 20% 25%
SS 38 32
SL 85-90 85-90
Which top do you think would spin better?
Judy Turk
Notes: <number>
<footer>
Written by: Ms. J. Turk, G.H. Michell & Sons Pty Ltd.
This is a specific example of the performance of two batches of tops produced at Michell & Sons. It is provided to illustrate the importance of raw wool parameters to the top-maker.
These 2 batches were produced from 22µm, 100% fleece wool.
The resultant difference in Hauteur would cause no problem in processing. However, the major difference between the batches is the CVH caused by the difference in the staple strength of the wool.
The processing (spinning) performance parameters for each batch are listed below.
Top A Top B
Spindle Speed 10800 8500
Product/Day 3551 Kg 2795 Kg
Conversion cost/kg US $4.01 US $5.10
Top B cost more to produce with yarn of reduced evenness and yarn strength. Its performance is clearly inferior in spinning.
This example shows that raw wool specifications are critical. To achieve a CVH of 45%, strong wools must be used. The correlation between CVH and short fibres is high.