## Slide 1: Sampling Theory
Produced for the CRC for Premium Quality Wool undergraduate program by;
Angus Ireland, Australian Wool Testing Authority Ltd. and
Dr. Peter Auer, The University of New South Wales.
Notes: <number>
<footer>
Metrology comprises sampling and measurement. Generally, the aim is to obtain an estimation of the average value of a property within a population.
This module addresses some basic theory which will aid the understanding of metrology.
At the completion of this module you should understand the principles of sampling, the meaning of accuracy and precision, and how precision is calculated.
Produced for the CRC for Premium Quality Wool undergraduate program by Angus Ireland, Australian Wool Testing Authority Ltd. and Dr. Peter Auer, The University of New South Wales.

## Slide 2: Populations
Beers in the bar
Life jackets in aeroplanes
Diameters of wool fibres
Angus Ireland
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
Samples are taken to reliably describe some characteristic of a population. This happens routinely in many industries.
In the absence of sampling and testing there would be less confidence in our lives. For example:
As you get in the car to drive home from university, you couldn’t be sure whether the beer you’d just drunk was 2.5% or 7.5% alcohol; or
When the plane you are flying in flops down into the ocean and you pull on the cords of your life jacket to release the compressed air, there would be no guarantee that the jacket would actually inflate; finally
If you are a wool buyer with a contract to deliver 16,000kg of 19.5µm wool to an Italian mill, and there was no sampling and testing, you would be relying entirely on your subjective skills of looking at and handling wool to save yourself from exceeding the tolerance and suffering a high financial penalty.

## Slide 3: Consequences of lack of confidence in test methods or results
Angus Ireland & Peter Auer
Brokers: Check each sample
Buyers: Call up bales
Carry risk
Processors: Repeat testing
Financial claim
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
In the wool industry, lack of confidence will have a number of consequences, including:
Brokers who lack confidence in test methods will carefully check each sale lot against the results to determine if the testing was wrong so that a check test can be performed if necessary.
Buyers will pay less for wool because they carry a risk that the test results are wrong.
Processors will insist on repeating the test on receival of the wool, so that if they haven’t got what they asked for, they can make a financial claim against the buyer.
Uncertainty at each stage in the pipeline adds costs to the final product which ultimately reduces the competitiveness of wool against other natural fibres and synthetics.

## Slide 4
Precise
Imprecise
Accurate
Inaccurate
Angus Ireland & Peter Auer
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
A test result obtained through metrology can vary from the “true” result in two ways.
It can be inaccurate, i.e. moving to the right of the chart, the test results are some distance away from the target. This can be caused by poor calibration, or instrument failure.
It can be imprecise, i.e. moving down the chart, the test results are scattered. This can be caused by an inadequate sampling regime, or a highly variable population. These two factors go hand in hand, since the sampling regime should reflect the variability of the population, but it is not always economically viable to do this. In reality the precision of the test can be defined by statistical analysis. This figure is called the 95% confidence limit. This is commonly called “precision” in metrology parlance.
Ideally, metrology should return a result which is both accurate and precise, i.e. the average result is repeatable and within clearly defined limits of the “true” result.

## Slide 5: There are a HUGE number of fibres in a sale lot.
7 bales per sale lot
7 bales * 40 fleeces = 280 fleeces / lot
280 fleeces * 54,000,000 fibres/fleece
15,120,000,000 fibres/lot (rough estimate)
How do we get a REPRESENTATIVE sample?
Angus Ireland & Peter Auer
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
A good example of the difficulty in sampling an entire population is to consider the number of fibres in a sale lot.
How many fibres need to be sampled and measured in order to give a reasonable estimate of average fibre diameter?
For fibre diameter measurement using Laserscan, 7 bales of fibres (approx. 1200kg) are reduced to a sample weighing less than 0.1 grams. Clearly, sampling and preparation must be thorough to give a result that is representative of the entire sale lot.

## Slide 6: Principles of Sampling
Angus Ireland & Peter Auer
sample
  unbiased (representative)
achieved by design
  equal chance
    design
  free from manipulation
    machines more consistent
  sufficient sample size
    dependent on population variability
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
The outcome of metrology is an estimation of the “true” value of a property within a certain population (or group).
In most cases the total population can’t be measured, e.g. the diameter of all the fibres in a wool bale. Therefore sound metrology must be based on measurements made on an unbiased or representative sample.
There are some basic steps to achieve a representative sample.
The design of the sampling regime (e.g. how many cores need to be taken per bale) will ensure that there is an equal chance for each of the population to be picked. During the selection of the sample, manipulation needs to be avoided. (Generally, machines perform this function most consistently).
The variability within a population determines how many samples need to be taken (e.g. if all the fibres in a wool bale had the same diameter, then only one fibre would need to be sampled to estimate the diameter of all the fibres). If the population is more variable then more samples must be taken to adequately represent the population.

## Slide 7: Natural Variation: 22 micron wool fibres
No diameter variation
Between fibre variation
Along fibre variation
Angus Ireland & Peter Auer
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
A good example of natural variation in the raw material is that of fibre diameter.
It has been found that the BETWEEN fibre variation can be from 8µm to 65 µm.
The variation ALONG a single fibre can also be very significant. Normal growth patterns can lead to a small variation, while abnormal health and nutritional conditions, or pregnancy can lead to a complete “break”, a zero diameter in effect.

## Slide 8: Sources of Variation
Angus Ireland & Peter Auer
raw material
sampling
tests
measurements
operators
labs
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
The total variance of a test method takes into account all the sources of variation within a sampling and test regime. These sources of variation include the variability of the raw material, the variability inherent in sampling, the variability of the test itself, the variability of each measurement within the test, the variability between operators, and the variability between laboratories.
The relative influence of each of these sources of variation changes for each property measured. Some sources of variation may be negligible depending on the sampling and test regime.
The sources of variation for each raw wool property used commercially have generally been researched and calculated using a statistical method called Analysis of Variance. This is because these measurements are used in trading and process control, so the variability of the measurement is of vital interest in terms of the risk involved.
In some cases, the sources of variation may be broken down into a simple differentiation between WITHIN laboratory variance (which would include natural variation, sampling & testing variation) and BETWEEN laboratory variance.

## Slide 9: What is the Total Variance?
Total Variance = variance per bale + variance per core + variance per test + variance per sample + variance per fibre etc.
  the sum of the fractional variances
  apply known values to the formula
calculate precision
  PRECISION = +/- 1.96 X Total Variance
  95% confidence
Angus Ireland & Peter Auer
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
The Total Variance is therefore the sum of the fractional variances.
For example when measuring fibre diameter with FDA (a predecessor of Laserscan), it has been calculated that the variance caused by the fibre is 21.8µm2, however the variance per fibre (fractional variance) included in the calculation of Total Variance is 21.8 / 2000 since 2000 fibres were measured per FDA subsample.
The same reasoning can be applied to the inclusion of the fractional variances for the sampling and test regime. That is the number of samples and the number of tests has a direct effect on the Total Variance.
The value for the precision of the test is calculated from the Total Variance.
The precision, in statistical terms, is the 95% confidence interval (95% CI), i.e. when all the variation within the test is considered the “true” result will lie within the interval defined by the precision 95 times out of 100.

## Slide 10: Example of Total Variance
Total Variance (FDA)
= 0.083 / 20 + 0.016 / 2 + 21.8 / 2000
= 0.00415 (18.1%) cores
+ 0.008 (34.7%) subsamples
+ 0.0109 (47.3%) fibres
= 0.02305
Precision = 1.96 X 0.02305 = +/- 0.30
Angus Ireland & Peter Auer
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
This example should reinforce what has been learned about the calculation of Total Variance.
The following figures have been calculated for the sources of variation in the test for fibre diameter using the Fibre Diameter Analyser (FDA). This machine is obsolete but the example is still helpful, especially since the research was carried out that separates individual components of variance.
Source Variance
cores 0.083
subsamples 0.016
fibres 21.8
The sources of variation involve core sampling, subsampling, and the raw material.
The fractional variances are added to calculate the Total Variance. 20 cores were taken, two subsamples were measured and 2000 fibres were measured.
The precision can be calculated from this, and tells us that 95 times out of 100, the “true” result will be somewhere in an interval of 0.60 about the average (mean) result.

## Slide 11: 95% Confidence Limit & Interval
For Example:
30.0µm +/- 0.6µm (Limit)
29.4µm - 30.6µm (Interval)
Angus Ireland & Peter Auer
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
This is a further measure of the precision of diameter obtained after sampling and testing. This value is an estimate of the ‘true’ diameter and this estimate has definable levels of precision.
The measure of precision or confidence limits of the estimated mean fibre diameter are able to be specified because there is a tight control over the methods of sampling and testing to ensure they are conducted according to an agreed standard method.
So, if the true diameter of a sale lot was 30µm and it was repeatedly tested 100 times, it is known that on 95 of these occasions, the measured diameter would be within 0.6µm of the true diameter, or with the range 29.4µm to 30.6µm.
This measure of precision is known as the 95% confidence limit. The range is also known as the 95% confidence interval

## Slide 12: Improving the Precision of a Test Result
Angus Ireland & Peter Auer
Effect on 95% Confidence Limits
(wools > 26µ)
Multiple
Tests
%
Improvement
in Precision
1
2
4
10
0
29
50
68
0.60
0.42
0.30
0.19
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
The major opportunity for improving the precision of a test result is by conducting more sampling and testing.
The table demonstrates the benefit obtained by carrying out multiples of the current sampling and testing regime.
The same improvement in precision is obtained when individual sale lots are assembled into processing parcels for shipment to the mill. Most processing parcels (consignments) are at least 10 lots, giving a 68% improvement in precision, or diameter confidence limits +/- 0.19µm for wools coarser that 26µm.

## Slide 13: Precision - How it can vary
Angus Ireland & Peter Auer
Source: IWTO 12
0.21
0.35
0.48
0.60
0.73
0.85
0
0.2
0.4
0.6
0.8
1.0
0
10
20
30
40
50
Mean Fibre Diameter (µm)
95% Confidence Limit (µm)
Notes: Written by: Angus Ireland, Australian Wool Testing Authority and Dr. Peter Auer, The University of New South Wales.
Source: IWTO 12
An interesting example of how the precision of measurements can vary is provided by this chart. The precision as defined as the 95% confidence LIMIT of Laserscan diameter measurements for aqueous scoured wool is plotted against the average diameter (micron) values for the samples.
The chart shows that the precision of diameter measurements is related to the diameter over a wide range. However, it should be noted that the diameter range for Australian wool generally falls between the red lines, so the range of precision is quite narrow for Australian wool.
Note: For the derivation of the above Confidence Limits, see Lindsay, A.R., IWTO, Raw Wool Group, Nice meeting, December 1996.