## Slide 1: What Is Fibre Diameter?
Produced for the CRC for Premium Quality Wool undergraduate program by;
Michael Bow, retired, CSIRO Division of Wool Technology and,
David Petrie, The University of New South Wales,
Notes: This module explains the importance of wool fibre diameter, and explores the difficulties in defining just what diameter means in terms of wool diameter measurement.
Produced for the CRC for Premium Quality Wool undergraduate program by Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.

## Slide 2: What is Fibre Diameter?
Diameter
Mean fibre diameter
Variation in diameter
  Standard deviation
  Variance
  Coefficient of variation
Fibre Morphology
M. Bow & D. Petrie
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Diameter is defined as the length of a straight line through the centre of a circle or sphere.
Mean fibre diameter is the average diameter measured in micrometres (m), or a millionth of a metre. The unit is commonly called microns.
Statistically mean is expressed as:
X = Xi / N
(where Xi is the diameter of the ith fibre, N is the total number of fibres measured).
The variability of the measurement is also important. Terms such as Variance and Standard Deviation describe the extent of dispersion or variation around the mean.
Statistically Variance is expressed as:
Variance (SD2) =  (Xi - X)2 / N
Variance is also known as the Sum of Squares (SS) which is obvious from the formula.
The standard deviation (SD) is simply the square root of the Variance.
The coefficient of variation (CV) is defined as the Standard Deviation expressed as a percentage of the mean, i.e.
Coefficient of Variation (CV) = SD / X x 100 %
Why we measure average diameter becomes clear when we examine the morphology or form and shape of wool fibres. Not all fibres are circular in cross-section.

## Slide 3
M. Bow & D. Petrie
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
While the geometrical definition of diameter is unequivocal, how this relates to wool fibres is less clear.
Wool fibres are slightly elliptical as can be seen in this slide. While many fibres are circular in cross-section, the average ratio of the maximum width to the minimum width is 1.2 :1, while a few fibres may reach 4:1.
The fibre is a three dimensional object that is also curved in three dimensions and has a rough or scaly surface. Diameter is a planar concept, therefore there is a question of what plane through the fibre is to be considered. Scale edges are about 0.5 m above the fibre, therefore moving fractionally on or off a scale edges could change a measurement by 5%.
Perhaps we can consider the concept of "equivalent diameter”, i.e. no matter what the shape of the cross-section it can be converted to a circle and the diameter determined?
Even this concept needs further definition. Is the equivalent circle to be determined by area, perimeter or by projected width? The latter even needs further comment. For example, is it the average width or a width at random?
How diameter is actually measured is determined by the type of instrument used, e.g. Projection Microscope, Airflow, Sirolan-Laserscan, or Optical Fibre Diameter Analyser (OFDA).

## Slide 4: Diameter Distribution
Fibre Diameter (µm)
Frequency (%)
M. Bow & D. Petrie
Source: Bow, M. and Hanford, K. (1994)
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Source: Bow, M.R., and Hansford, K.A., (1994), “Fibre Diameter Variability”, In seminar Proc. Woolspec 94, Specification of Australian wool and its implications for marketing and processing, Nov. 1994
In the graphs above actual distributions for 17.5 and 23.3 µm wool are compared to the normal or “Gaussian” distribution (blue) with the same parameters of mean fibre diameter and SD.
The distribution of diameters is not normal, or Gaussian (bell-shaped). The distribution is noticeably skewed to the right, i.e. there seems to be a coarse “tail” inherent in the distribution.
However the terms used to describe these distributions are usually those of a Normal curve, i.e. mean, standard deviation (SD) and Coefficient of Variation (CV).
While this variation from “normal” is slight, it is a source of error. However, there does not appear to be any serious problems in using the assumption of normality.

## Slide 5: Importance of Fibre Diameter
75 - 80% of the value of top
Yarn
  spinning efficiency
  bending properties
Fabric
  fabric weight
  drape
  prickle
Supply
M. Bow & D. Petrie
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Mean fibre diameter is the most important raw wool property measured and accounts for 75 - 80% of the value of the top. Hence, mean fibre diameter is a significant determinant of the price of greasy wool.
Following are a number of reasons for the importance of fibre diameter. It is worth noting that it is one of the few raw wool parameters that remains virtually unchanged during processing.
Diameter limits the yarn thickness (count) that can be spun from a given raw material. A yarn requires a minimum number of fibres in its cross section. Yarn thickness or linear density is limited by both mean diameter and the diameter distribution (Martindale’s theorem).
For a given yarn count various physical characteristics of the yarn such as bending rigidity and extension depend on the diameter of its constituent fibres, as well as the yarn twist and the spinning method.
Yarns are woven or knitted into fabrics. Important fabric characteristics such as fabric weight, drape, handle, and comfort, “prickle” in next-to-skin wear (the mechanical effect of thick fibres poking into the skin) are dependent on the fibre diameter used.
While in most cases the finer the fibres the more attractive the material, there are two factors that work against the use of finer fibres. Sheep that grow fine wool generally grow less of it and the processing of finer wools is often more difficult and more expensive.
There is another important factor that governs the value of fibre diameter in the raw material and that is supply. In Australia, the world’s major supplier of apparel wool, the greater mass of wool is about 22 to 23 m, with the supply reducing as the diameter becomes finer or coarser.

## Slide 6
M. Bow & D. Petrie
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Finally in this module, it is worth noting that diameter as a specification is used only in wool and other animal fibres such as mohair and cashmere goat fibres.
In other textile fibres like cotton and man-made fibres the cross-section may not be remotely circular. This slide shows a micrograph of raw cotton fibres which are actually collapsed tubes.
The equivalent measurement for these fibres is linear density or mass per unit length. The units used are denier (g/9km) or decitex (g/10km) in man made fibres and Micronaire values for cotton which are in units of grains per inch.