## Slide 1: Core Sampling
Produced for the CRC for Premium Quality Wool undergraduate program by;
Angus Ireland, Australian Wool Testing Authority Ltd.
Notes: <number>
<footer>
The objectives of this module is to explain the procedures and apparatus involved in core sampling.
There are two (2) types of samples taken from bales: core samples and grab samples.
CORE samples are taken for the measurement of characteristics which don’t require fibre or staple integrity to be maintained, such as Mean Fibre Diameter, Yield, Vegetable Matter Base (VMB) and Colour.
GRAB samples must be taken where full length staples are needed, such as tests for Staple Length and Staple Strength and Style measurement.
Produced for the CRC for Premium Quality Wool undergraduate program by Angus Ireland, Australian Wool Testing Authority Ltd.

## Slide 2: Standards
IWTO Core Test Regulations
The purpose of core sampling is to obtain a sample (approx. 1kg) of raw wool snippets which is representative of the sale lot.
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The purpose of core sampling is to produce a sample of approximately one kilogram of raw wool snippets which is representative of the sale lot.
The key word here is "representative" because if the sample is not representative of the sale lot for the characteristics of Yield, Diameter, Colour and VM, then it doesn't matter how well the testing is conducted, the results won’t accurately reflect the wool being sold.

## Slide 3: Core Sampling Apparatus
Source : “Testing Your Woolclip”, AWTA customer brochure
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
Source: “Testing Your Woolclip”, AWTA Ltd.. customer brochure
This picture shows a core sampling machine at work. The coring tubes are inside the bale.
These tubes are pushed into the end of the bale and take a small core sample from each fleece as they pass through the bale.

## Slide 4: Sampling Method
i) 20 cores per sale lot (minimum)
ii) Every bale sampled
iii) Same number of cores per bale
iv) Cores randomly placed
v) Core penetrates full depth
Angus Ireland
Notes: Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
Core sampling is used to gather samples which are utilised to measure Fibre Diameter, Yield and Vegetable Matter Base of the sale lot.
The sampling regime is listed above. This regime produces a sample which is representative of the sale lot, providing the 5 basic rules listed are followed.
e.g. if there is a 7 bale sale lot, then:
3 cores * 7 bales = 21 cores
Any deviation from the 5 rules (requirements) might result in a sample failing to adequately represent the sale lot. Then no matter how well the test is performed, the result will not accurately reflect the sale lot.

## Slide 5: Sample EVERY bale
28µ
28µ
28µ
28µ
28µ
28µ
32µ
Angus Ireland
Notes: Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
Every bale must be cored. This is important as it is known that there is variation in fibre diameter between bales.
The example above demonstrates a sampling regime which doesn’t sample every bale. In this case the bale containing fibre averaging 32µm in diameter is left out of the core sample, an occurrence which would affect the result.

## Slide 6: Same number of cores EVERY bale
3
3
3
28µ
28µ
28µ
28µ
28µ
28µ
32µ
3
3
3
2
Angus Ireland
Notes: Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The same number of cores must be taken from every bale in the lot so that each bale has an equal weighting in the final test.
The example above shows a sampling regime whereby the bale containing wool with an average diameter of 32µm would be under-represented in the core sample.

## Slide 7: Random & Full Depth cores
Angus Ireland
Notes: Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The core samples must be taken at random over the base of the bale and the core tubes must penetrate the full depth of the bale to ensure that all wool in the bale has an equal opportunity of being sampled.
The example in the top left is incorrect because the coring doesn’t occur over the whole base of the bale.
The example in the bottom left is incorrect because the coring doesn’t penetrate to the full depth of the bale.