## Slide 1: Staple Sampling
Produced for the CRC for Premium Quality Wool undergraduate program by;
Angus Ireland, Australian Wool Testing Authority Ltd.
Notes: <number>
<footer>
The wool sample obtained through Grab Sampling must be sampled further to obtain staples, which are representative of the sale lot. These staples are then used to objectively measure Staple Length and Staple Strength.
This module follows on from Grab Sampling.
Produced for the CRC for Premium Quality Wool undergraduate program by Angus Ireland, Australian Wool Testing Authority Ltd.

## Slide 2: Standards
Angus Ireland
IWTO - 38 - 91:
  Method of grab sampling greasy wool from bales.
IWTO - 7 - 92:
  Sub-sampling staples from grab samples.
IWTO - 30 - 98:
  Determination of staple length & staple strength.
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The methods for sampling and testing for Staple Length and Strength are documented in Standards and Regulations maintained by the International Wool Textile Organisation (IWTO). They are listed in this slide.
In the absence of these “rules”, there could be no assurance that two different test houses would follow a consistent procedure. Consequently, if they both sampled and tested the same lot, they may use different techniques and the chances of producing similar results would be small.

## Slide 3
Angus Ireland
Tuft sampling of display sample for subsequent staple sampling
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The purpose of staple sampling is to obtain a set of 60 staples which is representative of the sale lot.
The first step in this process is performed by a machine known as a Mechanical Tuft Sampler (MTS). The MTS obtains 60 tufts of staples from the grab sample.
NB: a tuft is a bundle of wool consisting of between 1 and 10 staples.
The process involves spreading the grab samples (display sample) on a conveyor belt to a depth of about 100mm. The conveyor then steps the sample through the machine in 20 equal steps and at each step, 3 tufts are mechanically drawn.
The tufts are then rolled onto a reel where they are individually stored between successive layers of mesh.
This sequence of steps ensures that all wool in the grab samples has an equal opportunity of being sampled for tufts. Following the MTS, the reel containing the tufts is shipped to the test house.

## Slide 4: Rules to assist staple preparers obtain representative staples
Angus Ireland
“SQP”
Separate tufts into 20 sets of 3
Quickly obtain the first staple end identified
Prepare the staple by removing obvious wisps
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
At the test house the reel is unwound and one staple is manually taken from each tuft.
A set of rules has been developed as part of the procedures in the test house to ensure that the 60 staples finally obtained are representative of the lot.
The listed rules are designed for the manual operation of staple preparation. They are designed to ensure that operator bias is kept to a minimum in this sampling procedure.

## Slide 5
Wisp
95mm
100mm
10%RH = 95mm
90%RH = 100mm
Conditions
Tray
- Allows staple to recover; and
- Ensures staple is straight
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
Once staples have been sampled, they are placed in a tray to allow them to recover from the sampling procedure. The trays restrict the movement of the staple and they “set” in a straight configuration during conditioning.
Before being placed in the tray, either end of the staple is cleaned up to remove any obvious wisps of wool or vegetable matter. These wisps would interfere with Staple Length and Staple Strength results.
The staples are conditioned and tested in a standard atmosphere of 20°C and 65%RH. This is critical since changes in the level of moisture in the atmosphere will cause changes in the LENGTH of the staples (mainly from crimp changes).

## Slide 6: Assessing Representative Samples
Angus Ireland
Within laboratory trials
All preparers prepare the same lot
Between laboratory trials
Several labs routinely prepare and measure the same lots
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
At AWTA, further in-house quality control (QC) procedures ensure that operator bias is systematically checked, and action is implemented to control any bias that occurs.
The representativeness of the samples is routinely checked by two methods:
1. within-laboratory trials whereby all the preparers sample the same lot, and
2. between-laboratory trials whereby the same lot is sampled by different laboratories.

## Slide 7: Representative Sample Improvement
Angus Ireland
Prepare more staples
Use more staple preparers
Use a machine
  Automatic Staple Preparer (ASP)
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
Samples can be made more representative by a number of methods.
More staples can be prepared, although this would be more expensive.
Similarly, more staple preparers sharing the preparation of each lot, would improve the sampling but would also lead to greater costs.
A more representative sample could be obtained by using a machine as in core and grab sampling. Such a machine was trialled by AWTA in the 1980’s, however, the level of robotics available at the time proved inadequate. The machine was simply too slow.