## Slide 1: Grab Sampling
Produced for the CRC for Premium Quality Wool undergraduate program by;
Angus Ireland, Australian Wool Testing Authority Ltd.
Notes: <number>
<footer>
This module describes how a representative sample is obtained by grab sampling, and the instruments used to achieve this.
There are two (2) types of samples taken from bales; core samples and grab samples.
CORE samples are taken for all measurements of characteristics which don’t require fibre or staple integrity to be maintained such as Mean Fibre Diameter, Yield, Vegetable Matter Base and Colour. GRAB samples must be taken where full length staples are needed such as Staple Length and Staple Strength and Style measurement
Individual sale lot grab samples are combined to form a display sample. This is displayed at the selling centre to enable wool buyers to assess the unmeasured characteristics of the wool.
The sequence of wool sampling is as follows - grabbing, weighing, coring, tuft sampling and staple preparation.
Produced for the CRC for Premium Quality Wool undergraduate program by Angus Ireland, Australian Wool Testing Authority Ltd.

## Slide 2: Standards
IWTO- 38-91:
  Method of Grab Sampling Greasy Wool from Bales
The purpose of grab sampling is to obtain a sample (approx. 5kg) of full length wool which is representative of the sale lot.
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The purpose of grab sampling is to produce a bag of approximately five kilograms of full length wool (display sample) which is representative of the sale lot.
The key word here is "representative" because if the sample is not representative of the sale lot for the characteristics of Staple Length and Staple Strength, then it doesn't matter how well the testing is conducted, the results won’t accurately reflect the wool being sold.

## Slide 3: Grab Sampling Apparatus
Source : “Testing Your Woolclip”, AWTA customer brochure
Notes: Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
Source: “Testing Your Woolclip”, AWTA Ltd.. customer brochure
Grab sampling is performed by a machine. It has hydraulically operated jaws which reach through the side of the bale to obtain a handful of wool. It takes this sample with minimal contamination of the wool, either in the sample or in the bale.
This slide shows a grab sampling machine taking a “grab” from a bale. The bale covering has been cut with a hot knife before the grab arm descends into the bale.
This method of sampling produces a representative sample providing six basic rules are followed.

## Slide 4: Sampling Method
i) 20 grabs per sale lot
ii) Every bale sampled
iii) Same number of grabs per bale
iv) Same size grabs from each bale
v) Grabs randomly placed (side)
vi) Grab penetrates full width
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The grab is a mechanical arm which reaches into a bale to varying depths and takes a handful of wool.
The rules governing grab samples are similar to those for core sampling in that:
  a minimum of 20 grabs per sale lot are needed
  every bale must be sampled
  the same number of grabs must be taken from each bale
  grab positions through the side of the bale must be random; and
  the grab must be able to penetrate the full width of the bale.

## Slide 5: Sample every bale
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
i) The first requirement is that a minimum of 20 grabs must be taken from the sale lot. So, for a seven bale lot, three grabs must be taken from each bale.
Therefore the number of grabs for this lot is:
3grabs * 7 bales = 21 grabs
ii) Secondly, it is important to grab sample every bale in the lot.
It is not inconceivable to imagine the situation where, for whatever reason, the first six bales in the lot were about 90mm and the seventh was 100mm. It would be unacceptable to only grab the first six bales if this was the case.

## Slide 6: Same number of grabs
3
3
3
3
3
3
2
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
iii) Thirdly, the same number of grabs must be taken from every bale in the lot so that each bale has equal weighting in the final result.
Using the same example as before, it would be unacceptable to obtain the minimum 20 grabs by taking 3 grabs from the first six bales and two from the seventh. Clearly the full effect of the 100mm bale would not be felt in the final result. Three grabs must be taken from the seventh bale to make the sample truly representative.

## Slide 7: Grab jaw must be capable of penetrating the full width of the bale
X
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
iv) Fourthly, individual grabs must be a similar size. If grabs for the first six bales weighed 300g but only 100g for the seventh, then a non representative sample would be obtained.
v) The fifth consideration is the placement of grabs in each bale. The standard method requires the grabs be taken randomly through of the side of the bale.
vi) Finally, the grab jaw must be capable of penetrating the full width of the bale. It would be unacceptable for example, to sample only the top halves of bales.
These methods ensure that all the wool in the bale has an equal chance of being sampled.