## Slide 1: Yield Determination
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: <number>
<footer>
This module is about the determination of Yield as applied to the trading and processing of wool, and the considerations inherent in this determination. This module has been aimed at understanding the reasons behind the formulae listed in the Standards.
The questions being asked could be; How much fibre am I buying for my customer? How much fibre will I end up with at the end of my process?
The determination of Yield depends on the derivation of figures for Wool Base (WB) and Vegetable Matter Base (VMB). For further information see the “Determination of Wool Base and VM Base” module.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: What is Yield?
Peter Auer
mass of usable wool fibre obtained from greasy wool after processing
various processes
  scouring Scoured Yield
  carbonising Carbonising Yield
  carding Card Sliver Yield
  topmaking Top and Noil Yield
various Yields
various allowances
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Yield is defined as the mass of usable wool fibre obtained from greasy wool after processing.
Wool undergoes a variety of processes, e.g. scouring or topmaking. Therefore there are a number of different Yield figures which could apply to the same mass of greasy wool depending on its subsequent treatment, eg. Scoured Yield, or Top and Noil Yield. Obviously a processor who just scours will be interested in the Scoured Yield, while a topmaker would be interested in the Top and Noil Yield.
A further complication is that processors operate in different countries which have traditionally employed different figures to adjust the oven-dry weight back to a figure which reflects the weight of the fibre during use.
This Yield figure includes a Standard Regain (conditioned weight) PLUS additions for various processes (Yield).

## Slide 3: Wool Fibre Yields
IWTO Clean Wool Content (CWC)
  standard ash
  standard alcohol extractables
  standard regain
IWTO CWC = WB x 117
97.73
What are the standard levels used in this determination?
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Various Yield figures are used by different sectors of the wool industry.
Some just consider wool fibre Yields, some take into account VM content, i.e. scoured Yields, while others take in to consideration processing losses, i.e. processing allowance Yields.
Firstly the calculation of the IWTO Clean Wool Content (CWC) Yield requires;
the derived figure for Wool Base (WB)
the standard alcohol extractables are 1.7%
the standard ash content is 0.57%
the standard regain is 17%
This figure gives a calculation of the theoretical card sliver Yield at a regain of 17% with standard residues of 2.27% allowed for.
The IWTO CWC Yield figure thus obtained answers the question:
How much wool could be obtained if the lot was scoured and carded without processing loss?

## Slide 4: Further Wool Fibre Yields
Peter Auer
Japanese Clean Scoured Yield (JCSY)
ASTM Clean Wool Fibre Present
Theoretical Card Sliver Yield
Theoretical Top and Noil Yields
  Schlumberger Combed Dry (SCH DRY)
  Schlumberger Combed in Oil
  Noble Combed in Oil
  Noble Combed Dry
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Other wool fibre Yields are calculated at various regains (R) and contaminant levels, e.g.
JCSY: R% = 16%, contaminants = 1.5%
ASTM: R% = 13.64%, contaminants = 2.27%
Schlumberger Combed Dry (SCH DRY) is a standard figure considering the almost universal use of these types of combs in the industry. This is just one Theoretical Top and Noil Yield (TTNY) figure used in the industry.
TTNY figures are more complex in their determination and take into account standard regains of the top and noil, a standard tear ratio (the ratio between top and noil produced), and standard total fatty matter content (TFM).
TTNY calculations (WB x with single figure allowances) are as follows:
Schlumberger Combed Dry (1.0%TFM) WB x 1.207
Schlumberger Combed in Oil (4.6%TFM) WB x 1.257
Noble Combed in Oil (4.6%TFM) WB x 1.255
Noble Combed Dry (1.0%TFM) WB x 1.205

## Slide 5: Wool and Vegetable Matter Yields
Peter Auer
IWTO Scoured Yield at R% regain
SCD (R%) = WB x 100+R
97.73
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The above formula describes how the IWTO scoured Yield is determined.
Any regain figure can be placed in the formula, which has a standard allowance for residues of 2.27%.
This is just one example of a Wool and Vegetable Matter Yield. These apply to the scouring industry and the product they produce, scoured wool.

## Slide 6: Fibre Loss (VA) vs. VM1
0
1
2
3
4
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14
15
16
17
18
19
20
VM1 % (excluding hard heads and twigs)
VA %
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The above graph shows how the amount of wool removed during processing (VA or vegetable allowance) changes according to the amount of vegetable matter excluding hardheads and twigs (VM1).
This follows a regression equation
VA = 5.2 - 40.6
7.8 + VM1
VA (vegetable allowance) is used to determine some commercial Yields as shown in the following slides.

## Slide 7: Commercial Yields
Peter Auer
= Theoretical Yield - Processing Allowance (PA)
Schlumberger
  PA % = 2.5 + VA
Noble
PA % = 2.0 + VA
Australian Carbonising Yield
  ACY = 1.1972 WB + 0.162 V - 5.12
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Any Commercial Yield can be calculated by allowing for processing losses on the theoretical Yield. This allowance is called the processing allowance (PA)
Processing allowance (PA) increases as VA increases (see previous graph), and therefore the commercially obtainable Yield falls with increasing seed and shive and spiral burr (defined as VM1). Hard heads and twigs don’t feature in this calculation. The fear with hard heads and twigs is that they will actually damage sensitive card equipment rather than lead to fibre loss.
The processing allowance (PA) is a reflection of the likely fibre losses to be encountered in processing.
Australian Carbonising Yield (ACY)
This is another example of a Commercial Yield. This particular Yield has been derived from regression trials whereby it has been found that Carbonising Yield varies with both Wool Base and Vegetable Matter Base.
This Yield obviously applies to the carbonising industry.
ACY = 1.1972 WB + 0.162 VMB - 5.12
This formula shows that for a constant WB, an increasing VMB will result in an increasing Yield. This may seem unusual, but is really just a reflection of the efficiency of the VM removal during carbonising which falls as VMB increases.

## Slide 8: Standards
Peter Auer
IWTO -19 - 95 (E):
  Determination of wool base & vegetable matter base of core samples of raw wool.
AS/NZS 1134 (1997)
  Determination of wool base & vegetable matter base of core samples of raw wool.
IWTO Core Test Regulations
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The various formulae and calculations and tables are described fully in the above standards.