## Slide 1: Regain & Oven-dry Weight
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: <number>
<footer>
The significance of regain and its measurement is described in this module.
The use of oven-dry weight avoids the effect of the moisture content of wool during the determination of Wool Base (WB) and Vegetable Matter Base (VMB), which are then used in the derivation of Yield figures.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Definitions
regain = wt. of moisture x 100%
oven-dry weight
Yield, WB, VM base
  oven-dry weight
Invoice Mass
  standard regains applied
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Regain is defined as the amount of water in the wool expressed as a percentage of the oven-dry mass of the fibre present.
The regain of wool is influenced by the relative humidity of the ambient atmosphere since the wool fibre is hygroscopic and absorbs water from the atmosphere.
This means that the previous history of the wool will influence its weight, and stringent conditioning of wool samples is necessary to standardise the regain of wool samples before measurement.
Therefore to simplify measurement conditions, all yield, WB and VMB determinations are made on figures derived for the oven-dry weight of the fibre.
This is an easier and more accurate way of doing things, and the final figures are adjusted for standard regains to determine the invoice mass (sold mass) of the fibre. The amount of these standard regains depends on the market for the fibre. For further information see the “Yield” module.

## Slide 3: Regain vs. Humidity
Peter Auer
Source:Morton and Hearle (1962)
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source: Morton and Hearle (1962) “Physical Properties of Textile Fibres” Butterworth & Co. Ltd., London
This graph shows how the regain of wool is affected by the relative humidity of the atmosphere. If there is more moisture in the atmosphere there will be more moisture in the wool. The behaviour of other textile fibres is also graphed for comparison.
Wool can absorb up to 40% of its dry weight without feeling wet, the water is actually retained in the non-crystalline or amorphous regions of the wool microstructure.
Initially water molecules bond to the protein structure by hydrogen bonding (one molecule per site). Then more water molecules bond to these absorbed molecules (one molecule per absorbed molecule). Finally, loosely attached water molecules with no restrictions on numbers, bond to the intermediate molecules. This explains the shape of the observed curves.
The effect of moisture absorption can be observed in changes in such properties as rigidity (internal H-bonding disturbed), electrical resistance and fibre dimensions (length and diameter). These changes in moisture content can be reflected in changed textile performance (e.g. hygral expansion of fabric causing seam pucker in suiting).
This absorbed water is able to be removed by the action of heat and air-flow to determine the oven-dry mass.
It should be noted that during processing the regain of wool fibres is controlled ABOVE certain limits to ameliorate static electricity.

## Slide 4: Derivation of Conditioned Weight
Regain (R%) = wt. of moisture (M) x 100%
oven-dry weight (D)
M = R% x D
100
Conditioned Weight (C) = D + M
= D + R% x D
100
C = D ( 1 + R% )
100
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
This is an illustration of how the conditioned weight (C) can be derived from the oven-dry weight (D) and any standard regain (R).
This factor [1 + (R%/100)] can be seen in any derivation for yield where a standard regain is used. It appears as 100 + R since yield is a percentage figure.

## Slide 5: Direct Reading Regain Tester
Peter Auer
Source: ‘The Direct Reading Regain Tester’ manual
Weighing apparatus
Can containing wool sample
Dryer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source: The Direct Reading Regain Tester manual, National Instrument Co. Pty. Ltd., Jan. 1963.
This slide illustrates the machine that has been used extensively to measure the regain of wool samples.
The Direct Reading Regain Tester (DRRT) is in three parts:
the first part is a can which holds the wool during weighing and drying. The can has a mesh bottom to allow hot air to be blown through the wool sample.
the second part is a weighing apparatus which returns a reading for Regain when the sealed can of wool is first weighed on it and then dried in the third part before being weighed again.
the third part is a drying device which forces hot air through the wool sample.
An acceptable reading is obtained when the weighing part returns a steady figure.
The DRRT has been accepted as the industry standard for many years, despite the development of other methods using conductivity and resistance principles during that time.

## Slide 6: Latest Devlopments
Peter Auer
Near Infra-Red Sensing
  NIRS
Principle
  Near IR energy absorbed
    O-H “stretching”
  signal proportional to moisture content
    calibration required
Application
  scour technology
  at-line sensing
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The development of Near Infra-Red Sensing is the latest development in the monitoring of the moisture content of wool.
The basic principle is that Near IR energy is absorbed by the water molecules present which causes “stretching” vibrations of the O-H bonds in the molecule. The signal caused by this event can be measured and is proportional to amount of water present. Therefore, this method is a direct measurement of the moisture content of the wool.
The instruments need to be calibrated using a calibration equation, but the technique is not sensitive to the effects caused by the chemical processing history of the wool, namely shrink-proofing. These effects influence the results obtained using conductivity and resistance measurement techniques.
This development has been applied to at-line testing of scour output. It has been included as part of the equipment of the latest ANDAR scours.
The technique is faster and uses less wool than the DRRT method. However, a knowledge of NIRS equipment is necessary since routine monitoring and maintenance of the calibration is required, necessitating perhaps a greater level of operator training.

## Slide 7: Standards
Peter Auer
ITWO-19-95
  Determination of wool base and vegetable matter base of core samples of raw wool
IWTO-33-88
  Method for the determination of oven-dry mass & calculated invoice mass of scoured or carbonised wool
IWTO-34-85
  Determination of oven-dry mass, calculated invoice mass & calculated merchant mass of wool tops
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The above standards use the concept of oven-dry mass in their determinations of various wool properties.
In each case the wool samples must be dried to a constant weight at elevated temperatures to determine the oven-dry weight (using the DRRT).
In the latter two cases, the invoice mass can be adjusted to various standard regains once the oven-dry mass is determined.