## Slide 1: Wool Base & Vegetable Base
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: <number>
<footer>
This module is about the determination of Wool Base and Vegetable Matter Base. These figures are subsequently employed to determine the various Yield values used in the processing industry.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Wool Base (WB)
oven-dry mass of clean wool
  (free from all impurities)
impurities
  vegetable matter (VM)
  non-VM
    skin flakes, wool pack, dags, string etc.
  alcohol extractables
  ash (mineral matter)
  (water)
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Greasy wool contains wool fibre as well as impurities such as wool wax and scourable and non-scourable contaminants.
The oven-dry mass of clean wool fibre is defined as Wool Base (WB). This is expressed as a percentage of greasy wool. Clean wool is defined as being free from ALL impurities.
The amount of vegetable matter (VM) present is defined as the Vegetable Base (V), one of the main impurities present.
All subsequent yield calculations use Wool Base and Vegetable Base.
Scoured or washed wool consists of alkali soluble keratin protein and various contaminants which are largely alkali insoluble (VM and non-VM impurities).
A certain amount of wool wax also remains in scoured wool. This wax can be largely removed by extraction with alcohol. The wax also contains some amount of mineral matter.

## Slide 3: Determination of Wool Base 1
Peter Auer
Sample is prepared
  take subsamples (i) from core (weight W)
  weigh greasy wool (Wi)
  scour and oven-dry greasy wool (Pi)
  ash & alcohol extract specimens removed and weighed
Dissolve wool
  dissolve weighed wool in alkali
  VM, others in residue
Consider Residue
  dry and separate (VM and others)
  weigh VM residue (Vi) & weigh other residues
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Sub-samples (~150g each) are randomly selected after the initial core sample has been weighed.
After scouring with either a non-ionic detergent or soap and soda-ash the oven-dry weight of the scoured sample is obtained (Pi). (The moisture content of the drying air is corrected for ambient relative humidity and temperature.)
Test specimens for ash content and alcohol extractables and alkali insolubles are removed within 60 seconds from each oven-dry subsample.
The test specimen for alkali extractables is transferred to a dissolving vessel containing boiling NaOH (10% w/v). This solution completely dissolves the wool fibre, but leaves the residue relatively unscathed (some is dissolved which is accounted for by calibration factors).
The residue contains VM, and other alkali insoluble material such as minerals, skin flakes and synthetic material (woolpacks, string etc.).
The VM component is sorted into (i) hardheads (burrs) and twigs , (ii) spiral burr and (iii) seeds, leaves and grasses.
A subsample of the residue is tested for ash content (mineral matter).
The remaining residue is sorted and weighed.

## Slide 4: Determination of Wool Base 2
Peter Auer
Adjust Residue Value
  ash content of residue (separate test)
  allow for alkali dissolving (correction factors)
Calculate total alkali insolubles (Ti %)
  compared to Pi
Determine Ash content by burning (Ai%)
  @ 750 degrees C
  compared to Pi
Alcohol extractable matter (Ei %)
  compared to Pi
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The alkali does dissolve some of the residue so allowances are made for the amount of VM and other material dissolved in the alkali. The Total residue value is adjusted upwards.
Allowance is also made for the ash content of the Total Residue which is determined in a separate test and subtracted from the Total Residue value. Finally the derived value for Total Residue (Ti) is used in the determination of Wool Base.
The derivation of values for Ash Content (Ai) and Alcohol Extractable matter (Ei) are described in the following two slides.
Ei, Ai, Ti are expressed as percentages of the oven-dry weight of the test specimens drawn from the scoured subsample, i.e. compared to Pi.

## Slide 5: Alcohol Extractable Matter
Source : “Testing Your Woolclip”, AWTA customer brochure
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source: “Testing Your Woolclip”, Australian Wool Testing Authority Limited, customer brochure
This slide shows the set-up for a block of Soxhlet extractors used in the determination of Ei (alcohol extractable matter).
The principle of Soxhlet extraction is explained in the next slide.

## Slide 6: Soxhlet Extraction
alcohol
sample
condenser
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The scouring procedures used in the determination of Wool Base are more efficient than commercial scouring but still leave a residue of wax which is typically <1%.
Alcohol extraction using Soxhlet apparatus determines the amount of alcohol extractable material (Ei).
A sample of wool is flushed with alcohol in a self-recirculating chamber for a minimum 20 cycles. The Alcohol Extractable material is flushed into a glass container below which is dried and weighed before and after the extraction. The mass of wax is determined by difference and Ei is calculated compared to Pi.

## Slide 7: Ash Content
Source : “Testing Your Woolclip”, AWTA customer brochure
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source: Testing Your Woolclip”, Australian Wool Testing Authority Limited, customer brochure
Ash content is a measure of the mineral matter remaining after scouring.
The temperature used in this determination (750°C) means that all carbonaceous material is vaporised, and only mineral matter remains.
The mass of ash is determined by weighing each crucible before and after burning and Ai is derived by comparing this to Pi.

## Slide 8: Wool Base Formulae
Wool Base (Bi) by difference
for each subsample (i)
Bi = Pi (100 - Ei - Ai - Ti) %
Wi
for whole sample
WB = Wb  Bi Wi
W  Wi
  Wb is total subsamples plus remainder
  at least 2 subsamples >150g
  blending factor (Wb/W) allows for weight loss during blending and subsampling
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Wool Base for each subsample (Bi) is determined by difference and multiplying by scoured oven-dry weight / greasy weight (i.e. Pi/Wi). Obviously from the formula, if Ti, Ai and Ei are zero then Bi would be simply the ratio between scoured oven-dry weight and greasy weight (Pi/Wi).
To compensate for any changes in mass between the initial core sampling and the subsampling a blending factor is used in the calculation of Wool Base (WB).
Essentially this is the mass of subsamples and remainder (Wb) divided by mass of sample as received (W).
Each value of Bi is then adjusted for differing subsample weights and WB is calculated.
At least 2 subsamples are tested, however if the range of results from these subsamples is greater than specified, then further testing is required. (These range checks are derived from the determined variance between cores, laboratories and subsamples, i.e. the total variance of Wool Base as determined by Round Trials over time.)

## Slide 9: Vegetable Matter Base
alkali-insoluble residue sorted
VM Content (Vi)
  Hard heads and Twigs (Hi)
  Spiral Burr
  Seeds and Shive
V = Wb Vi Pi
W  Wi
H = Wb  Hi Pi
W  Wi
Peter Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Figures need to be derived for Vegetable Matter Base (V) and related quantities in order to calculate yields.
The alkali-insoluble residue is sorted into various VM and non-VM categories.
The total vegetable matter mass (Vi) includes:
i) hard heads (ring burrs, Noogoora burrs, Bathurst burrs and similar), twigs (sticks, leaf stalks, woody material) (Hi)
ii) spiral burrs
iii) seeds and shive
The derivation of V and H (Hard Head Base) proceeds in a similar manner to the derivation of WB, as shown by the similar formulae.

## Slide 10: VM in Processing
Source: AWTA booklet
Hard-to-remove
Easy-to-remove
© Australian Wool Testing Authority Limited
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Source: “Vegetable Matter in Australian Wool”, Australian Wool Testing Authority Limited booklet
This diagram illustrates the various VM types found in raw wool. Easy-to-remove VM types are outlined in red.
VM contaminants vary in the ease with which they can be removed from the fibre. Due to the finer and more supple nature of things such as spiral burr and seeds and grasses and the like, these types of VM are difficult to remove in carding. Therefore they tend to be transferred through gilling to the combing stage where they are largely taken out (about 96% is removed).
However, removal at this stage inevitably leads to fibre losses, and the amount of VM of this type is taken into account in calculating worsted processing yields.
These types of VM are defined separately as VM1 in yield determinations.
It should also be remembered that the regain of the VM during carding has been found to be critical with regard to the size of particles in the card sliver, small particles being more likely to pass through to the combing stage and into the top.
Easy to remove VM is taken out at the carding stage by burr beaters, and only poses a problem when too great a percentage may cause some particles to advance into the swifts and damage delicate card wires. They do not cause any significant fibre loss.

## Slide 11: Standards
IWTO -19 - 95 (E)
  Determination of wool base & vegetable matter base of core samples of raw wool.
AS/NZS 1134 (1997)
  Determination of wool base and vegetable matter base of core samples of raw wool.
IWTO Core Test Regulations
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The various formulae and calculations and tables may be found fully in the above standards.