## Slide 1: Components of Variation of Fibre Diameter
Produced for the CRC for Premium Quality Wool undergraduate program by;
Michael Bow, retired, CSIRO Division of Wool Technology and,
David Petrie, The University of New South Wales,
Notes: In the early stage processing of wool, considerable effort is expended blending and homogenising the raw material with respect to diameter and other characteristics. The fibre diameter of the top is a primary customer requirement.
However, an understanding of the way diameter and its distribution is built up from the staple to the 20 (or 200) tons of wool in processing batches is useful in understanding sampling concepts and the interpretation of the measurement of diameter for breeding, sale and assembly of processing batches. This module examines these concepts.
Produced for the CRC for Premium Quality Wool undergraduate program by Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.

## Slide 2: Sources of Variation
Coarsest : Finest = 4 : 1
Genetics and Environment
  BETWEEN fibres within a single staple
  ALONG fibres
  BETWEEN staples
  BETWEEN positions on a single sheep
  BETWEEN sheep
Changes
  Average (mean)
  Variability (SD, CV)
M. Bow & D. Petrie
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
The ratio of the coarsest to finest fibre diameter can be over 4 to 1, whether the fibre is in a staple, a fleece or sale lot.
Most of the variability of fibre diameter, about 80%, occurs within a single staple. Diameter differences between fibres growing from adjacent follicles can be over 20 microns.
This is because sheep have primary and secondary follicles that are set prior to birth. Merino sheep have secondary to primary follicle ratios of 15:1 or higher. No other breed has S:P ratios this high. Therefore, variability is mainly due to variation in the secondary fibres since these predominate. This source of variation is a genetic effect.
For more information on follicles and follicle density see modules relating to follicle/ structure and follicle/ wool growth in the Wool Biology section of the database. More details on fibre diameter variation and within fleece gradients can be found in the Wool Production modules titled “Fibre diameter variation defined” and “Within-fleece gradients in diameter variation”.
The next few slides will look at other sources of variation.

## Slide 3: Along Fibre - Staple Profile
50
20
40
2mm Position from Tip
% of Fibres > 30 µm
30
20
25
6
4
30
20
10
0
10
30
Standard Deviation (µm)
Mean Diameter (µm)
M. Bow & D. Petrie
Source: Bow, M.R. & Hansford, K.A. 1994
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Source: Bow, M.R. & Hansford, K.A. (1994) Fibre Diameter Variability, Proc. Woolspec 94
Between shearings, stresses from physiological and environmental changes can cause a single fibre to vary by as much as 6 - 8 microns ALONG its length. Causes include pregnancy and lactation, disease and seasonal nutrition. Under extreme stress fibre production can cease, reducing the fibre diameter to zero.
The figure above shows how the change of diameter along the length usually produces a significant position of minimum fibre diameter. During processing, particularly carding, fibres will preferentially break at this point. The degree of diameter reduction and its position are the major components in the measurement of staple strength (SS) and staple position of break (POB).
The second effect of a change of diameter ALONG the length of fibres is a change in the value of Standard Deviation (SD) of the distribution. If the sampling allows all parts of the fibres to be equally represented, as is the case in coring or minicoring, the resultant SD is the sum of the BETWEEN and ALONG fibre variability in diameter. This is the case in samples tested commercially for fibre diameter.
However if a sample is cut (by guillotining) across staples at one period of growth only the BETWEEN fibre variability is represented. This is the case in the Staple Profiles shown above. The SD at any one point indicates the between fibre variation at that point in the staple.
Remember that the largest part of the variation in diameter is expressed in the staple (about 80%).

## Slide 4: Between Staples
M. Bow & D. Petrie
Source: Bow, M.R. & Hansford, K.A. 1994
MEAN 23.3 µm
CV 22.1%
Fibre Diameter (µm)
Frequency (%)
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Source: Bow, M.R. & Hansford, K.A. (1994) Fibre Diameter Variability, Proc. Woolspec 94.
The above figure demonstrates a further complication to the determination of wool fibre diameter. The diameter frequency distributions of fibres from two different staples are shown.
The mean fibre diameter of the top distribution is 17.5m, the bottom is 23.3m. The CV of fibre diameter is around 22% for both distributions.
This figure demonstrates that no two fibres are alike, but form a distribution of diameters at any level of aggregation, even in a staple.

## Slide 5: Diameter Variation over Sheep
22.0
22.1
21.4
21.5
22.3
20.8
23.0
23.3
23.2
M. Bow & D. Petrie
Source: Young and Chapman, 1958
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Source: Young, S.S.Y. and Chapman, R.E. (1958). Aust. J. Agric. Res. 9:363
A number of studies, mainly on medium diameter Peppin types, revealed an average pattern for mean fibre diameter that is finer at the shoulder and becomes coarser at the breech. These changes can be 2 microns and more.
It is important to remember that this is an average pattern, individual sheep may have different degrees of the pattern or another pattern altogether.
The midside sample is regarded as being most representative of the whole fleece for measured wool characteristics.
Recent data at the CSIRO Textile and Fibre Technology suggests that in superfine animals the midside sample may on average be the finest portion of the fleece.
The study of the patterns of diameter over sheep, the variability and correlations between them are necessary so that the selection of samples for fibre diameter measurement in breeding programs are representative.
Diameter variability can also change with position. Wool from the breech or thigh is more variable than wool from the shoulder. Wool on a fold is more variable than wool in a fold.

## Slide 6: Individual Merinos
Mean Fibre Diameter (µm)
Standard Deviation (µm)
14
16
18
20
22
24
26
28
0
1
2
6
7
8
5
4
3
M. Bow & D. Petrie
Source: Bow, M.R. & Hansford, K.A. 1994
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Source: Bow, M.R. & Hansford, K.A. (1994) Fibre Diameter Variability, Proc. Woolspec 94.
The figure above plots the relationship between mean fibre diameter and SD of fibre diameter for 737 Merino sheep of varying diameter. A red regression line is fitted to this data.
The equation for the regression line is:
SD = 0.25 (mean fibre diameter) - 1.19
It can be seen that as mean diameter increases so does the SD. The reason for this is not known, but it is possibly related to the mechanisms of follicle development.
The spread of values about the regression line is due to the inclusion of the ALONG fibre component of diameter variation which changes with environmental factors, as well as being inherent to the fibre.
Because of this relationship between mean fibre diameter and standard deviation, it is common for the coefficient of variation to be used in comparing diameter variability in sheep of differing average diameter.

## Slide 7: Individual Corriedales
Standard Deviation (µm)
Mean Fibre Diameter (µm)
Merino
Corriedale
M. Bow & D. Petrie
Source: Bow, M.R. & Hansford, K.A. 1994
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Source: Bow, M.R. & Hansford, K.A. (1994) Fibre Diameter Variability, Proc. Woolspec 94.
The relationship between fibre diameter and SD of fibre diameter may vary in slope for different breeds. In this figure results from 79 Corriedale sheep are overlaid on the regression line for Merino sheep.
The equation for the regression line is:
SD = 0.20 (mean fibre diameter) - 0.23
Again environmental factors are apparent in the spread about the regression line.

## Slide 8: Sale Lots
Standard Deviation (µm)
Mean Diameter (µm)
Merino Sheep
Sale Lots
M. Bow & D. Petrie
Source: Bow, M.R. & Hansford, K.A. 1994
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Source: Bow, M.R. & Hansford, K.A. (1994) Fibre Diameter Variability, Proc. Woolspec 94.
The next stage for consideration is the distribution of mean diameters of sheep in a flock (or mob). A mob consists of animals that are genetically similar and have been subjected to the same environmental conditions between shearings. After shearing and classing the fleeces of these animals will be put together as a lot of bales for sale (called a sale lot).
Fine and superfine flocks show a range in mean fleece diameter of about 5 microns. The range for medium Merinos can be 8 microns or more.
The distribution of mean diameter in a mob is very close to normally distributed.
Classing will not modify the value of the diameter distribution by a great deal because of the poor relationship, particularly in fine wool, between staple crimp frequency and mean fibre diameter. The classer uses this relationship to class the wool according to diameter, but while a general relationship does exist over a wide range of breeds and strains, the correlation within a mob is poor.
It should be noted that this between animal variability contains the genetic variability that allows for breeding selection to change the average diameter of the flock.
The lotting of fleeces of varying mean diameter increases the overall SD of the diameter distribution. This can be seen in above diagram where results from 156 sale lots have been plotted. It can be seen that the average value of SD for sale lots (purple line) is greater for all diameters than that for individual sheep (dashed red line).

## Slide 9: Consignments
Mean Diameter (µm)
Standard Deviation (µm)
Sale Lots
Consignments
M. Bow & D. Petrie
Source: Bow, M.R. & Hansford, K.A. 1994
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Source: Bow, M.R. & Hansford, K.A. (1994) Fibre Diameter Variability, Proc. Woolspec 94.
The final aggregation of wool that occurs before processing is begun is the combination of sale lots into processing batches. Another factor governs what occurs in this process.
For Australian wool virtually all sale lots are measured for mean diameter before they are put into processing batches. The requirements of processors and the realities of wool value and trading, which is another whole subject, tend to cause batches to be made of sale lots with values of mean diameter close together, usually within 0.5mm for fleece wool. The inclusion of skirtings and crossbred wool may increase this range to 1 or 2 mm.
The effect of this on SD in processing batches can be seen in the above figure. The slope of the (black) regression line for processing batches is higher than the line for sale lots.
Not all batches may be put together with a small distribution in mind. For example, a wide diameter distribution will achieve a "Harris Tweed" fabric.
There are other factors that affect the sampling and measurement of diameter. In most wool there is a relationship between diameter and length. Coarser fibres are longer. This means that with most of our sampling methods, the mean value is "length biased”, i.e. it is very slightly coarser than the true numerical average of the fibres. The homogeneity of scoured lots will be different to greasy sale lots and for the same sampling schedules the precision would be different.
Diameter does not exist alone. While it may be the most important specification of raw wool, decisions on value, batching and processing will of necessity include many other specifications.

## Slide 10: Summary
Source of variation Variance (µm2)
Sound Tender
Between fibres within a staple 16 (64%) 16 (43%)
Along fibres within a staple 4 (16%) 16 (43%)
Between staples within a fleece 1 1
Between fleeces within a classed line 3.5 3.5
Between classed lines within a mob 0.5 0.5
Total Variance 25 37
M. Bow & D. Petrie
Source: Whiteley, K. W. 1972
Notes: Written by: Michael Bow, retired, CSIRO Division of Wool Technology and David Petrie, The University of New South Wales.
Source: Whiteley, K.W. (1972), Some Observations on the Classing of Fleeces for Fineness, Wool Technology & Sheep Breeding, Vol. 19(2), Dec.
The table above is a summary of the sources of fibre diameter variation, for both sound and tender lots.
This table shows that the between fibre variation within the staple has the greatest influence on fibre diameter variability in sound lots. However, within a tender lot, both the between fibre and along fibre variation have significant effect.