## Slide 1: Introducing :Fibre Curvature
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Paul Swan, Paul G. Swan and Associates.
Notes: This module is designed to introduce the concept of fibre curvature. Items such as the definition of curvature, the measurement of curvature and its importance to the wool industry are covered.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Paul Swan, Paul G. Swan and Associates.

## Slide 2: Fibre Curvature
Paul Swan
Source: Rossouw 1931
Section of
Merino wool fibre
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
Source: Rossouw, S.D. (1931), Journal of the Textile Institute, 22 T374
Fibre Curvature represents a new technology for measuring the crimp of wool fibres. Unlike conventional assessments of wool crimp such a Quality Number, Curvature measurements can be applied at any stage of the wool-processing pipeline, from fleece to fabric.
Curvature is basically a measurement of how much the fibre bends along an average standard short length of the fibre. To illustrate this, the figure in this slide represents a section of Merino wool fibre under the microscope.
It is important to note that wool fibres do not usually curve in one plane. There is a certain amount of torsion present.
Curvature relates strongly to the old Quality Number system for greasy wool, which used to be the basis of wool trading. In the Quality Number system the number of crimp waves along a length of the staple is estimated to assess how often the fibre crimps. This relates to how fine the curves are along the fibre.

## Slide 3: Comparison of crimp frequency
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
To measure Fibre Curvature, imagine a section fibre being physically ’chopped’ into short sections, imaged, and then further subdivided by an image analysis system. It is a simple matter then to measure how much the fibre curves or bends along its’ length.
The figure on this slide shows separate sections of 80’s and 56’s Quality Count fibres, superimposed with lines representing the points where the fibres are ‘chopped’. Once fibres have been subdivided into short sections, it is a simple matter to measure the degree of curvature of the fibre.

## Slide 4: Degree of curvature
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
This figure shows magnified views of short (0.4 mm) sections of the “chopped” fibres (from the previous slide).
Both of these fibre sections are the same length, but differ markedly in their degree of curvature. The 80’s count section is much more highly curved than the 56’s count section, correlating to the number of crimps per inch along the staple.
To specify curvature, we measure the angle (Ø) specifying the fibre section. This is expressed as degrees of curve per millimetre along the fibre.

## Slide 5: Crimp frequency vs curvature
0
20
40
60
80
100
120
140
160
0
5
10
15
20
25
Staple crimp frequency (crimps per inch)
Average fibre curvature (deg/mm)
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
Fibre Curvature relates closely to Quality Number and Staple Crimp Frequency. Wools of high Quality Number have high fibre curvature, and vice versa. For example, most strong wools have curvature of less than 80 degrees/mm, whereas most superfine wools have curvatures in excess of 110 degrees per mm.
This figure demonstrates this relationship for a combined data set of Australian and New Zealand wools, where staple crimp frequency and fibre curvature are plotted. These measurements were performed using the Optical Fibre Diameter Analyser (OFDA).

## Slide 6: Crimp & fibre curvature
Quality
No.
No. crimps
per inch
Fibre
Curvature
(
o
/mm)
100s up
> 23
> 140
90's
19 – 22
130 - 140
80's
18 - 19
120 - 130
74's
17 - 18
115 - 120
70s
15 – 17
100 - 110
64's
13 – 15
85 - 100
60's
10 – 13
75 - 85
56's
8 – 10
65 - 75
48's
5 – 8
45 - 65
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
Clearly, there is a strong association between the mean fibre curvature and visual staple crimp frequency. Wools of higher visual staple crimp frequency or count tend to have higher average fibre curvature. This is because the individual fibres need to be more highly curved to make a shorter, more frequent wave.
The table in this slide illustrates this point by showing the likely relationship between the Quality Number system, the number of crimps per inch, and Fibre curvature (as measured using the New England Fibre Testing Pty. Ltd. OFDA).
The beauty of the curvature measurement is that it can be applied throughout the processing pipeline. In this way, curvature will allow later stage processors greater control over fibre quality, and will help us re-establish the quality communication links from grower to tailor, so evident in the wool industry prior to the 1960’s.
It should be noted that while curvature is retained throughout the processing pipeline, the stresses imposed on the fibre need to be relaxed before the fibre curvature at different processing stages can be measured for comparison purposes.

## Slide 7: Why is fibre curvature important?
relates strongly to the curvature of the follicle in the skin, an important genetic lever
relates to staple length and fleece weight
affects top making efficiency, and top tare ratio
influences yarn spinning efficiency and yarn evenness and quality
affects fabric thickness, handle, lustre, and efficiency of dyeing
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
Fibre Curvature measurements have the potential to become a widely used fibre specifications throughout the wool processing pipeline.
This is because Fibre Curvature:
relates strongly to the curvature of the follicle in the skin, an important genetic lever; since follicles of lower curvature produce quicker growing fibres.
consequently relates to staple length and fleece weight; since follicles of low curvature tend to produce longer staples and heavier fleeces.
affects top making efficiency, and top tear ratio; a reduction in fibre curvature at any micron is associated with increased efficiency.
influences yarn spinning efficiency and yarn evenness and quality; a reduction in fibre curvature at any micron improves yarn evenness.
affects fabric thickness, handle, lustre, and efficiency of dyeing; low curvature is associated with softer, sleeker, and of greater depth of shade.

## Slide 8: How should fibre curvature be used?
True to Type
Increasingly
soft and
efficient to
process
Increasingly
harsh and
inefficient to
process
Fibre
Curvature
Fibre Diameter
True - to - Type
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
When interpreting Curvature results, it is paramount that these be compared to the average diameter, to determine what is truly fine crimping or truly broad crimping.
The above figure gives a rough idea of how processors might use the new curvature information. Knowledge of the diameter:curvature combination for particular wools will tell processors of the suitability of the wool for particular uses, and provide useful clues as to how likely it is that the wool will be efficiently processed and soft.
The increased usage of curvature measurements by industry will depend on a number of factors:
the ability of the wool growing industry to supply wool differentiated on Curvature in sufficient quantities to regularly meet the industrial needs of the topmaker.
if retail products are available wherein the market advantage of differing fibre curvature is proven.
if the processing advantages of low curvature wool can be demonstrated at the spinning stage, whereby spinners will specify Curvature in their orders for top.

## Slide 9: Assessing wool
Fibre
Curvature
(deg / mm)
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
A simple tool for assessing adult wool (> 2 y/o) is shown in the this table, and roughly defines the Diameter:Curvature combinations for ‘true-to-type’ and potential low curvature wools. This Table has been developed in conjunction with New England Fibre Testing Limited (Walcha) and wool processors, and should enable processors to identify desirable combinations of diameter and curvature in order to create distinctive product properties (handle, drape, brightness, coverage etc.) to target for particular market niches.
Please note that for immature sheep (still laying down bone and muscle), the fibre diameter is generally 1 – 2 microns lower than the eventual adult diameter, even though the crimp characteristics of the wool generally change little after weaning. For this reason, the above relationship does not apply directly for young sheep – for any given fibre diameter, the curvature is usually 10 – 15 degrees per millimetre lower than that for adult wool.
It is also important to note that particular combinations of measured diameter and curvature are not sufficient to identify low curvature wools – other attributes of the wool are also important. Consider the case of doggy wool which has a low curvature for its’ diameter. Manufacturers need additional information, other than simply diameter and curvature, to distinguish these very different wool types. This is where the standard deviation of curvature can help.

## Slide 10: Standard deviation of curvature
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
Wool fibres vary in their crimp characteristics in several ways; along their length, between fibres, and between age groups (e.g. lambs wool versus adult wool). As a result, when one looks at wool fibres under a microscope, variation in the degree of curvature always appears. This can be quantified, in the same way we quantify the spread of fibre diameter.
The figure in this slide shows a microscopic view of 0.5 mm fibre snippets on a glass slide (at around 30 times magnification). These snippets were produced from a 22 micron woollen-spun yarn, by chopping the yarn in a guillotine. Clearly visible is a wide range of curvature of the individual snippets. This is no surprise given the different wools that would have been blended to produce this yarn.

## Slide 11: OFDA curvature histogram
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
The OFDA system automatically measures the distribution (or histogram) of fibre curvature, and produces a standardised measurement of the spread of curvature, called the standard deviation. What this means is how spread out the histogram is – the higher the standard deviation, the broader the spread.
Above is an example of an OFDA curvature histogram. According to the OFDA programming, the standard deviation equals the distance one has to travel on either side of the mean to encompass 66% of all of the observations. So, if it is a more spread out distribution, one has to travel further to collect 66% of the values.
It is interesting to note that the Laserscan, having only 9 possible curvature ‘bins’, does not produce this information on fibre curvature variation.
For the Fine wool sample shown, the average fibre curvature is 94.7 º/mm, with a standard deviation of 47 º/mm. The curvature values are in 8 º/mm increments, starting at zero (i.e. straight fibres at the top), and increasing down the page.
It should be emphasised that the term “standard deviation” is properly a measure of the variation of a population that is distributed normally, i.e. the same proportion of the population is found either side of the mean or average value. Work to date would indicate that the distribution of fibre curvature is not normal. Care should be exercised when using the term “standard deviation” to describe the variation in fibre curvature of a sample.

## Slide 12: Relationship between mean curvature & SD
20
30
40
50
60
70
80
90
0
20
40
60
80
100
120
140
160
Mean Fibre Curvature (deg/mm)
Std. Deviation of Curvature (deg/mm)
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
For fibre curvature, there is a general relationship between the mean curvature and the standard deviation – as the average curvature goes up, so to does the standard deviation. This is shown on the figure on this page. The data set shown includes both Merino and Alpaca samples, as well as tops, yarns, and fabrics.
Obviously, when trying to interpret the standard deviation of curvature, one needs to consider the value of the mean. For example, for Superfine wools (curvatures generally > 110 degrees/mm), one should expect to observe values for the standard deviation of in excess of 60 degrees. For Alpaca (curvature generally < 50 degrees/mm), our expectations as far as the standard deviation goes are much lower.

## Slide 13: Crimp definition
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
So, what possible use is the standard deviation of curvature?
Research conducted by the author while at CSIRO indicates that as the standard deviation of curvature increases, crimp definition (character) in greasy wool decreases.
This makes sense, since it is difficult to pack fibres close together (to form a deep crimp) if they vary in curvature.
This slide demonstrates this point.

## Slide 14: Fibre alignment
Good
Poor
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
Poorly aligned fibres make for poor character staples, blocky staples, and poorer early stage processing performance (the fibres are already entangled before scouring).
The picture above graphically illustrates this concept, using actual microscope images of wool staples taken by the author while at CSIRO.
The staple on the left is of reasonably good character, with fibre bundles peeling off the staple bulk. A closer examination (far left) shows that the fibres are generally well aligned within this staple, which must occur to form a deep, readily seen crimp wave. This is what is found in wools displaying excellent character.
The staple on the right is of poor character, and originates from the Northern Tablelands of NSW. The fibres within this ‘flat’ wool are poorly aligned, and of varying degrees of curvature.

## Slide 15
Std. Dev.
of
Curvature
Average Curvature
DEEPER
crimp
FLATTER
crimp
AVERAGE WOOLS
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
So, the general rule is that whatever the curvature, the lower the standard deviation of curvature, the better (i.e. better character, better processing efficiency).
However, one must take account of the general relationship between the average curvature and the standard deviation of curvature. This is shown schematically in the diagram on this slide.
At any given mean curvature, high values of the standard deviation will tend to reflect the wools of flatter, less defined crimp character. By comparison, at the same mean curvature, lower values of curvature will tend to reflect better, deeper crimp character.

## Slide 16: Word of caution
Curvature is a new technology
OFDA and Laserscan measurement techniques to be perfected
International standards to be established
More research required
Paul Swan
Notes: Written by: Dr. Paul Swan, Paul G. Swan and Associates.
Finally, a word of caution. Curvature is a new technology, and consequently, the OFDA and Laserscan measurement techniques have yet to be perfected and international standards established.
Nonetheless, it is not expected that this process will yield major changes to average values of fibre curvature; rather precision will most likely improve, and differences between laboratories, evident at present, should diminish.
Consequently, it is important that caution be exercised with the use of measured fibre curvature at this stage. Woolgrowers and wool processors are beginning an apprenticeship with what is a new and very powerful tool.