## Slide 1: Staple Length Staple Strength
Produced for the CRC for Premium Quality Wool undergraduate program by;
Angus Ireland, Australian Wool Testing Authority Ltd.
Notes: <number>
<footer>
This module outlines the procedures and instruments used in the objective measurement of Staple Length (SL) and Staple Strength (SS).
Produced for the CRC for Premium Quality Wool undergraduate program by Angus Ireland, Australian Wool Testing Authority Ltd.

## Slide 2: Methodology
Angus Ireland
IWTO- 38 Grab Sampling
IWTO- 7 Staple Sampling
IWTO- 30 Length & Strength Measurement
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
After conditioning, the staples sampled from the GRAB sample are ready to be tested for Staple Length (SL) and Staple Strength (SS). This module follows Staple Sampling.
The procedures outlined in IWTO - 30 are followed to test for SL and SS.

## Slide 3
Measuring staples for
length & strength
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The name of the machine that measures SL and SS is the Automatic Testing of Length and Strength (ATLAS). It was developed by the CSIRO Division of Textile Physics.
The ATLAS does three things. It measures the length of a staple, it measures the force required to break the staple in half, and it weighs the two halves of the staple.

## Slide 4: Length Measurement
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The principle of length measurement on ATLAS is to convey the staple through a light beam at a fixed speed. The length of the staple is determined by relating the speed of the conveyor to the amount of time the light beam was interrupted by the staple.
The process is in fact a little more sophisticated than this explanation suggests because there are actually eight beams of light (Light Emitting Diodes) aligned vertically across the conveyor belt with eight photocells opposite them to detect the beam. These eight beams allow more accurate detection of the beginning and end of the staple. For example, there are always a few fibres protruding from either end of the staple and it would be clearly wrong to add these to the measured length of the staple.
When a staple moves between the light source and the photocells it reduces the amount of light falling on a number of them. Length measurement starts when at least one cell can see less than 50% of the light from its corresponding beam. Similarly length measurement stops when all eight cells can see more than 50% of the light from their corresponding beams.

## Slide 5: Force Measurement
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
Following length measurement, the staple is picked up between twin rubber belts and fed to the strength section.
The tip of the staple is gripped by one jaw and the base by another jaw and then the staple is broken in half and the peak force required to do this is recorded in Newtons.
The amount of staple held by the jaws is approximately 25mm of the total length of the staple, consequently any staple less than 50mm would have little of the staple free to break as the jaws moved apart. The peak force recorded in such a case would not be an accurate measure of the strength of that staple. Consequently, a strength result is not reported for staples shorter than 50mm.

## Slide 6: Staple Mass
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The diagram above illustrates to the sample weighing part of ATLAS.
Each half of the broken staple is released from its jaw and blown down a tube to a balance underneath where it is weighed. The sum of the two weights is used to calculate the Staple Mass.
Broken staples are weighed and then compressed air blows the portions to a collection vessel.

## Slide 7: Calculating Staple Strength (N/ktex)
Staple Mass (g)
THICKNESS = _____________________
(ktex) Staple Length (M)
UNCORRECTED Force (Newtons) STRENGTH = _____________________ (N/ktex) Thickness (ktex)
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The Force (Newtons) required to break the staple is meaningless unless the Thickness (linear density) of the staple is known. All other things being equal, a thick staple is harder to break than a thin staple.
Thickness is reported in units known as Kilotex (ktex) (actually g/m). The calculation for Thickness uses Staple Mass and Staple Length values.
It is then possible to calculate the uncorrected staple strength. This calculation uses Force values and the derived Thickness value.

## Slide 8: Corrected Strength equals
Uncorrected Strength * 100
Strength factor * Staple yield
Where:
Strength Factor = 1.36704 - 0.006936WB + 0.06126Type
Staple Yield = 0.83WB + 0.314VMB - 6.18Type +29.6
Fleece Type = 1
Skirting Type = 0
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The next step is to convert the uncorrected staple strength to a corrected value.
This is necessary because when the staple mass was determined the staple was in the greasy form. A greasy staple contains dust, lanolin and some vegetable matter which all add to the Staple Mass. This causes the linear density to be overestimated and the strength to be consequently underestimated. The lower the yield of the wool, the greater the underestimation of staple strength.
Strength is corrected using the formulae shown above. Research has shown that Wool Base (WB), Vegetable Matter Base (VMB) and wool type (Type) (i.e. fleece or skirting) are all required to correct staple strength.

## Slide 9: Position of Break (POB)
0.1g
0.3g
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
The third piece of useful information that can be obtained from ATLAS is the position where each staple broke.
Staples break at their weakest position, which is usually at their thinnest point (point of minimum linear density).
This position can be determined because the weights of the tip and base portions of the staple are known. This is possible because the staples all enter ATLAS in the same direction.
If the tip is light and the base is heavy, the position of break will be close to the tip.

## Slide 10: Significance of POB
Longer Hauteur
Shorter Hauteur
Angus Ireland
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
Position of break is reported as the percentage of staples which broke in the tip, middle and base thirds of the staple.
This information is used, together with Staple Length and Staple Strength and other characteristics, in the prediction of fibre length in the combed wool, Hauteur. The combed fibre length will be longer if the position of break is near the end of the staple because a significant length of more sound wool remains after the initial breakage. The combed fibre length will be shortest where the position of break is in the middle of all staples as both parts of the staple are relatively short, and are retained in combing.

## Slide 11: Summary
Angus Ireland
Purpose
Prediction of fibre length after combing (Hauteur)
Indication of tear ratio
Methodology
Grab Sampling (representative)
Staple Sampling (representative)
SL & SS Measurement (accuracy)
Notes: <number>
<footer>
Written by: Angus Ireland, Australian Wool Testing Authority Ltd.
In summary, SL, SS and POB are measured so that fibre length after combing (Hauteur) can be predicted, and also an indication of the product (Top) to waste (Noil) ratio (commonly known as the tear ratio) can be estimated.
The sequence of Grab sampling, Staple Sampling and SL & SS measurement is essential for this information to be available to interested buyers.